Activated Biochars from Heavy Metal-Contaminated Biomass for CO2 Capture: Adsorption Performance and Dominant Mechanisms

Nastaran Abbaspour*, Christian Jordan1, Gregor Tondl2, Patrycja Wąsik1,3, Towhid Gholizadeh4, Daniela Tomasetig5, Andrzej Szlęk3, Christoph Pfeifer2, Michael Harasek1, Agnieszka Korus3, Franz Winter1

1 Institute of Chemical, Environmental and Bioscience Engineering, TU Wien, Vienna, Austria

2 Institute for Chemical and Energy Engineering, University of Natural Resources and Life Sciences, Vienna, Austria

3 Department of Thermal Technology, Silesian University of Technology, Gliwice, Poland

4Department of Power Engineering and Turbomachinery, Silesian University of Technology, Gliwice, Poland

5 Institute of Chemical Technologies and Analytics, TU Wien, Vienna, Austria

List of contents:

S1. Raman spectrum of selected  pine and birch biochar

S2. XPS survey for selected pine and birch activated biochar

S3. Pore size distributions of pine and birch biochars activated at 800 ℃

S4. Measured isotherms and model fittings for selected samples

Tables:

ST1. Content of inorganics in birch harvested from the contaminated and uncontaminated areas

ST2. Content of inorganics in pine harvested from the contaminated and uncontaminated areas

ST3. Summary of the activation tests

ST4. Adsorption kinetics parameters of CO2 on activated pine (TP and TCP) over different temperatures

ST5. Elemental analysis of activated biochar (on a dry basis)

ST6. Content of selected inorganics in pyrolyzed and activated biochars

ST7. Pyrolyzed and/or activated biochar yield

ST8. The compositional analysis of elements (XPS)

ST9. Total (3.6 – 500 Å) volume and specific surface area of the chars as well as the volume and area of ultramicropores (3.6 – 7 Å) and supermicropores (7 – 20 Å) calculated with 2D-NLDFT method

S1. Raman spectrum of selected  pine and birch biochar

S2. XPS survey for selected pine and birch activated biochar

S3. Pore size distributions of pine and birch chars activated at 800 ℃

S4. Measured isotherms and model fittings for selected samples

ST1. Content of inorganics in birch harvested from the contaminated and uncontaminated areas

| Elements | Contaminated Birch (mg/kg) | ± | Uncontaminated Birch (mg/kg) | ± |
| --- | --- | --- | --- | --- |
| Ag | 0.8 | 0 | 0.5 | 0.3 |
| Al | 92 | 10 | 65 | 11 |
| As | 2.3 | 0.1 | 1.2 | 0.3 |
| Ba | 15 | 0 | 29 | 0 |
| Ca | 4014 | 122 | 9109 | 811 |
| Cd | 88.9 | 2.8 | 1.2 | 0.1 |
| Co | 0.4 | 0 | 0.1 | 0.1 |
| Cr | 12 | 3 | 8 | 1 |
| Cu | 36 | 1 | 7 | 1 |
| Fe | 241 | 7 | 133 | 6 |
| K | 1567 | 28 | 2104 | 144 |
| Mg | 498 | 4 | 424 | 12 |
| Mn | 43 | 1 | 18 | 0 |
| Mo | 1.8 | 0.6 | 1.2 | 0.3 |
| Na | 239 | 6 | 233 | 17 |
| Ni | 6 | 2 | 3 | 0 |
| P | 454 | 2 | 501 | 7 |
| Pb | 1863 | 47 | 23 | 1 |
| Sb | 2.3 | 0.1 | 2.3 | 0.2 |
| Sn | 2.7 | 0.2 | 0 | 0.6 |
| Ti | 3.7 | 0.1 | 2.9 | 0.1 |
| Zn | 1580 | 39 | 308 | 41 |
| Si | 1130 | 260 | 951 | 250 |
| Hg | 0.094 | 0.002 | 0.01 | 0.001 |

ST2. Content of inorganics in pine harvested from the contaminated and uncontaminated areas

| Elements | Contaminated Birch (mg/kg) | ± | Uncontaminated Birch (mg/kg) | ± |
| --- | --- | --- | --- | --- |
| Ag | 1.3 | 0.2 | 0.5 | 0.1 |
| Al | 275 | 30 | 227 | 6 |
| As | 5 | 0 | 2.7 | 1 |
| Ba | 31 | 1 | 12 | 1 |
| Ca | 4388 | 237 | 2714 | 79 |
| Cd | 42 | 1 | 2.9 | 0 |
| Co | 1 | 0 | 0.6 | 0.2 |
| Cr | 15 | 1 | 47 | 7 |
| Cu | 65 | 4 | 20 | 5 |
| Fe | 442 | 54 | 407 | 63 |
| K | 3527 | 242 | 3344 | 186 |
| Mg | 818 | 36 | 474 | 16 |
| Mn | 66 | 3 | 241 | 5 |
| Mo | 3.1 | 0.4 | 3.9 | 0.8 |
| Na | 35 | 11 | 234 | 1 |
| Ni | 8 | 1 | 20 | 2 |
| P | 839 | 79 | 791 | 35 |
| Pb | 2105 | 61 | 76 | 1 |
| Sb | 0.8 | 0 | 4.9 | 1.8 |
| Sn | 8.9 | 0.6 | 1.8 | 0.6 |
| Ti | 7 | 0.7 | 8.6 | 1.3 |
| Zn | 835 | 48 | 117 | 9 |
| Si | 1900 | 300 | 2087 | 359 |
| Hg | 0.253 | 0.016 | 0.023 | 0.001 |

ST3. Summary of the activation tests

| No | Biochar Type | Atmosphere | Temperature (℃) | Reaction time(min) | Abbreviation |
| --- | --- | --- | --- | --- | --- |
| 1 | P | 50/50 vol.% H2O/CO2 | 800 | 60 | TP-H2O-800-60 |
| 2 | P | CO2 | 800 | 120 | TP-CO2-800-120 |
| 3 | CP | 50/50 vol.% H2O/CO2 | 800 | 60 | TCP-H2O-800-60 |
| 4 | CP | CO2 | 800 | 120 | TCP-CO2-800-120 |
| 5 | B | 50/50 vol.% H2O/CO2 | 800 | 60 | TB-H2O-800-60 |
| 6 | B | CO2 | 800 | 120 | TB-CO2-800-120 |
| 7 | CB | 50/50 vol.% H2O/CO2 | 700 | 120 | TCB-H2O-700-10 |
| 8 | CB | CO2 | 700 | 240 | TCB-CO2-700-240 |
| 9 | CB | 50/50 vol.% H2O/CO2 | 800 | 60 | TCB-H2O-800-60 |
| 10 | CB | CO2 | 800 | 120 | TCB-CO2-800-120 |
| 11 | CB | 50/50 vol.% H2O/CO2 | 900 | 10 | TCB-H2O-900-10 |
| 12 | CB | CO2 | 900 | 20 | TCB-CO2-900-20 |

ST4. Adsorption kinetics parameters of CO2 on  activated pine (TP and TCP) over different temperatures

| Samples | Model | Pseudo-first order model |  |  | Pseudo-second order model |  |  | Avrami model |  |  |  | Experimental |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Parameters |  |  |  |  |  |  |  |  |  |  |  |
|  | Temperature (℃) | k1(1/s) | qmax (mmol/g) | R² | k2 (g/(mmol·s)) | q max (mmol/g) | R² | kA | nA (1/s)n | q max (mmol/g) | R² | q max (mmol/g) |
| TP |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 30 | 0.0505 | 1.908 | 0.987 | 0.0464 | 1.9476 | 0.9999 | 0.0381 | 1.2914 | 1.908 | 0.9856 | 1.908 |
|  | 45 | 0.0516 | 1.5522 | 0.9791 | 0.063 | 1.5828 | 0.9999 | 0.0442 | 1.1439 | 1.5522 | 0.9854 | 1.5522 |
|  | 60 | 0.0552 | 1.2469 | 0.9857 | 0.1052 | 1.2623 | 0.9998 | 0.0507 | 1.0643 | 1.2469 | 0.9878 | 1.2469 |
|  | 75 | 0.0581 | 1.0192 | 0.9924 | 0.1364 | 1.0273 | 0.9999 | 0.0582 | 0.9712 | 1.0192 | 0.9854 | 1.0192 |
| TCP | 30 | 0.049 | 1.7087 | 0.9848 | 0.0488 | 1.7443 | 0.9999 | 0.0388 | 1.2298 | 1.7087 | 0.9858 | 1.7087 |
|  | 45 | 0.0518 | 1.3639 | 0.987 | 0.072 | 1.3901 | 0.9999 | 0.0439 | 1.1346 | 1.3639 | 0.986 | 1.3639 |
|  | 60 | 0.0553 | 1.0944 | 0.9908 | 0.11 | 1.1114 | 0.9999 | 0.051 | 1.0554 | 1.0944 | 0.9905 | 1.0944 |
|  | 75 | 0.0569 | 0.8895 | 0.9961 | 0.1465 | 0.896 | 0.9998 | 0.0573 | 0.9616 | 0.8895 | 0.9877 | 0.8895 |

ST5. Elemental analysis of activated biochar (on a dry basis)

| Sample name | C (Wt.%) | ± | H (Wt.%) | ± | N (Wt.%) | ± | S (Wt.%) | ± | O (Wt.%) | ± | Sum |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TP-H2O-800-60 | 76.31 | 2.32 | 0.97 | 0.08 | 1.02 | 0.03 | 0.06 | 0.01 | 13.61 | 0.60 | 91.97 |
| TP-CO2-800-120 | 74.03 | 0.05 | 0.89 | 0.03 | 2.46 | 0.01 | 0.10 | 0.01 | 14.14 | 0.43 | 91.61 |
| TCP-H2O-800-60 | 66.29 | 0.16 | 0.85 | 0.02 | 0.78 | 0.02 | 0.16 | 0.05 | 16.40 | 0.16 | 84.48 |
| TCP-CO2-800-120 | 67.96 | 0.56 | 0.86 | 0.07 | 2.18 | 0.03 | 0.48 | 0.10 | 15.38 | 0.56 | 86.87 |
| TB-H2O-800-60 | 66.92 | 0.16 | 0.89 | 0.01 | 0.81 | 0.00 | 0.00 | 0.00 | 17.92 | 0.86 | 86.56 |
| TB-CO2-800-120 | 71.00 | 0.02 | 0.77 | 0.01 | 1.89 | 0.01 | 0.03 | 0.01 | 16.81 | 0.38 | 90.51 |
| TCB-H2O-700-120 | 78.61 | 0.34 | 1.02 | 0.06 | 0.98 | 0.00 | 0.09 | 0.02 | 10.95 | 0.14 | 91.65 |
| TCB-CO2-700-240 | 77.42 | 0.33 | 0.92 | 0.02 | 1.67 | 0.02 | 0.14 | 0.02 | 12.18 | 0.13 | 92.34 |
| TCB-H2O-800-60 | 77.55 | 0.26 | 0.94 | 0.01 | 0.84 | 0.01 | 0.11 | 0.05 | 11.80 | 0.53 | 91.24 |
| TCB-CO2-800-120 | 77.57 | 0.17 | 0.74 | 0.01 | 1.76 | 0.01 | 0.11 | 0.04 | 12.32 | 1.19 | 92.50 |
| TCB-H2O-900-10 | 81.14 | 0.56 | 0.79 | 0.04 | 1.06 | 0.02 | 0.11 | 0.04 | 10.47 | 0.15 | 93.57 |
| TCB-CO2-900-20 | 81.50 | 0.47 | 0.83 | 0.14 | 1.36 | 0.02 | 0.14 | 0.05 | 10.21 | 0.47 | 94.03 |

ST6. Content of selected inorganics in pyrolyzed and activated biochars

| Sample name | Al (mg/kg) | ± | Ca (mg/kg) | ± | K(mg/kg) | ± | Pb (mg/kg) | ± | Zn (mg/kg) | ± |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CP | 860 | 50 | 16970 | 850 | 16560 | 190 | 7060 | 100 | 2150 | 30 |
| TCP-H2O-800-60 | 2210 | 110 | 46800 | 1320 | 41900 | 2510 | 8970 | 150 | 650 | 50 |
| TCP-CO2-800-120 | 1890 | 80 | 39000 | 1710 | 36400 | 1220 | 9730 | 170 | 1160 | 70 |
| CB | 330 | 2 | 20490 | 30 | 8130 | 10 | 6750 | 30 | 3920 | 13 |
| TCB-H2O-700-120 | 450 | 20 | 27700 | 1190 | 11700 | 360 | 11000 | 170 | 4830 | 80 |
| TCB-CO2-700-240 | 330 | 20 | 22300 | 930 | 10500 | 10 | 9500 | 100 | 5890 | 130 |
| TCB-H2O-800-60 | 590 | 10 | 39500 | 700 | 16700 | 100 | 11100 | 200 | 270 | 5 |
| TCB-CO2-800-120 | 710 | 20 | 37500 | 780 | 17400 | 360 | 8540 | 110 | 830 | 40 |
| TCB-H2O-900-10 | 540 | 10 | 24900 | 500 | 15100 | 370 | 1660 | 30 | 110 | 10 |
| TCB-CO2-900-20 | 340 | 10 | 20600 | 660 | 9470 | 220 | 3860 | 50 | 100 | 10 |

ST7. Pyrolyzed and/or activated biochar yield

| Sample name | Burn-off | biochar yield |
| --- | --- | --- |
| CP | 0.750 | 0.250 |
| TCP-H2O-800-60 | 0.600 | 0.100 |
| TCP-CO2-800-120 | 0.570 | 0.108 |
| CB | 0.790 | 0.210 |
| TCB-H2O-700-120 | 0.320 | 0.143 |
| TCB-CO2-700-240 | 0.340 | 0.139 |
| TCB-H2O-800-60 | 0.530 | 0.099 |
| TCB-CO2-800-120 | 0.460 | 0.113 |
| TCB-H2O-900-10 | 0.300 | 0.147 |
| TCB-CO2-900-20 | 0.290 | 0.149 |

ST8. Detected elemental contents via XPS test at the surface of biochar

| Sample name | C 1s (at%) | ± | O 1s (at%) | ± | N 1s (at%) | ± | S 2p (at%) | ± | Si 2p (at%) | ± | Ca 2p (at%) | ± | Pb2p (at%) | K 2p(at%) | Mg 2p(at%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TP-H2O-800-60 | 87.78 | 0.09 | 12.22 | 0.09 | <0.1 | 0 | <0.1 | 0 | <0.1 | 0 | 1 | 0 | ND | <0.1 | <0.1 |
| TP-CO2-800-120 | 70.07 | 0.07 | 27.96 | 0.3 | 1.97 | 0.36 | <0.1 | 0 | <0.1 | 0 | 4 | 1 | ND | <0.1 | <0.1 |
| TCP-H2O-800-60 | 84.72 | 0.17 | 15.28 | 0.17 | <0.1 | 0 | <0.1 | 0 | <0.1 | 0 | 2 | 2 | <0.1 | <0.1 | <0.1 |
| TCP-CO2-800-120 | 81.7 | 0.14 | 15.55 | 0.11 | 2.43 | 0.25 | 0.33 | 0.01 | <0.1 | 0 | 1 | 1 | <0.1 | <0.1 | <0.1 |
| TB-H2O-800-60 | 90.77 | 0.245 | 9.23 | 0.245 | <0.1 | 0 | <0.1 | 0 | <0.5 | 0 | 1.5 | 1 | ND | <0.1 | <0.1 |
| TB-CO2-800-120 | 86.18 | 1.76 | 12.26 | 1.94 | 1.54 | 0.19 | <0.1 | 0 | <0.1 | 0 | 2.5 | 0.5 | ND | <0.1 | <0.1 |
| TCB-H2O-800-60 | 88.38 | 1.405 | 11.11 | 1.78 | 0.51 | 0.375 | <0.1 | 0 | <0.5 | 0 | 1.5 | 0.5 | <0.1 | <0.1 | <0.1 |
| TCB-CO2-800-120 | 94.58 | 1.065 | 4.16 | 1.13 | 1.27 | 0.08 | <0.1 | 0 | <0.1 | 0 | 1 | 0 | <0.1 | <0.1 | <0.1 |
| ND – not detected |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

ST9. Total (3.6 – 500 Å) volume and specific surface area of the chars as well as the volume and area of ultramicropores (3.6 – 7 Å) and supermicropores (7 – 20 Å) calculated with 2D-NLDFT method

| Sample name | Volume (cm3/g) |  |  | Specific surface area (m2/g) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Ultramicropores | Supermicropores | Total | Ultramicropores | Supermicropores | Total |
| Coconut AC | 0.125 | 0.097 | 0.253 | 452 | 198 | 660 |
| Stone coal | 0.126 | 0.192 | 0.36 | 445 | 375 | 838 |
| TP-H2O-800-60 | 0.184 | 0.1 | 0.425 | 690 | 197 | 940 |
| TP-CO2-800-120 | 0.203 | 0.091 | 0.367 | 761 | 187 | 980 |
| TCP-H2O-800-60 | 0.167 | 0.114 | 0.418 | 622 | 230 | 899 |
| TCP-CO2-800-120 | 0.196 | 0.12 | 0.397 | 734 | 242 | 1010 |
| TB-H2O-800-60 | 0.148 | 0.045 | 0.375 | 559 | 83 | 705 |
| TB-CO2-800-120 | 0.179 | 0.054 | 0.281 | 675 | 107 | 805 |
| TCB-H2O-700-120 | 0.132 | 0.087 | 0.407 | 498 | 169 | 735 |
| TCB-CO2-700-240 | 0.184 | 0.052 | 0.288 | 689 | 112 | 821 |
| TCB-H2O-800-60 | 0.118 | 0.104 | 0.383 | 438 | 217 | 711 |
| TCB-CO2-800-120 | 0.194 | 0.066 | 0.317 | 720 | 142 | 886 |
| TCB-H2O-900-10 | 0.173 | 0.052 | 0.282 | 653 | 105 | 783 |
| TCB-CO2-900-20 | 0.187 | 0.034 | 0.283 | 714 | 67 | 805 |

* Corresponding author: Nastaran Abbaspour, email: nastaran.abbaspour@tuwien.ac.at