Supplementary Material

Kinetics of model tar decomposition over activated biochar from a heavy metal-contaminated area

Nastaran Abbaspour1, Andrzej Szlęk2, Franz Winter1, Agnieszka Korus2*

1Institute of Chemical, Environmental and Bioscience Engineering, TU Wien

2Department of Thermal Technology, Silesian University of Technology

List of contents:

S1. Isotherms (measured and fitted)

S2. Comparison of the PDS in TCB and TB biochars

S3. Comparison of the XRD pattern of HT-treated and non HT-treated biochars

S4. XRD pattern versus 2Ѳ angle for CB-HT, TCB-HT and TCB-TU800-HT

Tables:

ST1. Content of inorganics in birch harvested from the contaminated and uncontaminated areas

ST2. Elemental analysis and ash content in pyrolytic and thermally activated biochar (on a dry basis, O by diff)

ST3. Summary of conducted tests

ST4. Contents of selected inorganics in both HT and non-HT chars

ST5. Surface area (S) and volume (V) of the fresh, spent and high temperature-treated biochars

S1. Isotherms (measured and fitted)

S2. Comparison of the PSD in TCB and TB biochars

S3. Comparison of the XRD pattern of HT-treated and non HT-treated biochars

S4. XRD pattern versus 2Ѳ angle for CB-HT, TCB-HT and TCB-TU800-HT

ST1. Content of inorganics in birch harvested from the contaminated and uncontaminated areas

| Elements | Contaminated Birch (mg/kg) | ± | Uncontaminated Birch (mg/kg) | ± |
| --- | --- | --- | --- | --- |
| Ag | 0.8 | 0 | 0.5 | 0.3 |
| Al | 92 | 10 | 65 | 11 |
| As | 2.3 | 0.1 | 1.2 | 0.3 |
| Ba | 15 | 0 | 29 | 0 |
| Ca | 4014 | 122 | 9109 | 811 |
| Cd | 88.9 | 2.8 | 1.2 | 0.1 |
| Co | 0.4 | 0 | 0.1 | 0.1 |
| Cr | 12 | 3 | 8 | 1 |
| Cu | 36 | 1 | 7 | 1 |
| Fe | 241 | 7 | 133 | 6 |
| K | 1567 | 28 | 2104 | 144 |
| Mg | 498 | 4 | 424 | 12 |
| Mn | 43 | 1 | 18 | 0 |
| Mo | 1.8 | 0.6 | 1.2 | 0.3 |
| Na | 239 | 6 | 233 | 17 |
| Ni | 6 | 2 | 3 | 0 |
| P | 454 | 2 | 501 | 7 |
| Pb | 1863 | 47 | 23 | 1 |
| Sb | 2.3 | 0.1 | 2.3 | 0.2 |
| Sn | 2.7 | 0.2 | 0 | 0.6 |
| Ti | 3.7 | 0.1 | 2.9 | 0.1 |
| Zn | 1580 | 39 | 308 | 41 |
| Si | 1130 | 260 | 951 | 250 |
| Hg | 0.094 | 0.002 | 0.01 | 0.001 |

ST2. Elemental analysis and ash content in pyrolytic and thermally activated biochar (on a dry basis, O by diff)

|  | C (wt.%) | ± | O (wt.%) | H (wt.%) | ± | N (wt.%) | ± | S (wt.%) | ± | Ash (wt.%) | ± |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| B | 75.67 | 0.05 | 12.55 | 2.21 | 0.02 | 1.73 | 0.05 | 0.098 | 0.004 | 7.76 | 0.95 |
| CB | 79.71 | 0.03 | 8.51 | 2.71 | 0.03 | 1.80 | 0.02 | 0.156 | 0.002 | 7.11 | 1.12 |
| TB | 58.29 | 0.25 | 22.36 | 1.50 | 0.01 | 0.88 | 0.01 | 0.078 | 0.002 | 16.89 | 0.90 |
| TCB | 70.12 | 0.15 | 13.93 | 1.79 | 0.01 | 0.96 | 0.02 | 0.167 | 0.004 | 13.04 | 1.48 |

ST3. Summary of conducted tests

| No | Biochar | Temperature (℃) | Atmosphere | Compound | Abbreviation |
| --- | --- | --- | --- | --- | --- |
| 1 | TCB | 800 |  |  | TCB-TU800 |
| 2 | TCB | 750 |  |  | TCB-TU750 |
| 3 | TCB | 700 | N2 | Toluene | TCB-TU700 |
| 4 | TCB | 650 |  |  | TCB-TU650 |
| 5 | TB | 800 |  |  | TB-TU800 |
| 6 | TB | 700 |  |  | TB-TU700 |

ST4. Content of selected inorganics in both HT and non-HT chars

|  | CB (mg/kg) | ± | CB-HT (mg/kg) | ± | TCB (mg/kg) | ± | TCB-HT (mg/KG) | ± | TCB-TU800(mg/kg) | ± | TCB-TU800-HT (mg/kg) | ± |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Al | 330 | 2 | 410 | 7 | 590 | 10 | 620 | 10 | 420 | 4 | 520 | 10 |
| Ca | 20490 | 30 | 28440 | 60 | 39500 | 700 | 34700 | 200 | 33390 | 90 | 33000 | 400 |
| K | 8130 | 10 | 14130 | 30 | 16700 | 100 | 15900 | 500 | 13370 | 50 | 15100 | 300 |
| Pb | 6750 | 30 | 7 | 5 | 11100 | 200 | ND (<15) |  | 990 | 10 | ND (<15) |  |
| Zn | 3920 | 13 | ND (<1) |  | 270 | 5 | ND (<5) |  | 42 | 1 | ND (<5) |  |
| ND – not detected |  |  |  |  |  |  |  |  |  |  |  |  |

ST5. Surface area (S) and volume (V) of the fresh, spent and high temperature-treated biochars

|  | SBET | STotal | SMicro | SUtramicro | SSupermicro | SMeso | VTotal | VMicro | VUtramicro | VSupermicro | VMeso |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (m2/g) | (m2/g) | (m2/g) | (m2/g) | (m2/g) | (m2/g) | (cm3/g) | (cm3/g) | (cm3/g) | (cm3/g) | (cm3/g) |
| B | 278 | 503 | 497 | 497 | 0 | 6 | 0.145 | 0.122 | 0.122 | 0.000 | 0.023 |
| CB | 273 | 526 | 522 | 522 | 0 | 4 | 0.145 | 0.126 | 0.126 | 0.000 | 0.019 |
| TB | 548 | 677 | 601 | 485 | 116 | 76 | 0.411 | 0.191 | 0.126 | 0.065 | 0.220 |
| TCB | 646 | 791 | 722 | 575 | 147 | 69 | 0.422 | 0.232 | 0.151 | 0.081 | 0.190 |
| TCB-800TU | 19 | 53 | 42 | 36 | 6 | 11 | 0.053 | 0.014 | 0.011 | 0.002 | 0.040 |
| TCB-750TU | 34 | 310 | 292 | 283 | 8 | 19 | 0.140 | 0.079 | 0.076 | 0.003 | 0.061 |
| TCB-700TU | 70 | 498 | 465 | 435 | 31 | 33 | 0.224 | 0.127 | 0.115 | 0.011 | 0.097 |
| TCB-650TU | 142 | 485 | 428 | 378 | 50 | 57 | 0.278 | 0.125 | 0.097 | 0.028 | 0.154 |
| TB-800TU | 14 | 90 | 82 | 72 | 10 | 8 | 0.059 | 0.026 | 0.022 | 0.004 | 0.033 |
| TB-700TU | 67 | 420 | 388 | 361 | 27 | 32 | 0.206 | 0.106 | 0.096 | 0.010 | 0.100 |
| CB-HT | 46 | 139 | 136 | 136 | 0 | 3 | 0.054 | 0.034 | 0.034 | 0.000 | 0.021 |
| TCB-HT | 347 | 580 | 521 | 521 | 0 | 58 | 0.305 | 0.129 | 0.129 | 0.000 | 0.176 |
| TCB-800TU-HT | 64 | 245 | 229 | 183 | 46 | 16 | 0.128 | 0.068 | 0.050 | 0.018 | 0.060 |

Corresponding authors: Nastaran Abbaspour, email: nastaran.abbaspour@tuwien.ac.at; Agnieszka Korus, email: agnieszka.korus@polsl.pl