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S1. Isotherms (measured and fitted)



























S2. Comparison of the PSD in TCB and TB biochars
 

S3. Comparison of the XRD pattern of HT-treated and non HT-treated biochars
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S4. XRD pattern versus 2Ѳ angle for CB-HT, TCB-HT and TCB-TU800-HT
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[bookmark: _Hlk162993510]ST1. Content of inorganics in birch harvested from the contaminated and uncontaminated areas
	Elements

	Contaminated Birch (mg/kg)
	±
	Uncontaminated Birch (mg/kg)
	±

	Ag
	0.8
	0
	0.5
	0.3

	Al
	92
	10
	65
	11

	As
	2.3
	0.1
	1.2
	0.3

	Ba
	15
	0
	29
	0

	Ca
	4014
	122
	9109
	811

	Cd
	88.9
	2.8
	1.2
	0.1

	Co
	0.4
	0
	0.1
	0.1

	Cr
	12
	3
	8
	1

	Cu
	36
	1
	7
	1

	Fe
	241
	7
	133
	6

	K
	1567
	28
	2104
	144

	Mg
	498
	4
	424
	12

	Mn
	43
	1
	18
	0

	Mo
	1.8
	0.6
	1.2
	0.3

	Na
	239
	6
	233
	17

	Ni
	6
	2
	3
	0

	P
	454
	2
	501
	7

	Pb
	1863
	47
	23
	1

	Sb
	2.3
	0.1
	2.3
	0.2

	Sn
	2.7
	0.2
	0
	0.6

	Ti
	3.7
	0.1
	2.9
	0.1

	Zn
	1580
	39
	308
	41

	Si
	1130
	260
	951
	250

	Hg
	0.094
	0.002
	0.01
	0.001



ST2. Elemental analysis and ash content in pyrolytic and thermally activated biochar (on a dry basis, O by diff)

	
	C (wt.%)
	±
	O (wt.%)
	H (wt.%)
	±
	N (wt.%)
	±
	S (wt.%)
	±
	[bookmark: _Hlk174529541]Ash (wt.%)
	±

	[bookmark: _Hlk174529602]B
	75.67
	0.05
	12.55
	2.21
	0.02
	1.73
	0.05
	0.098
	0.004
	7.76
	0.95

	CB
	79.71
	0.03
	8.51
	2.71
	0.03
	1.80
	0.02
	0.156
	0.002
	7.11
	1.12

	TB
	58.29
	0.25
	22.36
	1.50
	0.01
	0.88
	0.01
	0.078
	0.002
	16.89
	0.90

	TCB
	70.12
	0.15
	13.93
	1.79
	0.01
	0.96
	0.02
	0.167
	0.004
	13.04
	1.48




ST3. Summary of conducted tests
	No
	Biochar 
	Temperature
(℃)
	Atmosphere
	Compound
	Abbreviation 

	1
	TCB
	800
	 
	 
	TCB-TU800

	2
	TCB
	750
	 
	 
	TCB-TU750

	3
	TCB
	700
	N2
	Toluene
	TCB-TU700

	4
	TCB
	650
	 
	 
	TCB-TU650

	5
	TB
	800
	 
	 
	TB-TU800

	6
	TB
	700
	 
	 
	TB-TU700




ST4. Content of selected inorganics in both HT and non-HT chars

	
	CB (mg/kg)
	±
	CB-HT (mg/kg)
	±
	TCB (mg/kg)
	±
	TCB-HT
(mg/KG)
	±
	TCB-TU800(mg/kg)
	±
	TCB-TU800-HT (mg/kg)
	±

	Al
	330
	2
	410
	7
	590
	10
	620
	10
	420
	4
	520
	10

	Ca
	20490
	30
	28440
	60
	39500
	700
	34700
	200
	33390
	90
	33000
	400

	K
	8130
	10
	14130
	30
	16700
	100
	15900
	500
	13370
	50
	15100
	300

	Pb
	6750
	30
	7
	5
	11100
	200
	ND (<15)
	
	990
	10
	ND (<15)
	

	Zn
	3920
	13
	ND (<1)
	
	270
	5
	ND (<5)
	
	42
	1
	ND (<5)
	

	ND – not detected
	
	
	
	
	
	
	
	
	
	






ST5. Surface area (S) and volume (V) of the fresh, spent and high temperature-treated biochars
	 
	SBET
	STotal
	SMicro
	SUtramicro
	SSupermicro
	SMeso
	VTotal
	VMicro
	VUtramicro
	VSupermicro
	VMeso

	 
	(m2/g)
	(m2/g)
	(m2/g)
	(m2/g)
	(m2/g)
	(m2/g)
	(cm3/g)
	(cm3/g)
	(cm3/g)
	(cm3/g)
	(cm3/g)

	B
	278
	503
	497
	497
	0
	6
	0.145
	0.122
	0.122
	0.000
	0.023

	CB
	273
	526
	522
	522
	0
	4
	0.145
	0.126
	0.126
	0.000
	0.019

	TB
	548
	677
	601
	485
	116
	76
	0.411
	0.191
	0.126
	0.065
	0.220

	TCB
	646
	791
	722
	575
	147
	69
	0.422
	0.232
	0.151
	0.081
	0.190

	TCB-800TU
	19
	53
	42
	36
	6
	11
	0.053
	0.014
	0.011
	0.002
	0.040

	TCB-750TU
	34
	310
	292
	283
	8
	19
	0.140
	0.079
	0.076
	0.003
	0.061

	TCB-700TU
	70
	498
	465
	435
	31
	33
	0.224
	0.127
	0.115
	0.011
	0.097

	TCB-650TU
	142
	485
	428
	378
	50
	57
	0.278
	0.125
	0.097
	0.028
	0.154

	TB-800TU
	14
	90
	82
	72
	10
	8
	0.059
	0.026
	0.022
	0.004
	0.033

	TB-700TU
	67
	420
	388
	361
	27
	32
	0.206
	0.106
	0.096
	0.010
	0.100

	CB-HT
	46
	139
	136
	136
	0
	3
	0.054
	0.034
	0.034
	0.000
	0.021

	TCB-HT
	347
	580
	521
	521
	0
	58
	0.305
	0.129
	0.129
	0.000
	0.176

	TCB-800TU-HT
	64
	245
	229
	183
	46
	16
	0.128
	0.068
	0.050
	0.018
	0.060



TB

Measured CO2	9.2600000000000001E-5	2.4000000000000001E-4	4.1199999999999999E-4	5.9900000000000003E-4	8.0000000000000004E-4	1.01E-3	1.24E-3	1.47E-3	1.6999999999999999E-3	1.9400000000000001E-3	2.1900000000000001E-3	2.4399999999999999E-3	2.7000000000000001E-3	2.96E-3	3.2100000000000002E-3	3.48E-3	3.7499999999999999E-3	4.0200000000000001E-3	4.2900000000000004E-3	4.5599999999999998E-3	4.8399999999999997E-3	5.1200000000000004E-3	5.4000000000000003E-3	5.6899999999999997E-3	5.9800000000000001E-3	6.2599999999999999E-3	6.5500000000000003E-3	6.8300000000000001E-3	7.1199999999999996E-3	7.4099999999999999E-3	7.7000000000000002E-3	7.9900000000000006E-3	8.2900000000000005E-3	8.5800000000000008E-3	8.8800000000000007E-3	9.1699999999999993E-3	9.4800000000000006E-3	9.7800000000000005E-3	1.01E-2	1.04E-2	1.0699999999999999E-2	1.0999999999999999E-2	1.1299999999999999E-2	1.1599999999999999E-2	1.1900000000000001E-2	1.2200000000000001E-2	1.2500000000000001E-2	1.29E-2	1.32E-2	1.35E-2	1.38E-2	1.41E-2	1.46E-2	1.4999999999999999E-2	1.54E-2	1.5900000000000001E-2	1.6299999999999999E-2	1.6799999999999999E-2	1.72E-2	1.77E-2	1.8100000000000002E-2	1.8599999999999998E-2	1.9E-2	1.9400000000000001E-2	1.9900000000000001E-2	2.0299999999999999E-2	2.0799999999999999E-2	2.12E-2	2.1700000000000001E-2	2.2100000000000002E-2	2.2599999999999999E-2	2.3E-2	2.35E-2	2.3900000000000001E-2	2.4400000000000002E-2	2.4799999999999999E-2	2.53E-2	2.5700000000000001E-2	2.6200000000000001E-2	2.6599999999999999E-2	2.7099999999999999E-2	2.75E-2	2.8000000000000001E-2	2.8400000000000002E-2	2.8799999999999999E-2	2.93E-2	2.9700000000000001E-2	3.0200000000000001E-2	2.75	4.93	6.84	8.56	10.1	11.6	12.9	14.2	15.4	16.600000000000001	17.600000000000001	18.7	19.7	20.6	21.5	22.4	23.2	24	24.8	25.6	26.3	27	27.7	28.4	29	29.7	30.3	30.9	31.5	32.1	32.6	33.200000000000003	33.700000000000003	34.299999999999997	34.799999999999997	35.299999999999997	35.799999999999997	36.200000000000003	36.700000000000003	37.1	37.6	38.1	38.5	39	39.4	39.799999999999997	40.200000000000003	40.6	40.9	41.3	41.7	42.1	42.6	43.1	43.6	44.1	44.6	45.2	45.7	46.2	46.7	47.2	47.6	48.1	48.6	49.1	49.5	50	50.5	50.9	51.4	51.8	52.2	52.7	53.1	53.5	53.9	54.4	54.8	55.2	55.6	56	56.4	56.7	57.1	57.5	57.9	58.3	Fit	9.2600000000000001E-5	2.4000000000000001E-4	4.1199999999999999E-4	5.9900000000000003E-4	8.0000000000000004E-4	1.01E-3	1.24E-3	1.47E-3	1.6999999999999999E-3	1.9400000000000001E-3	2.1900000000000001E-3	2.4399999999999999E-3	2.7000000000000001E-3	2.96E-3	3.2100000000000002E-3	3.48E-3	3.7499999999999999E-3	4.0200000000000001E-3	4.2900000000000004E-3	4.5599999999999998E-3	4.8399999999999997E-3	5.1200000000000004E-3	5.4000000000000003E-3	5.6899999999999997E-3	5.9800000000000001E-3	6.2599999999999999E-3	6.5500000000000003E-3	6.8300000000000001E-3	7.1199999999999996E-3	7.4099999999999999E-3	7.7000000000000002E-3	7.9900000000000006E-3	8.2900000000000005E-3	8.5800000000000008E-3	8.8800000000000007E-3	9.1699999999999993E-3	9.4800000000000006E-3	9.7800000000000005E-3	1.01E-2	1.04E-2	1.0699999999999999E-2	1.0999999999999999E-2	1.1299999999999999E-2	1.1599999999999999E-2	1.1900000000000001E-2	1.2200000000000001E-2	1.2500000000000001E-2	1.29E-2	1.32E-2	1.35E-2	1.38E-2	1.41E-2	1.46E-2	1.4999999999999999E-2	1.54E-2	1.5900000000000001E-2	1.6299999999999999E-2	1.6799999999999999E-2	1.72E-2	1.77E-2	1.8100000000000002E-2	1.8599999999999998E-2	1.9E-2	1.9400000000000001E-2	1.9900000000000001E-2	2.0299999999999999E-2	2.0799999999999999E-2	2.12E-2	2.1700000000000001E-2	2.2100000000000002E-2	2.2599999999999999E-2	2.3E-2	2.35E-2	2.3900000000000001E-2	2.4400000000000002E-2	2.4799999999999999E-2	2.53E-2	2.5700000000000001E-2	2.6200000000000001E-2	2.6599999999999999E-2	2.7099999999999999E-2	2.75E-2	2.8000000000000001E-2	2.8400000000000002E-2	2.8799999999999999E-2	2.93E-2	2.9700000000000001E-2	3.0200000000000001E-2	0.73599999999999999	2.04	3.7	5.54	7.38	9.1199999999999992	10.8	12.3	13.7	15.1	16.399999999999999	17.600000000000001	18.8	19.899999999999999	20.9	21.9	22.8	23.8	24.7	25.5	26.3	27.1	27.9	28.6	29.3	30	30.6	31.3	31.9	32.5	33.1	33.6	34.200000000000003	34.700000000000003	35.299999999999997	35.799999999999997	36.299999999999997	36.799999999999997	37.299999999999997	37.799999999999997	38.200000000000003	38.700000000000003	39.1	39.5	40	40.4	40.799999999999997	41.2	41.6	42	42.4	42.8	43.3	43.8	44.3	44.7	45.2	45.7	46.1	46.6	47	47.4	47.8	48.2	48.6	49	49.4	49.8	50.1	50.5	50.9	51.2	51.6	51.9	52.2	52.6	52.9	53.2	53.5	53.8	54.1	54.4	54.7	55	55.3	55.6	55.8	56.1	Measured N2	6.5099999999999999E-4	1.4300000000000001E-3	2.99E-3	5.3600000000000002E-3	7.5799999999999999E-3	1.0500000000000001E-2	3.3500000000000002E-2	6.0499999999999998E-2	7.6999999999999999E-2	0.1	0.126	0.152	0.17699999999999999	0.20200000000000001	0.28000000000000003	0.373	0.46	0.54700000000000004	0.63500000000000001	0.72599999999999998	0.80700000000000005	0.89	0.93500000000000005	0.96399999999999997	0.98299999999999998	79.900000000000006	98.9	107	112	115	118	128	133	135	138	141	144	146	149	156	165	174	184	195	209	221	237	248	261	272	Fit	6.5099999999999999E-4	1.4300000000000001E-3	2.99E-3	5.3600000000000002E-3	7.5799999999999999E-3	1.0500000000000001E-2	3.3500000000000002E-2	6.0499999999999998E-2	7.6999999999999999E-2	0.1	0.126	0.152	0.17699999999999999	0.20200000000000001	0.28000000000000003	0.373	0.46	0.54700000000000004	0.63500000000000001	0.72599999999999998	0.80700000000000005	0.89	0.93500000000000005	0.96399999999999997	0.98299999999999998	93.5	99	105	111	114	117	128	133	135	139	141	144	146	149	156	165	174	184	196	208	221	237	248	261	272	Realative pressure 


Amount adsorbed, cm3/g (STP)




TCB

Measured CO2	1.16E-4	2.9700000000000001E-4	5.1199999999999998E-4	7.5199999999999996E-4	1.01E-3	1.3699999999999999E-3	1.7600000000000001E-3	2.1800000000000001E-3	2.6199999999999999E-3	3.0799999999999998E-3	3.5599999999999998E-3	4.0600000000000002E-3	4.5700000000000003E-3	5.11E-3	5.6499999999999996E-3	6.2100000000000002E-3	6.7799999999999996E-3	7.3600000000000002E-3	7.9600000000000001E-3	8.5599999999999999E-3	9.1699999999999993E-3	9.7900000000000001E-3	1.04E-2	1.0999999999999999E-2	1.17E-2	1.23E-2	1.2999999999999999E-2	1.37E-2	1.43E-2	1.4999999999999999E-2	1.5699999999999999E-2	1.6299999999999999E-2	1.7000000000000001E-2	1.77E-2	1.84E-2	1.9099999999999999E-2	1.9800000000000002E-2	2.0500000000000001E-2	2.12E-2	2.1899999999999999E-2	2.2700000000000001E-2	2.3400000000000001E-2	2.41E-2	2.4799999999999999E-2	2.5499999999999998E-2	2.63E-2	2.7E-2	2.7699999999999999E-2	2.8500000000000001E-2	2.92E-2	2.9899999999999999E-2	3.0700000000000002E-2	3.12	5.81	8.27	10.5	12.7	15.1	17.5	19.7	21.8	23.8	25.7	27.6	29.3	31	32.6	34.1	35.6	37.1	38.4	39.799999999999997	41.1	42.3	43.5	44.7	45.8	47	48	49.1	50.1	51.1	52.1	53	54	54.9	55.7	56.6	57.4	58.3	59.1	59.9	60.7	61.4	62.2	62.9	63.6	64.3	65	65.7	66.400000000000006	67	67.7	68.3	Fit	1.16E-4	2.9700000000000001E-4	5.1199999999999998E-4	7.5199999999999996E-4	1.01E-3	1.3699999999999999E-3	1.7600000000000001E-3	2.1800000000000001E-3	2.6199999999999999E-3	3.0799999999999998E-3	3.5599999999999998E-3	4.0600000000000002E-3	4.5700000000000003E-3	5.11E-3	5.6499999999999996E-3	6.2100000000000002E-3	6.7799999999999996E-3	7.3600000000000002E-3	7.9600000000000001E-3	8.5599999999999999E-3	9.1699999999999993E-3	9.7900000000000001E-3	1.04E-2	1.0999999999999999E-2	1.17E-2	1.23E-2	1.2999999999999999E-2	1.37E-2	1.43E-2	1.4999999999999999E-2	1.5699999999999999E-2	1.6299999999999999E-2	1.7000000000000001E-2	1.77E-2	1.84E-2	1.9099999999999999E-2	1.9800000000000002E-2	2.0500000000000001E-2	2.12E-2	2.1899999999999999E-2	2.2700000000000001E-2	2.3400000000000001E-2	2.41E-2	2.4799999999999999E-2	2.5499999999999998E-2	2.63E-2	2.7E-2	2.7699999999999999E-2	2.8500000000000001E-2	2.92E-2	2.9899999999999999E-2	3.0700000000000002E-2	1.07	2.92	5.33	7.9	10.4	13.4	16.100000000000001	18.7	21.2	23.5	25.7	27.7	29.6	31.4	33.200000000000003	34.799999999999997	36.4	37.9	39.200000000000003	40.6	41.9	43.1	44.3	45.4	46.5	47.5	48.6	49.5	50.5	51.4	52.2	53.1	53.9	54.7	55.5	56.3	57	57.7	58.4	59.1	59.8	60.4	61	61.7	62.3	62.9	63.4	64	64.5	65.099999999999994	65.599999999999994	66.099999999999994	Measured N2	7.5699999999999997E-4	9.0799999999999995E-4	1.98E-3	4.0000000000000001E-3	5.2199999999999998E-3	7.5399999999999998E-3	9.5099999999999994E-3	3.2399999999999998E-2	5.3600000000000002E-2	7.6799999999999993E-2	0.10100000000000001	0.128	0.154	0.18	0.20499999999999999	0.29199999999999998	0.372	0.45900000000000002	0.54500000000000004	0.63300000000000001	0.72399999999999998	0.80500000000000005	0.89500000000000002	0.93500000000000005	0.96399999999999997	0.98299999999999998	99.5	104	122	131	134	138	140	151	156	160	163	166	169	171	173	181	189	197	206	217	229	240	255	264	272	280	Fit	7.5699999999999997E-4	9.0799999999999995E-4	1.98E-3	4.0000000000000001E-3	5.2199999999999998E-3	7.5399999999999998E-3	9.5099999999999994E-3	3.2399999999999998E-2	5.3600000000000002E-2	7.6799999999999993E-2	0.10100000000000001	0.128	0.154	0.18	0.20499999999999999	0.29199999999999998	0.372	0.45900000000000002	0.54500000000000004	0.63300000000000001	0.72399999999999998	0.80500000000000005	0.89500000000000002	0.93500000000000005	0.96399999999999997	0.98299999999999998	111	112	119	128	132	136	138	152	156	160	163	166	169	171	173	181	189	197	206	217	229	240	255	263	273	280	Relative pressure


Amount asorbed, cm3/g (STP)




TB-TU800

Measured CO2	3.0731600000000002E-4	6.1742500000000001E-4	9.2707300000000005E-4	1.2338200000000001E-3	1.5374799999999999E-3	1.84297E-3	2.1504599999999999E-3	2.4530899999999998E-3	2.7540099999999999E-3	3.0564400000000001E-3	3.35914E-3	3.66213E-3	3.9630500000000001E-3	4.2659000000000004E-3	4.5685099999999996E-3	4.8730099999999997E-3	5.1744199999999999E-3	5.4805899999999996E-3	5.7864500000000003E-3	6.0883100000000004E-3	6.3936399999999999E-3	6.69127E-3	6.9964199999999997E-3	7.2974900000000002E-3	7.6022399999999997E-3	7.9069899999999992E-3	8.2119199999999993E-3	8.5149700000000002E-3	8.8139700000000008E-3	9.1182699999999995E-3	9.42227E-3	9.7260599999999999E-3	1.0023600000000001E-2	1.0326399999999999E-2	1.0629700000000001E-2	1.0933500000000001E-2	1.12376E-2	1.153E-2	1.1833E-2	1.21371E-2	1.24289E-2	1.27315E-2	1.30337E-2	1.33238E-2	1.36261E-2	1.39186E-2	1.4220500000000001E-2	1.45226E-2	1.48135E-2	1.51147E-2	1.5406E-2	1.5708799999999998E-2	1.6002300000000001E-2	1.6305E-2	1.6595200000000001E-2	1.6896999999999999E-2	1.7188200000000001E-2	1.74904E-2	1.7778700000000001E-2	1.8080700000000002E-2	1.8368300000000001E-2	1.8669600000000001E-2	1.8953399999999999E-2	1.9241600000000001E-2	1.9542199999999999E-2	1.9829300000000001E-2	2.0129000000000001E-2	2.0414000000000002E-2	2.0698999999999999E-2	2.09997E-2	2.12859E-2	2.1572500000000001E-2	2.1861499999999999E-2	2.2161299999999998E-2	2.2445699999999999E-2	2.2729599999999999E-2	2.30133E-2	2.3313400000000001E-2	2.3597699999999999E-2	2.3881400000000001E-2	2.41636E-2	2.4446699999999998E-2	2.4729299999999999E-2	2.5029599999999999E-2	2.5311299999999998E-2	2.5592299999999998E-2	2.5874299999999999E-2	2.6154799999999999E-2	2.6434900000000001E-2	2.67184E-2	2.7000099999999999E-2	2.7280700000000001E-2	2.7562199999999999E-2	2.78429E-2	2.8125000000000001E-2	2.8405400000000001E-2	2.8687399999999998E-2	2.89681E-2	2.9248400000000001E-2	2.95283E-2	2.9808399999999999E-2	3.02288E-2	3.6464499999999997E-2	4.5450200000000003E-2	6.0916499999999998E-2	0.10064099999999999	0.16359799999999999	0.21856999999999999	0.25899899999999998	0.33246500000000001	0.417491	0.48987799999999998	0.56059800000000004	0.63223300000000004	0.72179099999999996	0.79624300000000003	0.87433300000000003	0.93786199999999997	1.0254000000000001	1.08301	1.1382000000000001	1.2236400000000001	1.2811600000000001	1.39452	1.45533	1.54454	1.6100099999999999	1.6756800000000001	1.7429699999999999	1.82138	1.9184399999999999	1.9862500000000001	2.0596100000000002	2.1331199999999999	2.2726799999999998	2.3549600000000002	2.4319700000000002	2.5077799999999999	2.5826099999999999	2.7241200000000001	2.8079700000000001	2.8850799999999999	3.0318800000000001	3.11666	3.2088000000000001	3.3647900000000002	3.4586299999999999	3.6021100000000001	3.6926800000000002	3.7815799999999999	3.9408500000000002	4.0337500000000004	4.1792100000000003	4.2677100000000001	4.4098699999999997	4.50495	4.66709	4.7597300000000002	4.9162100000000004	5.0030000000000001	5.1735699999999998	5.2649100000000004	5.4388699999999996	5.5368000000000004	5.7336	5.9030699999999996	5.9971899999999998	6.1728399999999999	6.2808099999999998	6.4588299999999998	6.6353600000000004	6.7405099999999996	6.9149799999999999	7.0955000000000004	7.2496	7.3594200000000001	7.5443100000000003	7.7178199999999997	7.9031500000000001	8.0060800000000008	8.1902500000000007	8.36829	8.5485900000000008	8.7381200000000003	8.9105100000000004	9.0061400000000003	9.1929099999999995	9.3838000000000008	9.5695599999999992	9.7671200000000002	9.9427500000000002	10.105399999999999	10.282299999999999	10.4483	10.619199999999999	10.782299999999999	10.940200000000001	11.1	11.2522	11.411	11.5761	11.7354	11.900399999999999	12.091699999999999	Fit	3.0731600000000002E-4	6.1742500000000001E-4	9.2707300000000005E-4	1.2338200000000001E-3	1.5374799999999999E-3	1.84297E-3	2.1504599999999999E-3	2.4530899999999998E-3	2.7540099999999999E-3	3.0564400000000001E-3	3.35914E-3	3.66213E-3	3.9630500000000001E-3	4.2659000000000004E-3	4.5685099999999996E-3	4.8730099999999997E-3	5.1744199999999999E-3	5.4805899999999996E-3	5.7864500000000003E-3	6.0883100000000004E-3	6.3936399999999999E-3	6.69127E-3	6.9964199999999997E-3	7.2974900000000002E-3	7.6022399999999997E-3	7.9069899999999992E-3	8.2119199999999993E-3	8.5149700000000002E-3	8.8139700000000008E-3	9.1182699999999995E-3	9.42227E-3	9.7260599999999999E-3	1.0023600000000001E-2	1.0326399999999999E-2	1.0629700000000001E-2	1.0933500000000001E-2	1.12376E-2	1.153E-2	1.1833E-2	1.21371E-2	1.24289E-2	1.27315E-2	1.30337E-2	1.33238E-2	1.36261E-2	1.39186E-2	1.4220500000000001E-2	1.45226E-2	1.48135E-2	1.51147E-2	1.5406E-2	1.5708799999999998E-2	1.6002300000000001E-2	1.6305E-2	1.6595200000000001E-2	1.6896999999999999E-2	1.7188200000000001E-2	1.74904E-2	1.7778700000000001E-2	1.8080700000000002E-2	1.8368300000000001E-2	1.8669600000000001E-2	1.8953399999999999E-2	1.9241600000000001E-2	1.9542199999999999E-2	1.9829300000000001E-2	2.0129000000000001E-2	2.0414000000000002E-2	2.0698999999999999E-2	2.09997E-2	2.12859E-2	2.1572500000000001E-2	2.1861499999999999E-2	2.2161299999999998E-2	2.2445699999999999E-2	2.2729599999999999E-2	2.30133E-2	2.3313400000000001E-2	2.3597699999999999E-2	2.3881400000000001E-2	2.41636E-2	2.4446699999999998E-2	2.4729299999999999E-2	2.5029599999999999E-2	2.5311299999999998E-2	2.5592299999999998E-2	2.5874299999999999E-2	2.6154799999999999E-2	2.6434900000000001E-2	2.67184E-2	2.7000099999999999E-2	2.7280700000000001E-2	2.7562199999999999E-2	2.78429E-2	2.8125000000000001E-2	2.8405400000000001E-2	2.8687399999999998E-2	2.89681E-2	2.9248400000000001E-2	2.95283E-2	2.9808399999999999E-2	3.02288E-2	0.1036859	0.21415339999999999	0.33009460000000002	0.4497816	0.5724437	0.69946039999999998	0.82991610000000005	0.96072389999999996	1.0924100000000001	1.2258370000000001	1.360314	1.4954689999999999	1.629769	1.7648969999999999	1.899462	2.0343680000000002	2.1672739999999999	2.3009930000000001	2.4335830000000001	2.5630480000000002	2.6924450000000002	2.8181470000000002	2.9434650000000002	3.0671080000000002	3.189918	3.3101419999999999	3.4304380000000001	3.5469040000000001	3.6591879999999999	3.7734619999999999	3.8861669999999999	3.9937230000000001	4.0990650000000004	4.20627	4.3100880000000004	4.4105569999999998	4.5111249999999998	4.6078239999999999	4.7055509999999998	4.7984859999999996	4.8876619999999997	4.9801390000000003	5.0724929999999997	5.1563480000000004	5.2407329999999996	5.322381	5.4066539999999996	5.4909819999999998	5.5696709999999996	5.6456939999999998	5.7192189999999998	5.7956459999999996	5.869726	5.9461279999999999	6.0164859999999996	6.084689	6.1504969999999997	6.2187900000000003	6.2839429999999998	6.3521910000000004	6.4171860000000001	6.4800890000000004	6.5370600000000003	6.5949150000000003	6.6552600000000002	6.7128940000000004	6.7730569999999997	6.8302699999999996	6.8870129999999996	6.9400300000000001	6.9904909999999996	7.0410209999999998	7.0919749999999997	7.1448330000000002	7.1949759999999996	7.245031	7.295051	7.3445970000000003	7.3884280000000002	7.4321679999999999	7.4756749999999998	7.5193219999999998	7.5628919999999997	7.6091899999999999	7.6526209999999999	7.6959439999999999	7.7394210000000001	7.7783670000000003	7.815925	7.8539399999999997	7.8917130000000002	7.9293389999999997	7.967085	8.0047239999999995	8.0425509999999996	8.0801499999999997	8.1179629999999996	8.1556029999999993	8.1897230000000008	8.2222770000000001	8.2548539999999999	8.3037489999999998	Measured N2	9.9853499999999998E-2	0.12492	0.14990500000000001	0.17486199999999999	0.199796	0.28694700000000001	0.375689	0.46320499999999998	0.55081899999999995	0.63869900000000002	0.72966200000000003	0.809504	0.89833300000000005	0.94774400000000003	1.70164	1.8795599999999999	2.07544	2.2907000000000002	2.5223399999999998	3.4942799999999998	4.7715399999999999	6.3051199999999996	8.1371900000000004	10.333299999999999	13.0496	15.9899	20.495999999999999	24.938500000000001	Fit	9.9853499999999998E-2	0.12492	0.14990500000000001	0.17486199999999999	0.199796	0.28694700000000001	0.375689	0.46320499999999998	0.55081899999999995	0.63869900000000002	0.72966200000000003	0.809504	0.89833300000000005	0.94774400000000003	4.9636180000000003	5.1154539999999997	5.2533890000000003	5.3866849999999999	5.5195129999999999	6.0257129999999997	6.5233569999999999	6.9853319999999997	7.5920740000000002	9.2268740000000005	12.079560000000001	15.157030000000001	20	24.367740000000001	Relative  pressure


Amount adsorbed, cm3/g (STP)




TB-TU700

Measured CO2	1.5324800000000001E-4	2.8837399999999999E-4	4.26272E-4	5.8098600000000002E-4	7.4694699999999998E-4	9.1246600000000001E-4	1.0802699999999999E-3	1.25614E-3	1.4413099999999999E-3	1.6194499999999999E-3	1.80785E-3	2.0089399999999999E-3	2.2047999999999998E-3	2.41501E-3	2.6159999999999998E-3	2.8346999999999999E-3	3.0357399999999999E-3	3.2601499999999999E-3	3.47789E-3	3.69506E-3	3.9150799999999996E-3	4.1324200000000004E-3	4.3612900000000003E-3	4.5950799999999997E-3	4.82535E-3	5.0530599999999998E-3	5.2940599999999997E-3	5.5328900000000004E-3	5.7718700000000001E-3	6.0050700000000004E-3	6.2438299999999997E-3	6.4936100000000004E-3	6.7222100000000002E-3	6.9657E-3	7.2097400000000001E-3	7.4538699999999996E-3	7.7140799999999999E-3	7.9514500000000005E-3	8.1940099999999998E-3	8.4470900000000008E-3	8.7031999999999995E-3	8.94321E-3	9.1975200000000007E-3	9.4601400000000006E-3	9.6963299999999995E-3	9.9487399999999993E-3	1.0203800000000001E-2	1.0461700000000001E-2	1.07213E-2	1.0977799999999999E-2	1.1221699999999999E-2	1.1476200000000001E-2	1.1741100000000001E-2	1.1993800000000001E-2	1.2252300000000001E-2	1.25065E-2	1.27679E-2	1.30305E-2	1.3299200000000001E-2	1.3543100000000001E-2	1.3797200000000001E-2	1.4063900000000001E-2	1.43249E-2	1.45878E-2	1.48548E-2	1.511E-2	1.53749E-2	1.5633500000000002E-2	1.5888699999999999E-2	1.6154000000000002E-2	1.6419199999999998E-2	1.66848E-2	1.6950799999999999E-2	1.7216499999999999E-2	1.74717E-2	1.7735799999999999E-2	1.7998900000000002E-2	1.8263100000000001E-2	1.8527200000000001E-2	1.8791700000000001E-2	1.9058599999999998E-2	1.93229E-2	1.9584399999999998E-2	1.98487E-2	2.0114699999999999E-2	2.0374400000000001E-2	2.0637699999999998E-2	2.0902500000000001E-2	2.1167499999999999E-2	2.1437000000000001E-2	2.1702200000000001E-2	2.1967E-2	2.2234E-2	2.2500300000000001E-2	2.2764900000000001E-2	2.3031900000000001E-2	2.32961E-2	2.35614E-2	2.3825800000000001E-2	2.4092300000000001E-2	2.4354399999999998E-2	2.4620099999999999E-2	2.4884799999999999E-2	2.5159299999999999E-2	2.54267E-2	2.5689699999999999E-2	2.59565E-2	2.6226300000000001E-2	2.6491299999999999E-2	2.6759700000000001E-2	2.70245E-2	2.72933E-2	2.7560100000000001E-2	2.7827399999999999E-2	2.8097299999999999E-2	2.8364400000000001E-2	2.8632600000000001E-2	2.8898500000000001E-2	2.9163700000000001E-2	2.9426000000000001E-2	2.9689699999999999E-2	2.9957899999999999E-2	3.0219599999999999E-2	1.12178	2.3671099999999998	3.55782	4.6091199999999999	5.5464799999999999	6.4618399999999996	7.4168000000000003	8.2857000000000003	9.0778300000000005	9.9203399999999995	10.681800000000001	11.346	12.0512	12.6463	13.309100000000001	13.8452	14.510999999999999	14.9933	15.5236	16.061699999999998	16.581499999999998	17.124099999999999	17.5761	17.994900000000001	18.4361	18.899699999999999	19.261399999999998	19.641200000000001	20.015799999999999	20.4343	20.8125	21.107700000000001	21.563199999999998	21.9008	22.235499999999998	22.573899999999998	22.789000000000001	23.174700000000001	23.518799999999999	23.7837	24.026700000000002	24.3932	24.651900000000001	24.8444	25.2392	25.5136	25.770499999999998	26.0017	26.217500000000001	26.461400000000001	26.8017	27.057099999999998	27.2318	27.503	27.734100000000002	27.9938	28.198899999999998	28.390799999999999	28.54	28.871700000000001	29.127500000000001	29.284800000000001	29.488399999999999	29.673200000000001	29.8291	30.0809	30.258199999999999	30.4816	30.734100000000002	30.909700000000001	31.085000000000001	31.257999999999999	31.4297	31.602699999999999	31.8553	32.0381	32.226700000000001	32.405500000000004	32.584400000000002	32.758699999999997	32.914299999999997	33.089599999999997	33.2849	33.457799999999999	33.624899999999997	33.836500000000001	34.018099999999997	34.191200000000002	34.371299999999998	34.511000000000003	34.684899999999999	34.860700000000001	35.021900000000002	35.195599999999999	35.375	35.529299999999999	35.708599999999997	35.879100000000001	36.055300000000003	36.218299999999999	36.413699999999999	36.576300000000003	36.7468	36.841299999999997	36.989400000000003	37.174999999999997	37.325000000000003	37.463000000000001	37.630400000000002	37.777700000000003	37.945300000000003	38.087600000000002	38.243499999999997	38.392899999999997	38.522799999999997	38.671500000000002	38.805900000000001	38.963999999999999	39.101700000000001	39.258600000000001	39.405500000000004	39.521099999999997	39.679099999999998	Fit	1.5324800000000001E-4	2.8837399999999999E-4	4.26272E-4	5.8098600000000002E-4	7.4694699999999998E-4	9.1246600000000001E-4	1.0802699999999999E-3	1.25614E-3	1.4413099999999999E-3	1.6194499999999999E-3	1.80785E-3	2.0089399999999999E-3	2.2047999999999998E-3	2.41501E-3	2.6159999999999998E-3	2.8346999999999999E-3	3.0357399999999999E-3	3.2601499999999999E-3	3.47789E-3	3.69506E-3	3.9150799999999996E-3	4.1324200000000004E-3	4.3612900000000003E-3	4.5950799999999997E-3	4.82535E-3	5.0530599999999998E-3	5.2940599999999997E-3	5.5328900000000004E-3	5.7718700000000001E-3	6.0050700000000004E-3	6.2438299999999997E-3	6.4936100000000004E-3	6.7222100000000002E-3	6.9657E-3	7.2097400000000001E-3	7.4538699999999996E-3	7.7140799999999999E-3	7.9514500000000005E-3	8.1940099999999998E-3	8.4470900000000008E-3	8.7031999999999995E-3	8.94321E-3	9.1975200000000007E-3	9.4601400000000006E-3	9.6963299999999995E-3	9.9487399999999993E-3	1.0203800000000001E-2	1.0461700000000001E-2	1.07213E-2	1.0977799999999999E-2	1.1221699999999999E-2	1.1476200000000001E-2	1.1741100000000001E-2	1.1993800000000001E-2	1.2252300000000001E-2	1.25065E-2	1.27679E-2	1.30305E-2	1.3299200000000001E-2	1.3543100000000001E-2	1.3797200000000001E-2	1.4063900000000001E-2	1.43249E-2	1.45878E-2	1.48548E-2	1.511E-2	1.53749E-2	1.5633500000000002E-2	1.5888699999999999E-2	1.6154000000000002E-2	1.6419199999999998E-2	1.66848E-2	1.6950799999999999E-2	1.7216499999999999E-2	1.74717E-2	1.7735799999999999E-2	1.7998900000000002E-2	1.8263100000000001E-2	1.8527200000000001E-2	1.8791700000000001E-2	1.9058599999999998E-2	1.93229E-2	1.9584399999999998E-2	1.98487E-2	2.0114699999999999E-2	2.0374400000000001E-2	2.0637699999999998E-2	2.0902500000000001E-2	2.1167499999999999E-2	2.1437000000000001E-2	2.1702200000000001E-2	2.1967E-2	2.2234E-2	2.2500300000000001E-2	2.2764900000000001E-2	2.3031900000000001E-2	2.32961E-2	2.35614E-2	2.3825800000000001E-2	2.4092300000000001E-2	2.4354399999999998E-2	2.4620099999999999E-2	2.4884799999999999E-2	2.5159299999999999E-2	2.54267E-2	2.5689699999999999E-2	2.59565E-2	2.6226300000000001E-2	2.6491299999999999E-2	2.6759700000000001E-2	2.70245E-2	2.72933E-2	2.7560100000000001E-2	2.7827399999999999E-2	2.8097299999999999E-2	2.8364400000000001E-2	2.8632600000000001E-2	2.8898500000000001E-2	2.9163700000000001E-2	2.9426000000000001E-2	2.9689699999999999E-2	2.9957899999999999E-2	3.0219599999999999E-2	0.83673620000000004	1.663368	2.5658479999999999	3.5810369999999998	4.6133620000000004	5.5650729999999999	6.4601620000000004	7.3233230000000002	8.170083	8.9331720000000008	9.6919740000000001	10.45439	11.157080000000001	11.873749999999999	12.516579999999999	13.183529999999999	13.776590000000001	14.39711	14.977880000000001	15.534140000000001	16.07103	16.58539	17.103010000000001	17.613009999999999	18.100349999999999	18.557469999999999	19.041260000000001	19.482759999999999	19.922190000000001	20.34159	20.743310000000001	21.16357	21.538709999999998	21.912210000000002	22.286560000000001	22.66104	23.024380000000001	23.35538	23.693619999999999	24.034179999999999	24.357959999999999	24.661380000000001	24.982890000000001	25.30209	25.57207	25.860589999999998	26.15213	26.446919999999999	26.716429999999999	26.98104	27.23265	27.495200000000001	27.767769999999999	28.002369999999999	28.242349999999998	28.478339999999999	28.721019999999999	28.96481	29.19922	29.402239999999999	29.61375	29.835750000000001	30.05301	30.271840000000001	30.48218	30.67212	30.869289999999999	31.06176	31.251709999999999	31.449169999999999	31.646560000000001	31.828140000000001	32.004600000000003	32.18085	32.350140000000003	32.52534	32.699869999999997	32.875129999999999	33.045659999999998	33.201560000000001	33.358879999999999	33.514670000000002	33.668799999999997	33.824590000000001	33.981380000000001	34.134450000000001	34.289650000000002	34.430030000000002	34.567549999999997	34.707410000000003	34.845030000000001	34.98245	35.121000000000002	35.2592	35.396509999999999	35.535069999999997	35.663490000000003	35.784050000000001	35.904209999999999	36.025320000000001	36.14443	36.265180000000001	36.385469999999998	36.510219999999997	36.631740000000001	36.751260000000002	36.871569999999998	36.978169999999999	37.082880000000003	37.188929999999999	37.293559999999999	37.399769999999997	37.505189999999999	37.610810000000001	37.717449999999999	37.822989999999997	37.928959999999996	38.034030000000001	38.133049999999997	38.22296	38.313339999999997	38.405270000000002	38.494970000000002	Measured N2	0.102004	0.124901	0.14984900000000001	0.17477699999999999	0.199739	0.28481699999999999	0.375305	0.46261799999999997	0.549786	0.63790400000000003	0.72823700000000002	0.80822400000000005	0.89593599999999995	0.94579199999999997	14.7546	15.508699999999999	16.306799999999999	17.113299999999999	17.9175	20.8324	24.3414	28.264600000000002	32.919899999999998	38.485799999999998	45.370399999999997	52.655700000000003	63.042099999999998	72.455699999999993	Fit	0.102004	0.124901	0.14984900000000001	0.17477699999999999	0.199739	0.28481699999999999	0.375305	0.46261799999999997	0.549786	0.63790400000000003	0.72823700000000002	0.80822400000000005	0.89593599999999995	0.94579199999999997	16.103760000000001	16.648499999999999	17.194579999999998	17.72833	18.295780000000001	20.752520000000001	24.030819999999999	28.117450000000002	32.54766	38.493259999999999	45.240690000000001	52.514749999999999	63.03257	72.353369999999998	Relative pressure


Amount adsorbed, cm3/g(STP)




TCB-TU800

Measured CO2	2.8489200000000002E-4	5.7015799999999997E-4	8.5481100000000003E-4	1.13959E-3	1.42391E-3	1.70835E-3	1.9917200000000002E-3	2.2753000000000001E-3	2.5581900000000001E-3	2.8406299999999998E-3	3.1233200000000002E-3	3.40523E-3	3.6867699999999998E-3	3.9689E-3	4.2503100000000002E-3	4.5322299999999999E-3	4.8140099999999996E-3	5.0947500000000003E-3	5.3753899999999999E-3	5.6559000000000002E-3	5.9363799999999998E-3	6.2162199999999997E-3	6.4957900000000004E-3	6.7753700000000002E-3	7.0546200000000002E-3	7.3336399999999998E-3	7.6120199999999997E-3	7.8902799999999995E-3	8.1691899999999998E-3	8.44022E-3	8.71859E-3	8.9971500000000006E-3	9.2749300000000007E-3	9.5531399999999999E-3	9.8300699999999998E-3	1.01078E-2	1.0385200000000001E-2	1.0663199999999999E-2	1.0939300000000001E-2	1.1217299999999999E-2	1.1493700000000001E-2	1.1770299999999999E-2	1.2045999999999999E-2	1.2323499999999999E-2	1.2599600000000001E-2	1.28757E-2	1.3151100000000001E-2	1.34278E-2	1.37018E-2	1.39775E-2	1.42524E-2	1.4529200000000001E-2	1.4802600000000001E-2	1.5077500000000001E-2	1.5352299999999999E-2	1.5626600000000001E-2	1.59013E-2	1.6176200000000002E-2	1.6451299999999999E-2	1.6725400000000001E-2	1.69996E-2	1.7273899999999998E-2	1.7548000000000001E-2	1.7821199999999999E-2	1.8078299999999999E-2	1.8351099999999999E-2	1.8624000000000002E-2	1.8896099999999999E-2	1.9150799999999999E-2	1.94228E-2	1.9696399999999999E-2	1.99668E-2	2.0238300000000001E-2	2.0510799999999999E-2	2.0783099999999999E-2	2.10546E-2	2.1326399999999999E-2	2.1596400000000002E-2	2.18683E-2	2.2139099999999998E-2	2.2410099999999999E-2	2.26816E-2	2.2952400000000001E-2	2.3221100000000001E-2	2.34936E-2	2.3760799999999999E-2	2.40322E-2	2.4301699999999999E-2	2.4569500000000001E-2	2.48373E-2	2.5104700000000001E-2	2.5374399999999998E-2	2.5641199999999999E-2	2.59098E-2	2.6176499999999998E-2	2.6446799999999999E-2	2.6714000000000002E-2	2.6980299999999999E-2	2.7248100000000001E-2	2.75134E-2	2.7779100000000001E-2	2.80475E-2	2.8313899999999999E-2	2.85493E-2	2.88145E-2	2.90756E-2	2.9339199999999999E-2	2.95997E-2	2.9861200000000001E-2	3.0122900000000001E-2	-2.1333499999999998E-2	-5.1166999999999997E-2	-7.2851700000000005E-2	-9.9071000000000006E-2	-0.108525	-0.124628	-0.13011700000000001	-0.13720499999999999	-0.13714000000000001	-0.13481399999999999	-0.12948399999999999	-0.11874999999999999	-0.104695	-9.3740599999999993E-2	-7.6990900000000001E-2	-6.2321300000000003E-2	-4.5357399999999999E-2	-1.8371200000000001E-2	7.0416100000000002E-3	3.7502000000000001E-2	6.4602599999999996E-2	9.4882300000000003E-2	0.12654099999999999	0.158943	0.194464	0.23492099999999999	0.27454699999999999	0.316581	0.35478599999999999	0.45050400000000002	0.49320799999999998	0.533412	0.57965999999999995	0.61880800000000002	0.66872100000000001	0.71298499999999998	0.75899300000000003	0.80537599999999998	0.86735099999999998	0.916462	0.97997400000000001	1.0371699999999999	1.09501	1.14852	1.2085399999999999	1.2645500000000001	1.3276399999999999	1.38289	1.4553400000000001	1.51342	1.5759399999999999	1.6300600000000001	1.7054100000000001	1.7755300000000001	1.8461700000000001	1.92635	1.9940199999999999	2.0642399999999999	2.1385100000000001	2.22139	2.2959299999999998	2.3651599999999999	2.4402900000000001	2.51735	2.7028300000000001	2.7829100000000002	2.8626399999999999	2.94807	3.1317699999999999	3.21698	3.2907799999999998	3.38666	3.4709099999999999	3.54861	3.6332200000000001	3.72404	3.8105799999999999	3.9077500000000001	3.99369	4.0880599999999996	4.1815300000000004	4.2703300000000004	4.3593599999999997	4.4689699999999997	4.5490599999999999	4.6709399999999999	4.75223	4.8470899999999997	4.9520499999999998	5.0578900000000004	5.1657999999999999	5.2496	5.3556600000000003	5.4548500000000004	5.5699100000000001	5.6574499999999999	5.7606700000000002	5.8749900000000004	5.9768699999999999	6.0899200000000002	6.2080399999999996	6.3048299999999999	6.4168900000000004	6.61972	6.7411099999999999	6.86172	6.9623499999999998	7.0868000000000002	7.2046799999999998	7.3153899999999998	Fit	2.8489200000000002E-4	5.7015799999999997E-4	8.5481100000000003E-4	1.13959E-3	1.42391E-3	1.70835E-3	1.9917200000000002E-3	2.2753000000000001E-3	2.5581900000000001E-3	2.8406299999999998E-3	3.1233200000000002E-3	3.40523E-3	3.6867699999999998E-3	3.9689E-3	4.2503100000000002E-3	4.5322299999999999E-3	4.8140099999999996E-3	5.0947500000000003E-3	5.3753899999999999E-3	5.6559000000000002E-3	5.9363799999999998E-3	6.2162199999999997E-3	6.4957900000000004E-3	6.7753700000000002E-3	7.0546200000000002E-3	7.3336399999999998E-3	7.6120199999999997E-3	7.8902799999999995E-3	8.1691899999999998E-3	8.44022E-3	8.71859E-3	8.9971500000000006E-3	9.2749300000000007E-3	9.5531399999999999E-3	9.8300699999999998E-3	1.01078E-2	1.0385200000000001E-2	1.0663199999999999E-2	1.0939300000000001E-2	1.1217299999999999E-2	1.1493700000000001E-2	1.1770299999999999E-2	1.2045999999999999E-2	1.2323499999999999E-2	1.2599600000000001E-2	1.28757E-2	1.3151100000000001E-2	1.34278E-2	1.37018E-2	1.39775E-2	1.42524E-2	1.4529200000000001E-2	1.4802600000000001E-2	1.5077500000000001E-2	1.5352299999999999E-2	1.5626600000000001E-2	1.59013E-2	1.6176200000000002E-2	1.6451299999999999E-2	1.6725400000000001E-2	1.69996E-2	1.7273899999999998E-2	1.7548000000000001E-2	1.7821199999999999E-2	1.8078299999999999E-2	1.8351099999999999E-2	1.8624000000000002E-2	1.8896099999999999E-2	1.9150799999999999E-2	1.94228E-2	1.9696399999999999E-2	1.99668E-2	2.0238300000000001E-2	2.0510799999999999E-2	2.0783099999999999E-2	2.10546E-2	2.1326399999999999E-2	2.1596400000000002E-2	2.18683E-2	2.2139099999999998E-2	2.2410099999999999E-2	2.26816E-2	2.2952400000000001E-2	2.3221100000000001E-2	2.34936E-2	2.3760799999999999E-2	2.40322E-2	2.4301699999999999E-2	2.4569500000000001E-2	2.48373E-2	2.5104700000000001E-2	2.5374399999999998E-2	2.5641199999999999E-2	2.59098E-2	2.6176499999999998E-2	2.6446799999999999E-2	2.6714000000000002E-2	2.6980299999999999E-2	2.7248100000000001E-2	2.75134E-2	2.7779100000000001E-2	2.80475E-2	2.8313899999999999E-2	2.85493E-2	2.88145E-2	2.90756E-2	2.9339199999999999E-2	2.95997E-2	2.9861200000000001E-2	3.0122900000000001E-2	4.5316679999999998E-2	9.2498319999999995E-2	0.14142979999999999	0.1922893	0.24487149999999999	0.29911179999999998	0.35489559999999998	0.41207369999999999	0.47040029999999999	0.52975220000000001	0.59011009999999997	0.6511034	0.71289259999999999	0.77536859999999996	0.83799129999999999	0.90128509999999995	0.96463500000000002	1.0279929999999999	1.0912790000000001	1.1543779999999999	1.2174700000000001	1.2798719999999999	1.3421970000000001	1.404058	1.4651989999999999	1.526289	1.58633	1.645618	1.7050449999999999	1.762113	1.8192759999999999	1.8764780000000001	1.9335199999999999	1.9887699999999999	2.043015	2.0974179999999998	2.1517550000000001	2.204183	2.2552590000000001	2.3066870000000002	2.3578199999999998	2.408547	2.4561660000000001	2.5040969999999998	2.5517859999999999	2.5994739999999998	2.646925	2.691004	2.7346529999999998	2.778572	2.8223639999999999	2.8664589999999999	2.9088539999999998	2.948817	2.9887649999999999	3.0286409999999999	3.0685739999999999	3.1085370000000001	3.1485280000000002	3.185009	3.2210179999999999	3.2570410000000001	3.293037	3.3289149999999998	3.3626779999999998	3.3985029999999998	3.4321649999999999	3.464194	3.4941740000000001	3.5261909999999999	3.5583969999999998	3.5902250000000002	3.6221830000000002	3.6542590000000001	3.684933	3.7132670000000001	3.7416330000000002	3.7698109999999998	3.798187	3.8264480000000001	3.8547310000000001	3.8830650000000002	3.9113259999999999	3.9386420000000002	3.963765	3.9883989999999998	4.01342	4.0382660000000001	4.0629559999999998	4.0876450000000002	4.112298	4.137162	4.161759	4.1865220000000001	4.2084849999999996	4.2303959999999998	4.2520550000000004	4.2736409999999996	4.2953489999999999	4.3168540000000002	4.3383919999999998	4.3601479999999997	4.381742	4.4008240000000001	4.4223210000000002	4.4432669999999996	4.4620139999999999	4.4805409999999997	4.4991399999999997	4.5177519999999998	Measured N2	9.9790699999999996E-2	0.124898	0.14990000000000001	0.17482900000000001	0.199792	0.28690700000000002	0.37567600000000001	0.46314699999999998	0.55080300000000004	0.63883299999999998	0.72959700000000005	0.80960100000000002	0.89859599999999995	0.94830000000000003	1.7858499999999999	2.0346099999999998	2.29881	2.58588	2.8985099999999999	4.1336500000000003	5.6912399999999996	7.5452300000000001	9.74024	12.3126	15.457700000000001	18.777999999999999	23.616299999999999	27.988	Fit	9.9790699999999996E-2	0.124898	0.14990000000000001	0.17482900000000001	0.199792	0.28690700000000002	0.37567600000000001	0.46314699999999998	0.55080300000000004	0.63883299999999998	0.72959700000000005	0.80960100000000002	0.89859599999999995	0.94830000000000003	4.5671419999999996	4.7652970000000003	4.9460930000000003	5.1215349999999997	5.2977379999999998	5.9756640000000001	6.6453350000000002	7.4249830000000001	8.8122249999999998	11.48108	14.88109	18.215219999999999	23.283270000000002	27.600809999999999	Realative pressure


Amount adsorbed, cm3/g (STP)




TCB-TU750

Measured CO2	3.5251E-4	6.3909600000000002E-4	9.2826300000000003E-4	1.2740099999999999E-3	1.54123E-3	1.8803299999999999E-3	2.1944199999999999E-3	2.53682E-3	2.9009299999999999E-3	3.25976E-3	3.6466799999999998E-3	4.0164900000000002E-3	4.4089899999999998E-3	4.7929399999999999E-3	5.2005300000000001E-3	5.6116999999999998E-3	6.01652E-3	6.4191700000000001E-3	6.8396100000000003E-3	7.2598200000000002E-3	7.6805399999999996E-3	8.1091099999999992E-3	8.5408800000000007E-3	8.9764600000000003E-3	9.4255499999999996E-3	9.8582300000000008E-3	1.03105E-2	1.0751200000000001E-2	1.1211199999999999E-2	1.16556E-2	1.21187E-2	1.2570700000000001E-2	1.30195E-2	1.34892E-2	1.3948500000000001E-2	1.44151E-2	1.48854E-2	1.53521E-2	1.5813899999999999E-2	1.62699E-2	1.6736899999999999E-2	1.7193099999999999E-2	1.7648299999999999E-2	1.8108900000000001E-2	1.8558700000000001E-2	1.90222E-2	1.9477899999999999E-2	1.9920299999999998E-2	2.0384699999999999E-2	2.08506E-2	2.1305899999999999E-2	2.1767100000000001E-2	2.2221299999999999E-2	2.2684300000000001E-2	2.3146900000000002E-2	2.3605299999999999E-2	2.4065199999999998E-2	2.4519900000000001E-2	2.49792E-2	2.5438599999999999E-2	2.5896300000000001E-2	2.6354800000000001E-2	2.68148E-2	2.7272299999999999E-2	2.7730000000000001E-2	2.8188700000000001E-2	2.8646399999999999E-2	2.9102699999999999E-2	2.95593E-2	3.0014800000000001E-2	0.92781599999999997	2.2561	3.5308600000000001	4.4951299999999996	5.9590699999999996	6.9612100000000003	8.1235099999999996	9.1031700000000004	9.9446899999999996	10.8177	11.5198	12.3362	13.0083	13.738300000000001	14.319100000000001	14.874499999999999	15.4674	16.072600000000001	16.563500000000001	17.059000000000001	17.547499999999999	17.986799999999999	18.398299999999999	18.784099999999999	19.084499999999998	19.491399999999999	19.773499999999999	20.131499999999999	20.3674	20.697399999999998	20.913699999999999	21.197399999999998	21.5059	21.672899999999998	21.9145	22.110099999999999	22.2727	22.4725	22.693300000000001	22.946400000000001	23.139299999999999	23.398399999999999	23.663900000000002	23.8935	24.192299999999999	24.4041	24.660699999999999	24.999300000000002	25.198699999999999	25.3962	25.660299999999999	25.8889	26.165400000000002	26.380600000000001	26.595099999999999	26.841799999999999	27.078600000000002	27.347200000000001	27.575600000000001	27.809200000000001	28.0501	28.2836	28.517900000000001	28.762899999999998	29.008199999999999	29.247800000000002	29.483699999999999	29.729700000000001	29.974499999999999	30.220500000000001	Fit	3.5251E-4	6.3909600000000002E-4	9.2826300000000003E-4	1.2740099999999999E-3	1.54123E-3	1.8803299999999999E-3	2.1944199999999999E-3	2.53682E-3	2.9009299999999999E-3	3.25976E-3	3.6466799999999998E-3	4.0164900000000002E-3	4.4089899999999998E-3	4.7929399999999999E-3	5.2005300000000001E-3	5.6116999999999998E-3	6.01652E-3	6.4191700000000001E-3	6.8396100000000003E-3	7.2598200000000002E-3	7.6805399999999996E-3	8.1091099999999992E-3	8.5408800000000007E-3	8.9764600000000003E-3	9.4255499999999996E-3	9.8582300000000008E-3	1.03105E-2	1.0751200000000001E-2	1.1211199999999999E-2	1.16556E-2	1.21187E-2	1.2570700000000001E-2	1.30195E-2	1.34892E-2	1.3948500000000001E-2	1.44151E-2	1.48854E-2	1.53521E-2	1.5813899999999999E-2	1.62699E-2	1.6736899999999999E-2	1.7193099999999999E-2	1.7648299999999999E-2	1.8108900000000001E-2	1.8558700000000001E-2	1.90222E-2	1.9477899999999999E-2	1.9920299999999998E-2	2.0384699999999999E-2	2.08506E-2	2.1305899999999999E-2	2.1767100000000001E-2	2.2221299999999999E-2	2.2684300000000001E-2	2.3146900000000002E-2	2.3605299999999999E-2	2.4065199999999998E-2	2.4519900000000001E-2	2.49792E-2	2.5438599999999999E-2	2.5896300000000001E-2	2.6354800000000001E-2	2.68148E-2	2.7272299999999999E-2	2.7730000000000001E-2	2.8188700000000001E-2	2.8646399999999999E-2	2.9102699999999999E-2	2.95593E-2	3.0014800000000001E-2	1.424938	2.7082709999999999	3.9025150000000002	5.1683450000000004	6.0525130000000003	7.0762679999999998	7.9462460000000004	8.8223730000000007	9.6873509999999996	10.479609999999999	11.2758	11.98649	12.695959999999999	13.35345	14.004530000000001	14.621090000000001	15.205170000000001	15.74464	16.285959999999999	16.797979999999999	17.284770000000002	17.75732	18.212669999999999	18.64507	19.08353	19.468240000000002	19.870380000000001	20.23583	20.600570000000001	20.952929999999999	21.28566	21.603529999999999	21.919149999999998	22.220559999999999	22.505289999999999	22.794540000000001	23.07348	23.327300000000001	23.57846	23.826460000000001	24.063189999999999	24.27994	24.496220000000001	24.715070000000001	24.923030000000001	25.11504	25.303820000000002	25.487089999999998	25.679469999999998	25.86307	26.026630000000001	26.192309999999999	26.35547	26.521789999999999	26.68797	26.83155	26.974910000000001	27.11665	27.259820000000001	27.403020000000001	27.5457	27.671250000000001	27.795359999999999	27.918780000000002	28.042259999999999	28.16601	28.289490000000001	28.410810000000001	28.517379999999999	28.62369	Measured N2	9.9751900000000004E-2	0.12481399999999999	0.150006	0.17496100000000001	0.199929	0.28617900000000002	0.37557000000000001	0.46303899999999998	0.55047400000000002	0.63844599999999996	0.72894800000000004	0.80877500000000002	0.896976	0.94745299999999999	6.4720899999999997	6.9095300000000002	7.31473	7.7313799999999997	8.1725200000000005	9.8004099999999994	11.804600000000001	14.1107	16.869700000000002	20.174299999999999	24.3413	28.957000000000001	35.901899999999998	42.1524	Fit	9.9751900000000004E-2	0.12481399999999999	0.150006	0.17496100000000001	0.199929	0.28617900000000002	0.37557000000000001	0.46303899999999998	0.55047400000000002	0.63844599999999996	0.72894800000000004	0.80877500000000002	0.896976	0.94745299999999999	7.3425330000000004	7.6814999999999998	7.9941550000000001	8.2962249999999997	8.6002069999999993	9.8376509999999993	11.56345	13.979509999999999	16.648230000000002	20.125430000000001	24.23865	28.858270000000001	35.854109999999999	42.086509999999997	Relative pressure


Amount adsorbed,cm3/g (STP)




TCB-TU700

Measured CO2	1.47272E-4	2.7162900000000001E-4	4.0636900000000001E-4	5.3947700000000001E-4	6.8172899999999995E-4	8.2864799999999997E-4	9.7561700000000002E-4	1.1305899999999999E-3	1.2974600000000001E-3	1.46429E-3	1.6371300000000001E-3	1.8156699999999999E-3	1.99431E-3	2.1851800000000001E-3	2.3734199999999998E-3	2.5635599999999999E-3	2.76114E-3	2.95816E-3	3.1635299999999999E-3	3.3592100000000001E-3	3.5684100000000002E-3	3.7769800000000001E-3	3.9944300000000002E-3	4.2073500000000003E-3	4.4199799999999996E-3	4.6367999999999999E-3	4.85602E-3	5.0823099999999996E-3	5.3029599999999998E-3	5.5246799999999997E-3	5.7528500000000003E-3	5.9787199999999999E-3	6.2038900000000001E-3	6.4432100000000004E-3	6.6663800000000004E-3	6.9054499999999996E-3	7.1370799999999996E-3	7.3650499999999997E-3	7.6011100000000003E-3	7.8358999999999998E-3	8.0738200000000006E-3	8.3100699999999993E-3	8.5480899999999995E-3	8.7925099999999999E-3	9.0292099999999993E-3	9.2689599999999997E-3	9.5067699999999995E-3	9.75175E-3	9.9951599999999995E-3	1.0241200000000001E-2	1.04844E-2	1.07279E-2	1.0977499999999999E-2	1.1221E-2	1.1464800000000001E-2	1.1714199999999999E-2	1.1963700000000001E-2	1.22113E-2	1.2458500000000001E-2	1.27093E-2	1.2955100000000001E-2	1.32079E-2	1.34559E-2	1.3703399999999999E-2	1.39569E-2	1.4208200000000001E-2	1.4453000000000001E-2	1.4709E-2	1.49637E-2	1.5215299999999999E-2	1.5467099999999999E-2	1.5716899999999999E-2	1.5976299999999999E-2	1.6228599999999999E-2	1.6486899999999999E-2	1.6743500000000001E-2	1.6994700000000001E-2	1.7248699999999999E-2	1.75021E-2	1.77608E-2	1.8008799999999998E-2	1.8266500000000001E-2	1.8523999999999999E-2	1.87791E-2	1.9037100000000001E-2	1.9290399999999999E-2	1.9535799999999999E-2	1.9792299999999999E-2	2.0049500000000001E-2	2.03067E-2	2.05504E-2	2.0807599999999999E-2	2.1068099999999999E-2	2.1325500000000001E-2	2.1585500000000001E-2	2.1826000000000002E-2	2.20845E-2	2.2344900000000001E-2	2.2592399999999999E-2	2.2853600000000002E-2	2.3111900000000001E-2	2.3371699999999999E-2	2.3613499999999999E-2	2.38728E-2	2.41339E-2	2.43722E-2	2.4631E-2	2.4890900000000001E-2	2.5150700000000002E-2	2.53893E-2	2.56487E-2	2.5908199999999999E-2	2.6167599999999999E-2	2.6415500000000001E-2	2.6674900000000001E-2	2.6910199999999999E-2	2.71705E-2	2.7433800000000001E-2	2.76765E-2	2.79388E-2	2.81876E-2	2.8450699999999999E-2	2.8681700000000001E-2	2.8944899999999999E-2	2.9202599999999999E-2	2.9446400000000001E-2	2.9708700000000001E-2	2.9955900000000001E-2	3.0211200000000001E-2	1.13984	2.4522599999999999	3.6480600000000001	4.8365999999999998	5.9523200000000003	7.0331200000000003	8.1056500000000007	9.1179600000000001	10.0619	10.9756	11.8432	12.6669	13.4876	14.212199999999999	14.9573	15.6835	16.352799999999998	17.022200000000002	17.627099999999999	18.306000000000001	18.880299999999998	19.460699999999999	19.9693	20.514700000000001	21.061199999999999	21.575299999999999	22.0716	22.517600000000002	23.004999999999999	23.4861	23.913699999999999	24.357900000000001	24.806000000000001	25.1416	25.609200000000001	25.947199999999999	26.3476	26.773	27.1373	27.509599999999999	27.861499999999999	28.222200000000001	28.5671	28.8627	29.217300000000002	29.552700000000002	29.902799999999999	30.199000000000002	30.503499999999999	30.793500000000002	31.099799999999998	31.406099999999999	31.665099999999999	31.9754	32.2789	32.541800000000002	32.798900000000003	33.072600000000001	33.344799999999999	33.591999999999999	33.878500000000003	34.110999999999997	34.374600000000001	34.642699999999998	34.866999999999997	35.105600000000003	35.3917	35.597700000000003	35.812199999999997	36.049900000000001	36.288499999999999	36.536499999999997	36.724200000000003	36.964100000000002	37.156599999999997	37.360100000000003	37.6143	37.839199999999998	38.072499999999998	38.263300000000001	38.5092	38.704000000000001	38.897799999999997	39.111800000000002	39.298299999999998	39.518799999999999	39.765599999999999	39.957999999999998	40.152099999999997	40.348700000000001	40.606299999999997	40.803800000000003	40.980400000000003	41.175600000000003	41.354900000000001	41.627800000000001	41.813299999999998	41.988900000000001	42.225700000000003	42.396299999999997	42.589100000000002	42.763199999999998	43.003900000000002	43.188299999999998	43.3491	43.573900000000002	43.752600000000001	43.921300000000002	44.084899999999998	44.313000000000002	44.484200000000001	44.656100000000002	44.821300000000001	45.0291	45.205100000000002	45.430300000000003	45.597200000000001	45.733899999999998	45.9634	46.112000000000002	46.327500000000001	46.467399999999998	46.6935	46.831699999999998	46.985799999999998	47.204500000000003	47.347099999999998	47.549799999999998	47.72	Fit	1.47272E-4	2.7162900000000001E-4	4.0636900000000001E-4	5.3947700000000001E-4	6.8172899999999995E-4	8.2864799999999997E-4	9.7561700000000002E-4	1.1305899999999999E-3	1.2974600000000001E-3	1.46429E-3	1.6371300000000001E-3	1.8156699999999999E-3	1.99431E-3	2.1851800000000001E-3	2.3734199999999998E-3	2.5635599999999999E-3	2.76114E-3	2.95816E-3	3.1635299999999999E-3	3.3592100000000001E-3	3.5684100000000002E-3	3.7769800000000001E-3	3.9944300000000002E-3	4.2073500000000003E-3	4.4199799999999996E-3	4.6367999999999999E-3	4.85602E-3	5.0823099999999996E-3	5.3029599999999998E-3	5.5246799999999997E-3	5.7528500000000003E-3	5.9787199999999999E-3	6.2038900000000001E-3	6.4432100000000004E-3	6.6663800000000004E-3	6.9054499999999996E-3	7.1370799999999996E-3	7.3650499999999997E-3	7.6011100000000003E-3	7.8358999999999998E-3	8.0738200000000006E-3	8.3100699999999993E-3	8.5480899999999995E-3	8.7925099999999999E-3	9.0292099999999993E-3	9.2689599999999997E-3	9.5067699999999995E-3	9.75175E-3	9.9951599999999995E-3	1.0241200000000001E-2	1.04844E-2	1.07279E-2	1.0977499999999999E-2	1.1221E-2	1.1464800000000001E-2	1.1714199999999999E-2	1.1963700000000001E-2	1.22113E-2	1.2458500000000001E-2	1.27093E-2	1.2955100000000001E-2	1.32079E-2	1.34559E-2	1.3703399999999999E-2	1.39569E-2	1.4208200000000001E-2	1.4453000000000001E-2	1.4709E-2	1.49637E-2	1.5215299999999999E-2	1.5467099999999999E-2	1.5716899999999999E-2	1.5976299999999999E-2	1.6228599999999999E-2	1.6486899999999999E-2	1.6743500000000001E-2	1.6994700000000001E-2	1.7248699999999999E-2	1.75021E-2	1.77608E-2	1.8008799999999998E-2	1.8266500000000001E-2	1.8523999999999999E-2	1.87791E-2	1.9037100000000001E-2	1.9290399999999999E-2	1.9535799999999999E-2	1.9792299999999999E-2	2.0049500000000001E-2	2.03067E-2	2.05504E-2	2.0807599999999999E-2	2.1068099999999999E-2	2.1325500000000001E-2	2.1585500000000001E-2	2.1826000000000002E-2	2.20845E-2	2.2344900000000001E-2	2.2592399999999999E-2	2.2853600000000002E-2	2.3111900000000001E-2	2.3371699999999999E-2	2.3613499999999999E-2	2.38728E-2	2.41339E-2	2.43722E-2	2.4631E-2	2.4890900000000001E-2	2.5150700000000002E-2	2.53893E-2	2.56487E-2	2.5908199999999999E-2	2.6167599999999999E-2	2.6415500000000001E-2	2.6674900000000001E-2	2.6910199999999999E-2	2.71705E-2	2.7433800000000001E-2	2.76765E-2	2.79388E-2	2.81876E-2	2.8450699999999999E-2	2.8681700000000001E-2	2.8944899999999999E-2	2.9202599999999999E-2	2.9446400000000001E-2	2.9708700000000001E-2	2.9955900000000001E-2	3.0211200000000001E-2	0.96742039999999996	1.878825	2.9383910000000002	3.9992589999999999	5.0904040000000004	6.1426049999999996	7.1259889999999997	8.0839009999999991	9.0475630000000002	9.9492220000000007	10.826560000000001	11.680210000000001	12.488670000000001	13.30964	14.07738	14.80899	15.54233	16.240269999999999	16.930009999999999	17.574470000000002	18.216370000000001	18.85295	19.466830000000002	20.06766	20.626449999999998	21.19087	21.737580000000001	22.280200000000001	22.8093	23.297809999999998	23.799510000000001	24.289919999999999	24.743469999999999	25.225519999999999	25.67362	26.113130000000002	26.538959999999999	26.95806	27.36824	27.761009999999999	28.159020000000002	28.55424	28.922039999999999	29.293009999999999	29.652259999999998	30.01614	30.35501	30.691330000000001	31.025490000000001	31.36327	31.696149999999999	31.997820000000001	32.307049999999997	32.608730000000001	32.910769999999999	33.219760000000001	33.500250000000001	33.776119999999999	34.051540000000003	34.330970000000001	34.60483	34.878860000000003	35.126260000000002	35.373159999999999	35.626049999999999	35.876739999999998	36.120950000000001	36.376330000000003	36.60416	36.828110000000002	37.052230000000002	37.27458	37.505459999999999	37.730029999999999	37.959829999999997	38.162799999999997	38.361499999999999	38.56241	38.76285	38.967480000000002	39.163640000000001	39.36748	39.565730000000002	39.744399999999999	39.9251	40.102510000000002	40.274389999999997	40.454039999999999	40.634180000000001	40.814320000000002	40.984999999999999	41.154159999999997	41.314210000000003	41.472360000000002	41.632109999999997	41.779879999999999	41.93871	42.098700000000001	42.250770000000003	42.411250000000003	42.569960000000002	42.713180000000001	42.842880000000001	42.981969999999997	43.122030000000002	43.249859999999998	43.388680000000001	43.528089999999999	43.667450000000002	43.795439999999999	43.934579999999997	44.073779999999999	44.19679	44.312150000000003	44.432850000000002	44.542340000000003	44.663469999999997	44.785989999999998	44.898919999999997	45.020980000000002	45.136749999999999	45.259180000000001	45.366669999999999	45.489139999999999	45.599760000000003	45.697980000000001	45.803669999999997	45.903260000000003	46.006120000000003	Measured N2	0.102242	0.12481200000000001	0.14971899999999999	0.174618	0.199569	0.284244	0.37580799999999998	0.46274399999999999	0.55072100000000002	0.63773999999999997	0.72865100000000005	0.80840400000000001	0.89689799999999997	0.94747000000000003	15.3649	16.182200000000002	17.050999999999998	17.915400000000002	18.791499999999999	21.845099999999999	25.574400000000001	29.620699999999999	34.4054	40.061900000000001	47.0349	54.32	64.424300000000002	72.664500000000004	Fit	0.102242	0.12481200000000001	0.14971899999999999	0.174618	0.199569	0.284244	0.37580799999999998	0.46274399999999999	0.55072100000000002	0.63773999999999997	0.72865100000000005	0.80840400000000001	0.89689799999999997	0.94747000000000003	17.147680000000001	17.692060000000001	18.24381	18.780519999999999	19.33455	21.732030000000002	25.114159999999998	29.42165	34.106619999999999	39.897950000000002	46.921790000000001	54.144669999999998	64.359549999999999	72.554490000000001	Relative pressure


Amount adsorbed, cm3/g (STP)




TCB-TU600

Measured CO2	7.0189499999999996E-5	1.71554E-4	2.9303199999999998E-4	4.3045300000000002E-4	5.81783E-4	7.4558299999999997E-4	9.1794499999999998E-4	1.10144E-3	1.2915800000000001E-3	1.4899900000000001E-3	1.6958699999999999E-3	1.90639E-3	2.12182E-3	2.3429499999999999E-3	2.5684599999999998E-3	2.7969499999999999E-3	3.0291699999999999E-3	3.2647399999999999E-3	3.5031900000000002E-3	3.74362E-3	3.9875800000000001E-3	4.2329999999999998E-3	4.4806500000000001E-3	4.7313900000000002E-3	4.98162E-3	5.2337299999999998E-3	5.48958E-3	5.7476799999999998E-3	6.0045300000000001E-3	6.2638099999999999E-3	6.5236000000000001E-3	6.7851700000000001E-3	7.0474200000000004E-3	7.3112799999999999E-3	7.5747599999999998E-3	7.8404500000000005E-3	8.1067899999999991E-3	8.3715700000000001E-3	8.6400000000000001E-3	8.9095300000000006E-3	9.1793599999999993E-3	9.4501600000000009E-3	9.7212800000000005E-3	9.9944100000000004E-3	1.02655E-2	1.05384E-2	1.08129E-2	1.10878E-2	1.13638E-2	1.16399E-2	1.19162E-2	1.21943E-2	1.24715E-2	1.27499E-2	1.30285E-2	1.329E-2	1.35517E-2	1.38128E-2	1.4075600000000001E-2	1.4337900000000001E-2	1.4601299999999999E-2	1.48649E-2	1.51173E-2	1.53811E-2	1.5644999999999999E-2	1.5909400000000001E-2	1.61741E-2	1.6439599999999999E-2	1.6705399999999999E-2	1.69698E-2	1.72351E-2	1.75015E-2	1.7766899999999999E-2	1.80325E-2	1.8298399999999999E-2	1.85636E-2	1.8829800000000001E-2	1.9095299999999999E-2	1.93604E-2	1.9626399999999999E-2	1.9892300000000002E-2	2.0158700000000002E-2	2.0424899999999999E-2	2.0691899999999999E-2	2.0958999999999998E-2	2.1226200000000001E-2	2.1493700000000001E-2	2.17602E-2	2.2027600000000001E-2	2.2296E-2	2.2564799999999999E-2	2.2832000000000002E-2	2.3099700000000001E-2	2.3367099999999998E-2	2.36349E-2	2.39031E-2	2.4171499999999999E-2	2.44377E-2	2.47058E-2	2.4973100000000002E-2	2.52404E-2	2.5508300000000001E-2	2.5775099999999999E-2	2.6042200000000001E-2	2.6284200000000001E-2	2.6551399999999999E-2	2.68206E-2	2.7088899999999999E-2	2.73574E-2	2.76251E-2	2.7892299999999998E-2	2.8159699999999999E-2	2.8427999999999998E-2	2.86959E-2	2.89622E-2	2.92264E-2	2.94892E-2	2.97556E-2	3.0019400000000002E-2	2.2621699999999998	4.1967299999999996	5.9102800000000002	7.4500500000000001	8.8407199999999992	10.101800000000001	11.2692	12.325900000000001	13.309900000000001	14.2072	15.034000000000001	15.822800000000001	16.5732	17.268899999999999	17.923100000000002	18.5425	19.132999999999999	19.694800000000001	20.2303	20.744599999999998	21.229299999999999	21.684699999999999	22.1144	22.5336	22.948699999999999	23.3475	23.7258	24.073899999999998	24.429099999999998	24.764500000000002	25.084299999999999	25.382000000000001	25.692299999999999	25.974699999999999	26.248799999999999	26.520499999999998	26.787099999999999	27.064900000000002	27.318999999999999	27.536300000000001	27.7699	28.0017	28.232199999999999	28.4498	28.668600000000001	28.873200000000001	29.066800000000001	29.262699999999999	29.449000000000002	29.628699999999998	29.810099999999998	29.984300000000001	30.150600000000001	30.296700000000001	30.458300000000001	30.702400000000001	30.945499999999999	31.193899999999999	31.4312	31.673300000000001	31.9072	32.139200000000002	32.454999999999998	32.685299999999998	32.915399999999998	33.139899999999997	33.366199999999999	33.582900000000002	33.799700000000001	34.023800000000001	34.239100000000001	34.451099999999997	34.670099999999998	34.875500000000002	35.083199999999998	35.2941	35.491500000000002	35.693199999999997	35.893900000000002	36.094200000000001	36.288699999999999	36.4818	36.676499999999997	36.865600000000001	37.054900000000004	37.240699999999997	37.430199999999999	37.621400000000001	37.809800000000003	37.9878	38.161999999999999	38.349699999999999	38.530700000000003	38.707000000000001	38.883499999999998	39.0533	39.222299999999997	39.400700000000001	39.566699999999997	39.732399999999998	39.897300000000001	40.060499999999998	40.224200000000003	40.390300000000003	40.633800000000001	40.801699999999997	40.9529	41.115499999999997	41.263599999999997	41.424900000000001	41.583100000000002	41.740499999999997	41.886000000000003	42.0351	42.199399999999997	42.345700000000001	42.5105	42.635899999999999	42.784599999999998	Fit	7.0189499999999996E-5	1.71554E-4	2.9303199999999998E-4	4.3045300000000002E-4	5.81783E-4	7.4558299999999997E-4	9.1794499999999998E-4	1.10144E-3	1.2915800000000001E-3	1.4899900000000001E-3	1.6958699999999999E-3	1.90639E-3	2.12182E-3	2.3429499999999999E-3	2.5684599999999998E-3	2.7969499999999999E-3	3.0291699999999999E-3	3.2647399999999999E-3	3.5031900000000002E-3	3.74362E-3	3.9875800000000001E-3	4.2329999999999998E-3	4.4806500000000001E-3	4.7313900000000002E-3	4.98162E-3	5.2337299999999998E-3	5.48958E-3	5.7476799999999998E-3	6.0045300000000001E-3	6.2638099999999999E-3	6.5236000000000001E-3	6.7851700000000001E-3	7.0474200000000004E-3	7.3112799999999999E-3	7.5747599999999998E-3	7.8404500000000005E-3	8.1067899999999991E-3	8.3715700000000001E-3	8.6400000000000001E-3	8.9095300000000006E-3	9.1793599999999993E-3	9.4501600000000009E-3	9.7212800000000005E-3	9.9944100000000004E-3	1.02655E-2	1.05384E-2	1.08129E-2	1.10878E-2	1.13638E-2	1.16399E-2	1.19162E-2	1.21943E-2	1.24715E-2	1.27499E-2	1.30285E-2	1.329E-2	1.35517E-2	1.38128E-2	1.4075600000000001E-2	1.4337900000000001E-2	1.4601299999999999E-2	1.48649E-2	1.51173E-2	1.53811E-2	1.5644999999999999E-2	1.5909400000000001E-2	1.61741E-2	1.6439599999999999E-2	1.6705399999999999E-2	1.69698E-2	1.72351E-2	1.75015E-2	1.7766899999999999E-2	1.80325E-2	1.8298399999999999E-2	1.85636E-2	1.8829800000000001E-2	1.9095299999999999E-2	1.93604E-2	1.9626399999999999E-2	1.9892300000000002E-2	2.0158700000000002E-2	2.0424899999999999E-2	2.0691899999999999E-2	2.0958999999999998E-2	2.1226200000000001E-2	2.1493700000000001E-2	2.17602E-2	2.2027600000000001E-2	2.2296E-2	2.2564799999999999E-2	2.2832000000000002E-2	2.3099700000000001E-2	2.3367099999999998E-2	2.36349E-2	2.39031E-2	2.4171499999999999E-2	2.44377E-2	2.47058E-2	2.4973100000000002E-2	2.52404E-2	2.5508300000000001E-2	2.5775099999999999E-2	2.6042200000000001E-2	2.6284200000000001E-2	2.6551399999999999E-2	2.68206E-2	2.7088899999999999E-2	2.73574E-2	2.76251E-2	2.7892299999999998E-2	2.8159699999999999E-2	2.8427999999999998E-2	2.86959E-2	2.89622E-2	2.92264E-2	2.94892E-2	2.97556E-2	3.0019400000000002E-2	0.45636850000000001	1.1686810000000001	2.102236	3.2266270000000001	4.4617620000000002	5.7184210000000002	6.925268	8.0952979999999997	9.1921029999999995	10.24553	11.252700000000001	12.203150000000001	13.103899999999999	13.96419	14.785589999999999	15.569889999999999	16.327449999999999	17.038129999999999	17.724530000000001	18.388850000000001	19.012810000000002	19.63186	20.201360000000001	20.777950000000001	21.303129999999999	21.83061	22.330200000000001	22.81945	23.295680000000001	23.74081	24.186820000000001	24.614799999999999	25.021450000000002	25.430589999999999	25.821249999999999	26.192740000000001	26.56514	26.932670000000002	27.270710000000001	27.610140000000001	27.949940000000002	28.27891	28.586179999999999	28.89573	29.202970000000001	29.505330000000001	29.78546	30.065989999999999	30.347650000000002	30.62941	30.892880000000002	31.148399999999999	31.403089999999999	31.65889	31.914870000000001	32.141550000000002	32.35792	32.573790000000002	32.791060000000002	33.007919999999999	33.22569	33.431640000000002	33.619500000000002	33.815849999999998	34.012270000000001	34.209060000000001	34.406080000000003	34.60369	34.785269999999997	34.962490000000003	35.140309999999999	35.318869999999997	35.496760000000002	35.674790000000002	35.853009999999998	36.024180000000001	36.184989999999999	36.345370000000003	36.505510000000001	36.66619	36.826819999999998	36.987740000000002	37.148539999999997	37.309069999999998	37.453679999999999	37.598350000000003	37.743169999999999	37.887459999999997	38.032229999999998	38.17754	38.323070000000001	38.467739999999999	38.612670000000001	38.745609999999999	38.875190000000003	39.004959999999997	39.134830000000001	39.263629999999999	39.393360000000001	39.522689999999997	39.652030000000003	39.781660000000002	39.91075	40.034489999999998	40.138460000000002	40.253270000000001	40.368929999999999	40.484200000000001	40.599559999999997	40.714579999999998	40.82938	40.94426	41.059539999999998	41.174639999999997	41.289050000000003	41.394109999999998	41.494149999999998	41.595570000000002	41.695999999999998	Measured N2	0.10008599999999999	0.124616	0.149482	0.174459	0.19944400000000001	0.28262999999999999	0.37382300000000002	0.461621	0.54874999999999996	0.63668999999999998	0.72712699999999997	0.80750699999999997	0.89628099999999999	0.94644499999999998	33.347099999999998	35.014099999999999	36.631900000000002	38.243899999999996	39.8446	44.990600000000001	51.030299999999997	57.452399999999997	64.852000000000004	73.52	83.8626	94.291399999999996	107.52	117.352	Fit	0.10008599999999999	0.124616	0.149482	0.174459	0.19944400000000001	0.28262999999999999	0.37382300000000002	0.461621	0.54874999999999996	0.63668999999999998	0.72712699999999997	0.80750699999999997	0.89628099999999999	0.94644499999999998	33.258299999999998	34.867019999999997	36.574089999999998	38.039169999999999	39.813009999999998	45.268320000000003	51.26482	57.49541	64.713759999999994	73.378270000000001	83.972830000000002	94.17765	107.6088	117.3229	Realative pressure


Amount adsorbed, cm3/g (STP)




CB-HT

Measured CO2	2.2092800000000001E-4	4.6090200000000001E-4	7.1164899999999996E-4	9.6344300000000003E-4	1.22507E-3	1.48895E-3	1.7543700000000001E-3	2.0227299999999999E-3	2.2956600000000001E-3	2.5693199999999999E-3	2.8438199999999999E-3	3.1166900000000001E-3	3.3938599999999998E-3	3.6725500000000001E-3	3.9514299999999997E-3	4.2325899999999996E-3	4.51323E-3	4.7959300000000003E-3	5.0808399999999997E-3	5.3647199999999999E-3	5.6503100000000004E-3	5.9344799999999998E-3	6.2209199999999996E-3	6.5079600000000001E-3	6.7951299999999999E-3	7.0800000000000004E-3	7.3709700000000001E-3	7.6543399999999999E-3	7.9441700000000004E-3	8.2339600000000002E-3	8.5209799999999992E-3	8.8106199999999999E-3	9.1014300000000006E-3	9.39276E-3	9.6841900000000005E-3	9.97521E-3	1.0260999999999999E-2	1.05521E-2	1.0845E-2	1.1136699999999999E-2	1.1427100000000001E-2	1.17102E-2	1.20024E-2	1.22936E-2	1.25848E-2	1.28675E-2	1.31506E-2	1.34419E-2	1.3733199999999999E-2	1.40251E-2	1.4315899999999999E-2	1.4598E-2	1.48909E-2	1.5181399999999999E-2	1.54669E-2	1.5759200000000001E-2	1.6052299999999999E-2	1.6346900000000001E-2	1.66263E-2	1.69202E-2	1.7211400000000002E-2	1.74897E-2	1.7770600000000001E-2	1.8062999999999999E-2	1.8354700000000002E-2	1.8636900000000001E-2	1.8930599999999999E-2	1.92201E-2	1.95011E-2	1.97938E-2	2.00853E-2	2.03669E-2	2.06578E-2	2.095E-2	2.12444E-2	2.1522099999999999E-2	2.1811299999999999E-2	2.2090499999999999E-2	2.23831E-2	2.2674099999999999E-2	2.2952899999999998E-2	2.32464E-2	2.3535500000000001E-2	2.38097E-2	2.4101500000000001E-2	2.4375899999999999E-2	2.46655E-2	2.4939200000000002E-2	2.5231199999999999E-2	2.5497700000000002E-2	2.57661E-2	2.60605E-2	2.63322E-2	2.6624499999999999E-2	2.6915999999999999E-2	2.7190099999999998E-2	2.7481200000000001E-2	2.775E-2	2.8041199999999999E-2	2.83009E-2	2.8572500000000001E-2	2.8864299999999999E-2	2.9129700000000001E-2	2.9421099999999999E-2	2.9687600000000001E-2	2.9954600000000001E-2	3.0242399999999999E-2	0.80332099999999995	1.3864099999999999	1.8668800000000001	2.3244400000000001	2.7082099999999998	3.0697999999999999	3.4123000000000001	3.7296200000000002	4.0126099999999996	4.2852800000000002	4.5496299999999996	4.8189799999999998	5.0639700000000003	5.2953099999999997	5.5240099999999996	5.7307100000000002	5.9507000000000003	6.1547999999999998	6.3462199999999998	6.5370100000000004	6.7190000000000003	6.9033800000000003	7.0758799999999997	7.2429699999999997	7.4105100000000004	7.5906700000000003	7.7260799999999996	7.9249900000000002	8.0713000000000008	8.2141199999999994	8.3749699999999994	8.5207300000000004	8.6517999999999997	8.7857500000000002	8.9165600000000005	9.0536200000000004	9.2206600000000005	9.3555600000000005	9.4776600000000002	9.6100600000000007	9.7514500000000002	9.9367300000000007	10.0596	10.1922	10.319800000000001	10.508699999999999	10.6915	10.8156	10.942399999999999	11.060499999999999	11.1846	11.3695	11.4809	11.610099999999999	11.7742	11.896599999999999	12.012600000000001	12.1119	12.2994	12.4001	12.5259	12.7043	12.879899999999999	12.9922	13.113300000000001	13.2685	13.370699999999999	13.5014	13.658200000000001	13.7621	13.874499999999999	14.025499999999999	14.139900000000001	14.248799999999999	14.3384	14.5093	14.6363	14.825799999999999	14.9293	15.042199999999999	15.1934	15.2872	15.409800000000001	15.585100000000001	15.6907	15.856999999999999	15.972300000000001	16.1355	16.227399999999999	16.439499999999999	16.629000000000001	16.7013	16.8855	16.980699999999999	17.078299999999999	17.245000000000001	17.343399999999999	17.520700000000001	17.612100000000002	17.8201	17.975999999999999	18.060500000000001	18.2439	18.3324	18.508199999999999	18.6662	18.7682	Fit	2.2092800000000001E-4	4.6090200000000001E-4	7.1164899999999996E-4	9.6344300000000003E-4	1.22507E-3	1.48895E-3	1.7543700000000001E-3	2.0227299999999999E-3	2.2956600000000001E-3	2.5693199999999999E-3	2.8438199999999999E-3	3.1166900000000001E-3	3.3938599999999998E-3	3.6725500000000001E-3	3.9514299999999997E-3	4.2325899999999996E-3	4.51323E-3	4.7959300000000003E-3	5.0808399999999997E-3	5.3647199999999999E-3	5.6503100000000004E-3	5.9344799999999998E-3	6.2209199999999996E-3	6.5079600000000001E-3	6.7951299999999999E-3	7.0800000000000004E-3	7.3709700000000001E-3	7.6543399999999999E-3	7.9441700000000004E-3	8.2339600000000002E-3	8.5209799999999992E-3	8.8106199999999999E-3	9.1014300000000006E-3	9.39276E-3	9.6841900000000005E-3	9.97521E-3	1.0260999999999999E-2	1.05521E-2	1.0845E-2	1.1136699999999999E-2	1.1427100000000001E-2	1.17102E-2	1.20024E-2	1.22936E-2	1.25848E-2	1.28675E-2	1.31506E-2	1.34419E-2	1.3733199999999999E-2	1.40251E-2	1.4315899999999999E-2	1.4598E-2	1.48909E-2	1.5181399999999999E-2	1.54669E-2	1.5759200000000001E-2	1.6052299999999999E-2	1.6346900000000001E-2	1.66263E-2	1.69202E-2	1.7211400000000002E-2	1.74897E-2	1.7770600000000001E-2	1.8062999999999999E-2	1.8354700000000002E-2	1.8636900000000001E-2	1.8930599999999999E-2	1.92201E-2	1.95011E-2	1.97938E-2	2.00853E-2	2.03669E-2	2.06578E-2	2.095E-2	2.12444E-2	2.1522099999999999E-2	2.1811299999999999E-2	2.2090499999999999E-2	2.23831E-2	2.2674099999999999E-2	2.2952899999999998E-2	2.32464E-2	2.3535500000000001E-2	2.38097E-2	2.4101500000000001E-2	2.4375899999999999E-2	2.46655E-2	2.4939200000000002E-2	2.5231199999999999E-2	2.5497700000000002E-2	2.57661E-2	2.60605E-2	2.63322E-2	2.6624499999999999E-2	2.6915999999999999E-2	2.7190099999999998E-2	2.7481200000000001E-2	2.775E-2	2.8041199999999999E-2	2.83009E-2	2.8572500000000001E-2	2.8864299999999999E-2	2.9129700000000001E-2	2.9421099999999999E-2	2.9687600000000001E-2	2.9954600000000001E-2	3.0242399999999999E-2	0.63875729999999997	1.4508160000000001	2.2792940000000002	3.0037910000000001	3.6488459999999998	4.2129190000000003	4.7149010000000002	5.1670629999999997	5.5823229999999997	5.9599599999999997	6.3054880000000004	6.621683	6.9205899999999998	7.1924359999999998	7.4464189999999997	7.6912890000000003	7.9086360000000004	8.1225459999999998	8.3178929999999998	8.507835	8.6799979999999994	8.8513040000000007	9.0034279999999995	9.1550890000000003	9.2975340000000006	9.4287120000000009	9.5626979999999993	9.6811720000000001	9.7969589999999993	9.9127310000000008	10.018230000000001	10.118209999999999	10.2186	10.31733	10.40396	10.490460000000001	10.57541	10.658799999999999	10.73362	10.80814	10.88233	10.954660000000001	11.01956	11.083360000000001	11.147169999999999	11.209110000000001	11.27088	11.3255	11.38012	11.43486	11.489380000000001	11.54228	11.592549999999999	11.63913	11.68491	11.731780000000001	11.778779999999999	11.82602	11.86755	11.90784	11.94777	11.98592	12.024430000000001	12.06452	12.104509999999999	12.139799999999999	12.174289999999999	12.20828	12.24128	12.275650000000001	12.30988	12.34295	12.37711	12.4068	12.43634	12.46421	12.493230000000001	12.521240000000001	12.550599999999999	12.579800000000001	12.60778	12.636010000000001	12.660869999999999	12.68445	12.709540000000001	12.733140000000001	12.758050000000001	12.78158	12.80669	12.829610000000001	12.852690000000001	12.876519999999999	12.896520000000001	12.91804	12.939489999999999	12.959669999999999	12.98109	13.00088	13.022309999999999	13.04142	13.06141	13.082890000000001	13.10163	13.120010000000001	13.13682	13.15366	13.17182	Measured N2	0.100022	0.12509799999999999	0.15010000000000001	0.175118	0.20017299999999999	0.28674300000000003	0.375805	0.46323500000000001	0.55076999999999998	0.63873000000000002	0.72983799999999999	0.80982699999999996	0.89933600000000002	0.93982900000000003	0.96942899999999999	0.98456699999999997	11.611800000000001	11.888500000000001	12.1594	12.430899999999999	12.6981	13.6965	14.9344	16.403199999999998	18.1553	20.2241	22.697099999999999	25.2316	28.703800000000001	30.823399999999999	33.027999999999999	34.820500000000003	Fit	0.100022	0.12509799999999999	0.15010000000000001	0.175118	0.20017299999999999	0.28674300000000003	0.375805	0.46323500000000001	0.55076999999999998	0.63873000000000002	0.72983799999999999	0.80982699999999996	0.89933600000000002	0.93982900000000003	0.96942899999999999	0.98456699999999997	20.263940000000002	20.375990000000002	20.472169999999998	20.558969999999999	20.63983	20.902519999999999	21.139500000000002	21.346689999999999	21.554469999999998	21.83333	22.169070000000001	22.549289999999999	26.2	29.687390000000001	32.582599999999999	33.747459999999997	Relative pressure


Amount adsorbed, cm3/g (STP)




TCB-HT

Measured CO2	7.23392E-5	1.91941E-4	3.3839100000000001E-4	4.9648300000000004E-4	6.5417000000000003E-4	8.3168399999999996E-4	1.01509E-3	1.2097099999999999E-3	1.41569E-3	1.62532E-3	1.83852E-3	2.0592900000000001E-3	2.28649E-3	2.51798E-3	2.7570699999999999E-3	2.9984899999999999E-3	3.2469500000000002E-3	3.5013800000000001E-3	3.7587599999999999E-3	4.0175499999999999E-3	4.27765E-3	4.5449699999999997E-3	4.8147399999999996E-3	5.0839600000000002E-3	5.3578799999999998E-3	5.6171900000000002E-3	5.8967500000000001E-3	6.17703E-3	6.4617700000000004E-3	6.7433700000000003E-3	7.0301599999999997E-3	7.3146000000000001E-3	7.6037600000000002E-3	7.8951400000000001E-3	8.1879599999999993E-3	8.4830500000000007E-3	8.7772800000000002E-3	9.0734600000000002E-3	9.3694199999999998E-3	9.6485100000000008E-3	9.9310800000000001E-3	1.02153E-2	1.0501E-2	1.07876E-2	1.10746E-2	1.13574E-2	1.1645300000000001E-2	1.19341E-2	1.22232E-2	1.25142E-2	1.2803500000000001E-2	1.30896E-2	1.3382099999999999E-2	1.36738E-2	1.39662E-2	1.42603E-2	1.45544E-2	1.4839E-2	1.51349E-2	1.54305E-2	1.5726400000000001E-2	1.6022499999999999E-2	1.63061E-2	1.6604600000000001E-2	1.69032E-2	1.7201000000000001E-2	1.7499600000000001E-2	1.7799800000000001E-2	1.80862E-2	1.8385200000000001E-2	1.8684699999999999E-2	1.89847E-2	1.94077E-2	1.9708E-2	2.0008000000000001E-2	2.0309299999999999E-2	2.0609599999999999E-2	2.1031999999999999E-2	2.1333700000000001E-2	2.1635999999999999E-2	2.2063800000000001E-2	2.2365900000000001E-2	2.2669100000000001E-2	2.29737E-2	2.3400500000000001E-2	2.3839099999999998E-2	2.4278899999999999E-2	2.4702200000000001E-2	2.5141299999999998E-2	2.55798E-2	2.60197E-2	2.64427E-2	2.68854E-2	2.7313500000000001E-2	2.7757199999999999E-2	2.81988E-2	2.86409E-2	2.9064E-2	2.95062E-2	2.9927599999999999E-2	3.0369799999999999E-2	2.7732999999999999	4.9537000000000004	6.8317199999999998	8.54542	10.197800000000001	11.6776	13.1159	14.455	15.6983	16.9069	18.074100000000001	19.177199999999999	20.2254	21.231000000000002	22.173100000000002	23.087299999999999	23.943000000000001	24.749199999999998	25.5379	26.305599999999998	27.063400000000001	27.774799999999999	28.463100000000001	29.156199999999998	29.795500000000001	30.498000000000001	31.1006	31.699300000000001	32.261000000000003	32.843299999999999	33.383000000000003	33.929600000000001	34.442599999999999	34.942599999999999	35.422600000000003	35.895099999999999	36.3645	36.810299999999998	37.247700000000002	37.7654	38.271599999999999	38.765000000000001	39.249600000000001	39.731499999999997	40.208799999999997	40.710799999999999	41.179299999999998	41.637799999999999	42.0901	42.532800000000002	42.981200000000001	43.450699999999998	43.878700000000002	44.304600000000001	44.727499999999999	45.133699999999997	45.540999999999997	45.979799999999997	46.376100000000001	46.775700000000001	47.170099999999998	47.5625	48.002800000000001	48.380200000000002	48.750300000000003	49.122300000000003	49.489100000000001	49.842599999999997	50.264200000000002	50.624400000000001	50.9773	51.327399999999997	51.858499999999999	52.198399999999999	52.539299999999997	52.870899999999999	53.212600000000002	53.747900000000001	54.080399999999997	54.405799999999999	54.897500000000001	55.225999999999999	55.545299999999997	55.8536	56.335799999999999	56.760800000000003	57.179900000000004	57.692999999999998	58.104399999999998	58.518500000000003	58.919800000000002	59.411200000000001	59.811799999999998	60.273800000000001	60.654400000000003	61.0456	61.428100000000001	61.909300000000002	62.290799999999997	62.773000000000003	63.150599999999997	Fit	7.23392E-5	1.91941E-4	3.3839100000000001E-4	4.9648300000000004E-4	6.5417000000000003E-4	8.3168399999999996E-4	1.01509E-3	1.2097099999999999E-3	1.41569E-3	1.62532E-3	1.83852E-3	2.0592900000000001E-3	2.28649E-3	2.51798E-3	2.7570699999999999E-3	2.9984899999999999E-3	3.2469500000000002E-3	3.5013800000000001E-3	3.7587599999999999E-3	4.0175499999999999E-3	4.27765E-3	4.5449699999999997E-3	4.8147399999999996E-3	5.0839600000000002E-3	5.3578799999999998E-3	5.6171900000000002E-3	5.8967500000000001E-3	6.17703E-3	6.4617700000000004E-3	6.7433700000000003E-3	7.0301599999999997E-3	7.3146000000000001E-3	7.6037600000000002E-3	7.8951400000000001E-3	8.1879599999999993E-3	8.4830500000000007E-3	8.7772800000000002E-3	9.0734600000000002E-3	9.3694199999999998E-3	9.6485100000000008E-3	9.9310800000000001E-3	1.02153E-2	1.0501E-2	1.07876E-2	1.10746E-2	1.13574E-2	1.1645300000000001E-2	1.19341E-2	1.22232E-2	1.25142E-2	1.2803500000000001E-2	1.30896E-2	1.3382099999999999E-2	1.36738E-2	1.39662E-2	1.42603E-2	1.45544E-2	1.4839E-2	1.51349E-2	1.54305E-2	1.5726400000000001E-2	1.6022499999999999E-2	1.63061E-2	1.6604600000000001E-2	1.69032E-2	1.7201000000000001E-2	1.7499600000000001E-2	1.7799800000000001E-2	1.80862E-2	1.8385200000000001E-2	1.8684699999999999E-2	1.89847E-2	1.94077E-2	1.9708E-2	2.0008000000000001E-2	2.0309299999999999E-2	2.0609599999999999E-2	2.1031999999999999E-2	2.1333700000000001E-2	2.1635999999999999E-2	2.2063800000000001E-2	2.2365900000000001E-2	2.2669100000000001E-2	2.29737E-2	2.3400500000000001E-2	2.3839099999999998E-2	2.4278899999999999E-2	2.4702200000000001E-2	2.5141299999999998E-2	2.55798E-2	2.60197E-2	2.64427E-2	2.68854E-2	2.7313500000000001E-2	2.7757199999999999E-2	2.81988E-2	2.86409E-2	2.9064E-2	2.95062E-2	2.9927599999999999E-2	3.0369799999999999E-2	0.63951729999999996	1.792532	3.353351	5.1229740000000001	6.8297249999999998	8.5989439999999995	10.25098	11.84404	13.36364	14.7841	16.117640000000002	17.39669	18.620740000000001	19.787389999999998	20.921230000000001	22.001370000000001	23.031590000000001	24.03951	25.0169	25.925409999999999	26.819140000000001	27.674009999999999	28.5166	29.30575	30.096050000000002	30.79054	31.539259999999999	32.236629999999998	32.933869999999999	33.605240000000002	34.246200000000002	34.881909999999998	35.499389999999998	36.093330000000002	36.69021	37.268169999999998	37.814959999999999	38.365380000000002	38.912939999999999	39.385689999999997	39.864339999999999	40.345779999999998	40.826160000000002	41.268999999999998	41.71246	42.149430000000002	42.594279999999998	43.013350000000003	43.420740000000002	43.830800000000004	44.23847	44.641629999999999	45.023760000000003	45.398260000000001	45.773650000000004	46.151220000000002	46.528790000000001	46.880490000000002	47.226500000000001	47.57217	47.918190000000003	48.26444	48.596069999999997	48.932580000000002	49.250230000000002	49.567019999999999	49.884659999999997	50.204009999999997	50.508670000000002	50.826740000000001	51.123669999999997	51.413319999999999	51.821719999999999	52.111660000000001	52.401310000000002	52.692219999999999	52.98216	53.35528	53.61683	53.878909999999998	54.249789999999997	54.511690000000002	54.774549999999998	55.038620000000002	55.38561	55.723610000000001	56.062539999999998	56.388750000000002	56.727130000000002	57.065060000000003	57.396630000000002	57.682789999999997	57.98227	58.271880000000003	58.572049999999997	58.87079	59.169870000000003	59.455199999999998	59.716270000000002	59.965060000000001	60.226129999999998	Measured N2	3.6010100000000003E-2	6.2593099999999999E-2	7.6246400000000006E-2	0.10001	0.12510399999999999	0.150311	0.175786	0.20125899999999999	0.28009699999999998	0.37267800000000001	0.46044099999999999	0.54774400000000001	0.63545799999999997	0.72666299999999995	0.80680799999999997	0.89448899999999998	0.937087	0.96640300000000001	0.98279399999999995	79.247200000000007	83.401799999999994	85.133700000000005	87.581400000000002	89.915800000000004	92.161299999999997	94.306600000000003	96.421199999999999	102.68	110.315	118.10899999999999	126.754	136.602	147.899	158.637	172.04599999999999	180.392	188.66300000000001	195.80500000000001	Fit	3.6010100000000003E-2	6.2593099999999999E-2	7.6246400000000006E-2	0.10001	0.12510399999999999	0.150311	0.175786	0.20125899999999999	0.28009699999999998	0.37267800000000001	0.46044099999999999	0.54774400000000001	0.63545799999999997	0.72666299999999995	0.80680799999999997	0.89448899999999998	0.937087	0.96640300000000001	0.98279399999999995	83.219390000000004	85.58	86.722530000000006	88.607190000000003	90.282660000000007	92.047160000000005	93.879769999999994	95.839669999999998	102.2094	110.217	117.9636	126.5723	136.38069999999999	147.87090000000001	158.4658	172.06649999999999	180.2287	188.9693	195.53450000000001	Relative pressure


Amount adsorbed, cm3/g (STP)




TCB-800TU-HT
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Amount adsorbed, cm3/g (STP)




PSD
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Differential Pore Volume, (cm3/g)/Å




PSD

TB-TU700	3.6	3.6899109999999999	3.7820670000000001	3.8765239999999999	3.973341	4.0725759999999998	4.1742889999999999	4.278543	4.3853999999999997	4.4949260000000004	4.6071869999999997	4.7222530000000003	4.840192	4.9610760000000003	5.0849799999999998	5.2119780000000002	5.3421479999999999	5.4755690000000001	5.6123219999999998	5.752491	5.8961600000000001	6.0434169999999998	6.1943530000000004	6.3490580000000003	6.5076260000000001	6.6701550000000003	6.8367430000000002	7.0074920000000001	7.1825049999999999	7.3618889999999997	7.5457539999999996	7.73421	7.9273730000000002	8.1253609999999998	8.3282930000000004	8.5362930000000006	8.7494879999999995	8.9680079999999993	9.1919850000000007	9.421557	9.6568609999999993	9.8980429999999995	10.145250000000001	10.398630000000001	10.658329999999999	10.924530000000001	11.197369999999999	11.477029999999999	11.763669999999999	12.05747	12.358599999999999	12.667260000000001	12.98363	13.3079	13.64026	13.980930000000001	14.330109999999999	14.688000000000001	15.05484	15.43083	15.81622	16.21123	16.616109999999999	17.031099999999999	17.45646	17.892430000000001	18.339300000000001	18.797329999999999	19.26679	19.747990000000001	20.24119	20.74672	21.264869999999998	21.795970000000001	22.340319999999998	22.89828	23.47017	24.056339999999999	24.657150000000001	25.272960000000001	25.904160000000001	26.551120000000001	27.21424	27.893920000000001	28.59057	29.30463	30.03651	30.78668	31.555579999999999	32.343690000000002	33.151479999999999	33.979439999999997	34.82808	35.697920000000003	36.589480000000002	37.503309999999999	38.439959999999999	39.4	40.38402	41.392620000000001	42.426409999999997	43.48601	44.57208	45.685279999999999	46.826270000000001	47.99577	49.194470000000003	50.423110000000001	51.682429999999997	52.973210000000002	54.296219999999998	55.652279999999998	57.042200000000001	58.466839999999998	59.927059999999997	61.423749999999998	62.957819999999998	64.530199999999994	66.141850000000005	67.793750000000003	69.486909999999995	71.222359999999995	73.001149999999996	74.824359999999999	76.693110000000004	78.608530000000002	80.571789999999993	82.584090000000003	84.646640000000005	86.7607	88.92756	91.148539999999997	93.424989999999994	95.758290000000002	98.149870000000007	100.60120000000001	103.11369999999999	105.68899999999999	108.32859999999999	111.0341	113.80719999999999	116.64960000000001	119.5629	122.54900000000001	125.6097	128.74680000000001	131.9623	135.25800000000001	138.6361	142.0986	145.64750000000001	149.2851	153.01349999999999	156.83510000000001	160.75200000000001	164.76679999999999	168.8819	173.09979999999999	177.423	181.85409999999999	186.39599999999999	191.05119999999999	195.8228	200.71350000000001	205.72630000000001	210.86439999999999	216.13069999999999	221.52860000000001	227.06129999999999	232.73220000000001	238.54480000000001	244.5025	250.60890000000001	256.86790000000002	263.28320000000002	269.85879999999997	276.59859999999998	283.50659999999999	290.58730000000003	297.84469999999999	305.28339999999997	312.90789999999998	320.72289999999998	328.733	336.94310000000002	345.35829999999999	353.9837	362.8245	371.8861	381.17399999999998	390.69389999999999	400.45150000000001	410.4529	420.70400000000001	431.21109999999999	441.98070000000001	453.01920000000001	464.33350000000002	475.93029999999999	487.81670000000003	0	1.6207609999999999E-4	1.321001E-3	4.140192E-3	8.5820589999999995E-3	1.416922E-2	1.9559259999999998E-2	2.4607670000000002E-2	2.9186500000000001E-2	3.3140919999999997E-2	3.64972E-2	3.9059280000000002E-2	4.0866640000000003E-2	4.1969480000000003E-2	4.2406699999999999E-2	4.2246680000000002E-2	4.1554210000000001E-2	4.0395300000000002E-2	3.8833810000000003E-2	3.6931289999999999E-2	3.474066E-2	3.2311159999999998E-2	2.9683939999999999E-2	2.691752E-2	2.404007E-2	2.110911E-2	1.8184180000000001E-2	1.5333980000000001E-2	1.260872E-2	1.0107720000000001E-2	7.8657039999999994E-3	5.9048E-3	4.2483699999999996E-3	2.892145E-3	1.830131E-3	1.055765E-3	5.2465870000000003E-4	2.2773760000000001E-4	8.4274020000000001E-5	2.4672640000000001E-5	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	1.097399E-7	7.287603E-7	4.8831709999999999E-6	1.389364E-5	3.5149640000000003E-5	7.4605189999999994E-5	1.3296090000000001E-4	2.068386E-4	2.9336500000000002E-4	3.8940729999999997E-4	4.9204160000000002E-4	5.9837629999999996E-4	7.0568400000000004E-4	8.1127849999999997E-4	9.1298180000000005E-4	1.0089389999999999E-3	1.097436E-3	1.178017E-3	1.249429E-3	1.3114940000000001E-3	1.364119E-3	1.407234E-3	1.440925E-3	1.465336E-3	1.4808740000000001E-3	1.488252E-3	1.4880189999999999E-3	1.480999E-3	1.468008E-3	1.4500730000000001E-3	1.428215E-3	1.4035860000000001E-3	1.3769240000000001E-3	1.3488529999999999E-3	1.3198909999999999E-3	1.290107E-3	1.2597960000000001E-3	1.228961E-3	1.197596E-3	1.1656769999999999E-3	1.1332270000000001E-3	1.1001610000000001E-3	1.0664940000000001E-3	1.0323120000000001E-3	9.9764350000000005E-4	9.6268899999999997E-4	9.2763380000000003E-4	8.9267100000000005E-4	8.5797219999999999E-4	8.2371639999999997E-4	7.9002330000000004E-4	7.5700479999999998E-4	7.2475149999999999E-4	6.9344519999999996E-4	6.6314140000000004E-4	6.3402830000000002E-4	6.0627439999999999E-4	5.8007139999999996E-4	5.5543010000000002E-4	5.3258159999999995E-4	5.1150000000000002E-4	4.9213100000000004E-4	4.744328E-4	4.582888E-4	4.435838E-4	4.3018160000000001E-4	4.1791339999999998E-4	4.0664139999999999E-4	3.9619669999999999E-4	3.8642240000000001E-4	3.7716719999999999E-4	3.6828179999999998E-4	3.5963189999999999E-4	3.5109220000000002E-4	3.425503E-4	3.3390420000000001E-4	3.2507880000000002E-4	3.159929E-4	3.0658919999999997E-4	2.968216E-4	2.8664959999999997E-4	2.7605289999999997E-4	2.6501729999999998E-4	2.5354300000000001E-4	2.41654E-4	2.2936310000000001E-4	2.167157E-4	2.037579E-4	1.905434E-4	1.7716410000000001E-4	1.6367509999999999E-4	1.501757E-4	1.3676230000000001E-4	1.2352660000000001E-4	1.1061339999999999E-4	9.8106189999999999E-5	8.6140199999999999E-5	7.4829209999999999E-5	6.4284599999999998E-5	5.4529759999999998E-5	4.5652070000000001E-5	3.7661689999999998E-5	3.0554060000000003E-5	2.4329390000000001E-5	1.8955060000000001E-5	1.4396779999999999E-5	1.0610420000000001E-5	7.527509E-6	5.0996469999999997E-6	3.249355E-6	1.9031080000000001E-6	9.9708319999999999E-7	4.2658419999999999E-7	1.4423809999999999E-7	3.595797E-8	1.129987E-8	0	0	0	0	0	0	0	0	0	0	0	0	0	0	TCB-TU700	3.6	3.6899109999999999	3.7820670000000001	3.8765239999999999	3.973341	4.0725759999999998	4.1742889999999999	4.278543	4.3853999999999997	4.4949260000000004	4.6071869999999997	4.7222530000000003	4.840192	4.9610760000000003	5.0849799999999998	5.2119780000000002	5.3421479999999999	5.4755690000000001	5.6123219999999998	5.752491	5.8961600000000001	6.0434169999999998	6.1943530000000004	6.3490580000000003	6.5076260000000001	6.6701550000000003	6.8367430000000002	7.0074920000000001	7.1825049999999999	7.3618889999999997	7.5457539999999996	7.73421	7.9273730000000002	8.1253609999999998	8.3282930000000004	8.5362930000000006	8.7494879999999995	8.9680079999999993	9.1919850000000007	9.421557	9.6568609999999993	9.8980429999999995	10.145250000000001	10.398630000000001	10.658329999999999	10.924530000000001	11.197369999999999	11.477029999999999	11.763669999999999	12.05747	12.358599999999999	12.667260000000001	12.98363	13.3079	13.64026	13.980930000000001	14.330109999999999	14.688000000000001	15.05484	15.43083	15.81622	16.21123	16.616109999999999	17.031099999999999	17.45646	17.892430000000001	18.339300000000001	18.797329999999999	19.26679	19.747990000000001	20.24119	20.74672	21.264869999999998	21.795970000000001	22.340319999999998	22.89828	23.47017	24.056339999999999	24.657150000000001	25.272960000000001	25.904160000000001	26.551120000000001	27.21424	27.893920000000001	28.59057	29.30463	30.03651	30.78668	31.555579999999999	32.343690000000002	33.151479999999999	33.979439999999997	34.82808	35.697920000000003	36.589480000000002	37.503309999999999	38.439959999999999	39.4	40.38402	41.392620000000001	42.426409999999997	43.48601	44.57208	45.685279999999999	46.826270000000001	47.99577	49.194470000000003	50.423110000000001	51.682429999999997	52.973210000000002	54.296219999999998	55.652279999999998	57.042200000000001	58.466839999999998	59.927059999999997	61.423749999999998	62.957819999999998	64.530199999999994	66.141850000000005	67.793750000000003	69.486909999999995	71.222359999999995	73.001149999999996	74.824359999999999	76.693110000000004	78.608530000000002	80.571789999999993	82.584090000000003	84.646640000000005	86.7607	88.92756	91.148539999999997	93.424989999999994	95.758290000000002	98.149870000000007	100.60120000000001	103.11369999999999	105.68899999999999	108.32859999999999	111.0341	113.80719999999999	116.64960000000001	119.5629	122.54900000000001	125.6097	128.74680000000001	131.9623	135.25800000000001	138.6361	142.0986	145.64750000000001	149.2851	153.01349999999999	156.83510000000001	160.75200000000001	164.76679999999999	168.8819	173.09979999999999	177.423	181.85409999999999	186.39599999999999	191.05119999999999	195.8228	200.71350000000001	205.72630000000001	210.86439999999999	216.13069999999999	221.52860000000001	227.06129999999999	232.73220000000001	238.54480000000001	244.5025	250.60890000000001	256.86790000000002	263.28320000000002	269.85879999999997	276.59859999999998	283.50659999999999	290.58730000000003	297.84469999999999	305.28339999999997	312.90789999999998	320.72289999999998	328.733	336.94310000000002	345.35829999999999	353.9837	362.8245	371.8861	381.17399999999998	390.69389999999999	400.45150000000001	410.4529	420.70400000000001	431.21109999999999	441.98070000000001	453.01920000000001	464.33350000000002	475.93029999999999	487.81670000000003	0	2.0795310000000001E-4	1.697811E-3	5.3108060000000004E-3	1.0935459999999999E-2	1.7963819999999998E-2	2.451745E-2	3.0458410000000002E-2	3.567335E-2	4.0009780000000002E-2	4.3572180000000002E-2	4.6167420000000001E-2	4.7907850000000002E-2	4.8900779999999998E-2	4.9243929999999998E-2	4.9035380000000003E-2	4.8363059999999999E-2	4.7297260000000001E-2	4.5863019999999997E-2	4.4112369999999998E-2	4.2042700000000002E-2	3.9652470000000002E-2	3.6922950000000003E-2	3.3903580000000003E-2	3.0552269999999999E-2	2.6940660000000002E-2	2.3160449999999999E-2	1.9339519999999999E-2	1.558707E-2	1.214846E-2	9.0957269999999996E-3	6.4757759999999999E-3	4.3381460000000002E-3	2.6771009999999999E-3	1.4803209999999999E-3	7.0187039999999997E-4	2.4623849999999998E-4	5.0286739999999997E-5	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	8.8960350000000003E-9	1.7599760000000001E-6	1.051751E-5	3.1525990000000002E-5	7.0937929999999999E-5	1.292183E-4	2.122576E-4	3.14235E-4	4.2981010000000001E-4	5.5416809999999999E-4	6.827014E-4	8.1151240000000005E-4	9.3657579999999999E-4	1.054555E-3	1.1624210000000001E-3	1.2599930000000001E-3	1.3453479999999999E-3	1.418756E-3	1.48039E-3	1.5304769999999999E-3	1.568928E-3	1.5957650000000001E-3	1.6114879999999999E-3	1.616967E-3	1.612952E-3	1.600326E-3	1.5799919999999999E-3	1.5532370000000001E-3	1.5214569999999999E-3	1.486196E-3	1.4484719999999999E-3	1.4091799999999999E-3	1.3690639999999999E-3	1.3286319999999999E-3	1.288343E-3	1.248648E-3	1.209842E-3	1.1722239999999999E-3	1.1355130000000001E-3	1.099689E-3	1.06448E-3	1.029716E-3	9.9518780000000008E-4	9.6090050000000005E-4	9.2686220000000004E-4	8.9309429999999998E-4	8.5958430000000004E-4	8.2636319999999995E-4	7.9338070000000002E-4	7.6060690000000002E-4	7.2798700000000004E-4	6.958321E-4	6.6405040000000004E-4	6.3304289999999998E-4	6.0318510000000004E-4	5.7492649999999997E-4	5.4832350000000004E-4	5.2397689999999998E-4	5.0185669999999998E-4	4.8187479999999998E-4	4.6397140000000001E-4	4.4793090000000001E-4	4.3354450000000002E-4	4.2056640000000001E-4	4.0871419999999998E-4	3.9774439999999998E-4	3.8739850000000001E-4	3.7744280000000002E-4	3.6765989999999998E-4	3.5792149999999998E-4	3.4804029999999998E-4	3.3794819999999998E-4	3.2759869999999998E-4	3.1698380000000001E-4	3.0611450000000003E-4	2.950645E-4	2.838327E-4	2.7241260000000002E-4	2.608E-4	2.4897029999999999E-4	2.369026E-4	2.2457900000000001E-4	2.119968E-4	1.9914619999999999E-4	1.8604560000000001E-4	1.727171E-4	1.5919250000000001E-4	1.4556089999999999E-4	1.318584E-4	1.181934E-4	1.046733E-4	9.1392559999999994E-5	7.8565560000000003E-5	6.6267140000000004E-5	5.4713119999999998E-5	4.4087759999999999E-5	3.4597149999999998E-5	2.6215379999999998E-5	1.9161430000000001E-5	1.338783E-5	8.8178959999999998E-6	5.3968179999999998E-6	2.9915550000000001E-6	1.4670079999999999E-6	6.0755640000000004E-7	2.15066E-7	4.4856690000000003E-8	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	TB-TU800	3.6	3.6899109999999999	3.7820670000000001	3.8765239999999999	3.973341	4.0725759999999998	4.1742889999999999	4.278543	4.3853999999999997	4.4949260000000004	4.6071869999999997	4.7222530000000003	4.840192	4.9610760000000003	5.0849799999999998	5.2119780000000002	5.3421479999999999	5.4755690000000001	5.6123219999999998	5.752491	5.8961600000000001	6.0434169999999998	6.1943530000000004	6.3490580000000003	6.5076260000000001	6.6701550000000003	6.8367430000000002	7.0074920000000001	7.1825049999999999	7.3618889999999997	7.5457539999999996	7.73421	7.9273730000000002	8.1253609999999998	8.3282930000000004	8.5362930000000006	8.7494879999999995	8.9680079999999993	9.1919850000000007	9.421557	9.6568609999999993	9.8980429999999995	10.145250000000001	10.398630000000001	10.658329999999999	10.924530000000001	11.197369999999999	11.477029999999999	11.763669999999999	12.05747	12.358599999999999	12.667260000000001	12.98363	13.3079	13.64026	13.980930000000001	14.330109999999999	14.688000000000001	15.05484	15.43083	15.81622	16.21123	16.616109999999999	17.031099999999999	17.45646	17.892430000000001	18.339300000000001	18.797329999999999	19.26679	19.747990000000001	20.24119	20.74672	21.264869999999998	21.795970000000001	22.340319999999998	22.89828	23.47017	24.056339999999999	24.657150000000001	25.272960000000001	25.904160000000001	26.551120000000001	27.21424	27.893920000000001	28.59057	29.30463	30.03651	30.78668	31.555579999999999	32.343690000000002	33.151479999999999	33.979439999999997	34.82808	35.697920000000003	36.589480000000002	37.503309999999999	38.439959999999999	39.4	40.38402	41.392620000000001	42.426409999999997	43.48601	44.57208	45.685279999999999	46.826270000000001	47.99577	49.194470000000003	50.423110000000001	51.682429999999997	52.973210000000002	54.296219999999998	55.652279999999998	57.042200000000001	58.466839999999998	59.927059999999997	61.423749999999998	62.957819999999998	64.530199999999994	66.141850000000005	67.793750000000003	69.486909999999995	71.222359999999995	73.001149999999996	74.824359999999999	76.693110000000004	78.608530000000002	80.571789999999993	82.584090000000003	84.646640000000005	86.7607	88.92756	91.148539999999997	93.424989999999994	95.758290000000002	98.149870000000007	100.60120000000001	103.11369999999999	105.68899999999999	108.32859999999999	111.0341	113.80719999999999	116.64960000000001	119.5629	122.54900000000001	125.6097	128.74680000000001	131.9623	135.25800000000001	138.6361	142.0986	145.64750000000001	149.2851	153.01349999999999	156.83510000000001	160.75200000000001	164.76679999999999	168.8819	173.09979999999999	177.423	181.85409999999999	186.39599999999999	191.05119999999999	195.8228	200.71350000000001	205.72630000000001	210.86439999999999	216.13069999999999	221.52860000000001	227.06129999999999	232.73220000000001	238.54480000000001	244.5025	250.60890000000001	256.86790000000002	263.28320000000002	269.85879999999997	276.59859999999998	283.50659999999999	290.58730000000003	297.84469999999999	305.28339999999997	312.90789999999998	320.72289999999998	328.733	336.94310000000002	345.35829999999999	353.9837	362.8245	371.8861	381.17399999999998	390.69389999999999	400.45150000000001	410.4529	420.70400000000001	431.21109999999999	441.98070000000001	453.01920000000001	464.33350000000002	475.93029999999999	487.81670000000003	0	0	0	0	0	0	0	0	0	0	0	1.366708E-5	1.8440810000000001E-4	6.5331320000000005E-4	1.5842269999999999E-3	2.9997159999999999E-3	4.8982460000000002E-3	7.1562279999999997E-3	9.5274720000000004E-3	1.181316E-2	1.378645E-2	1.5251000000000001E-2	1.6009010000000001E-2	1.6105709999999999E-2	1.534774E-2	1.3860000000000001E-2	1.180428E-2	9.4097109999999994E-3	6.8664080000000001E-3	4.6183709999999996E-3	2.803453E-3	1.4624379999999999E-3	6.7104130000000004E-4	2.576659E-4	7.0599799999999994E-5	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	2.5269020000000001E-7	4.220406E-6	1.414423E-5	3.43216E-5	6.291864E-5	9.8225679999999996E-5	1.3871200000000001E-4	1.82366E-4	2.2797170000000001E-4	2.7343760000000001E-4	3.1692040000000002E-4	3.5653829999999999E-4	3.9208340000000002E-4	4.2170430000000001E-4	4.4574779999999997E-4	4.644537E-4	4.7800810000000002E-4	4.8643619999999999E-4	4.8956080000000005E-4	4.8735579999999997E-4	4.8019300000000002E-4	4.6814490000000002E-4	4.5227290000000002E-4	4.3355329999999998E-4	4.12958E-4	3.9109149999999999E-4	3.6883130000000001E-4	3.4638259999999999E-4	3.2393999999999999E-4	3.0158799999999999E-4	2.7987619999999999E-4	2.5872660000000002E-4	2.3881449999999999E-4	2.207589E-4	2.0533920000000001E-4	1.924475E-4	1.8315439999999999E-4	1.7721039999999999E-4	1.7427E-4	1.7406290000000001E-4	1.760252E-4	1.7962579999999999E-4	1.8428530000000001E-4	1.894094E-4	1.944572E-4	1.98937E-4	2.0241810000000001E-4	2.0452219999999999E-4	2.05164E-4	2.040418E-4	2.012107E-4	1.9678090000000001E-4	1.9095940000000001E-4	1.8407690000000001E-4	1.765665E-4	1.6868729999999999E-4	1.6063239999999999E-4	1.525834E-4	1.445661E-4	1.36599E-4	1.286631E-4	1.2071299999999999E-4	1.127131E-4	1.046164E-4	9.638374E-5	8.7984390000000003E-5	7.9457239999999998E-5	7.0779779999999995E-5	6.2028369999999995E-5	5.3285339999999999E-5	4.4617350000000001E-5	3.6294739999999999E-5	2.836185E-5	2.11117E-5	1.4783879999999999E-5	9.7170020000000008E-6	5.6098610000000003E-6	2.9110000000000002E-6	1.2846689999999999E-6	4.3413760000000002E-7	8.0980089999999997E-8	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	TCB-TU800	3.6	3.6899109999999999	3.7820670000000001	3.8765239999999999	3.973341	4.0725759999999998	4.1742889999999999	4.278543	4.3853999999999997	4.4949260000000004	4.6071869999999997	4.7222530000000003	4.840192	4.9610760000000003	5.0849799999999998	5.2119780000000002	5.3421479999999999	5.4755690000000001	5.6123219999999998	5.752491	5.8961600000000001	6.0434169999999998	6.1943530000000004	6.3490580000000003	6.5076260000000001	6.6701550000000003	6.8367430000000002	7.0074920000000001	7.1825049999999999	7.3618889999999997	7.5457539999999996	7.73421	7.9273730000000002	8.1253609999999998	8.3282930000000004	8.5362930000000006	8.7494879999999995	8.9680079999999993	9.1919850000000007	9.421557	9.6568609999999993	9.8980429999999995	10.145250000000001	10.398630000000001	10.658329999999999	10.924530000000001	11.197369999999999	11.477029999999999	11.763669999999999	12.05747	12.358599999999999	12.667260000000001	12.98363	13.3079	13.64026	13.980930000000001	14.330109999999999	14.688000000000001	15.05484	15.43083	15.81622	16.21123	16.616109999999999	17.031099999999999	17.45646	17.892430000000001	18.339300000000001	18.797329999999999	19.26679	19.747990000000001	20.24119	20.74672	21.264869999999998	21.795970000000001	22.340319999999998	22.89828	23.47017	24.056339999999999	24.657150000000001	25.272960000000001	25.904160000000001	26.551120000000001	27.21424	27.893920000000001	28.59057	29.30463	30.03651	30.78668	31.555579999999999	32.343690000000002	33.151479999999999	33.979439999999997	34.82808	35.697920000000003	36.589480000000002	37.503309999999999	38.439959999999999	39.4	40.38402	41.392620000000001	42.426409999999997	43.48601	44.57208	45.685279999999999	46.826270000000001	47.99577	49.194470000000003	50.423110000000001	51.682429999999997	52.973210000000002	54.296219999999998	55.652279999999998	57.042200000000001	58.466839999999998	59.927059999999997	61.423749999999998	62.957819999999998	64.530199999999994	66.141850000000005	67.793750000000003	69.486909999999995	71.222359999999995	73.001149999999996	74.824359999999999	76.693110000000004	78.608530000000002	80.571789999999993	82.584090000000003	84.646640000000005	86.7607	88.92756	91.148539999999997	93.424989999999994	95.758290000000002	98.149870000000007	100.60120000000001	103.11369999999999	105.68899999999999	108.32859999999999	111.0341	113.80719999999999	116.64960000000001	119.5629	122.54900000000001	125.6097	128.74680000000001	131.9623	135.25800000000001	138.6361	142.0986	145.64750000000001	149.2851	153.01349999999999	156.83510000000001	160.75200000000001	164.76679999999999	168.8819	173.09979999999999	177.423	181.85409999999999	186.39599999999999	191.05119999999999	195.8228	200.71350000000001	205.72630000000001	210.86439999999999	216.13069999999999	221.52860000000001	227.06129999999999	232.73220000000001	238.54480000000001	244.5025	250.60890000000001	256.86790000000002	263.28320000000002	269.85879999999997	276.59859999999998	283.50659999999999	290.58730000000003	297.84469999999999	305.28339999999997	312.90789999999998	320.72289999999998	328.733	336.94310000000002	345.35829999999999	353.9837	362.8245	371.8861	381.17399999999998	390.69389999999999	400.45150000000001	410.4529	420.70400000000001	431.21109999999999	441.98070000000001	453.01920000000001	464.33350000000002	475.93029999999999	487.81670000000003	0	0	0	0	0	0	0	0	0	0	0	3.5620430000000001E-7	0	1.724473E-5	1.014959E-4	4.5218029999999999E-4	1.2366549999999999E-3	2.4403839999999999E-3	3.8766809999999999E-3	5.400508E-3	6.8337659999999998E-3	8.0189170000000004E-3	8.7906619999999994E-3	9.1520390000000007E-3	8.9325900000000007E-3	8.1988359999999993E-3	7.0480789999999996E-3	5.6276609999999999E-3	4.0725809999999996E-3	2.6922970000000002E-3	1.5860690000000001E-3	7.8284419999999995E-4	3.3714839999999998E-4	1.238872E-4	3.3944769999999999E-5	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	2.0278860000000001E-8	5.0308790000000005E-7	4.598917E-6	1.296827E-5	2.900455E-5	5.4377640000000002E-5	9.1012489999999996E-5	1.3643250000000001E-4	1.883167E-4	2.4422650000000001E-4	3.0167829999999999E-4	3.5845700000000001E-4	4.1242379999999998E-4	4.617685E-4	5.0546290000000002E-4	5.4327749999999995E-4	5.7500100000000001E-4	6.0048770000000005E-4	6.1965459999999996E-4	6.3227659999999996E-4	6.3918690000000001E-4	6.3996880000000004E-4	6.3570100000000002E-4	6.2727349999999998E-4	6.155364E-4	6.0076379999999998E-4	5.8342870000000001E-4	5.637134E-4	5.4197339999999998E-4	5.1840359999999995E-4	4.9365759999999998E-4	4.6832779999999999E-4	4.4297070000000002E-4	4.178788E-4	3.9352730000000001E-4	3.6996210000000003E-4	3.4722760000000002E-4	3.2529910000000001E-4	3.0447379999999998E-4	2.8462680000000001E-4	2.6615090000000003E-4	2.4940580000000002E-4	2.3486340000000001E-4	2.224029E-4	2.1270060000000001E-4	2.0554699999999999E-4	2.0067119999999999E-4	1.978556E-4	1.9668830000000001E-4	1.967816E-4	1.9771839999999999E-4	1.990742E-4	2.0046199999999999E-4	2.015311E-4	2.0197349999999999E-4	2.0151819999999999E-4	2.0009469999999999E-4	1.9748669999999999E-4	1.9372120000000001E-4	1.8886350000000001E-4	1.830445E-4	1.7648300000000001E-4	1.6946370000000001E-4	1.621587E-4	1.5469680000000001E-4	1.4719930000000001E-4	1.396852E-4	1.3216890000000001E-4	1.2464069999999999E-4	1.17075E-4	1.0945179999999999E-4	1.017455E-4	9.3936020000000005E-5	8.6008849999999999E-5	7.7998920000000004E-5	6.9896860000000002E-5	6.1763209999999999E-5	5.3661749999999998E-5	4.5642729999999998E-5	3.7902150000000001E-5	3.047051E-5	2.355833E-5	1.7347449999999999E-5	1.2057880000000001E-5	7.625457E-6	4.3163870000000001E-6	2.0622540000000001E-6	6.969128E-7	1.2999580000000001E-7	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	TB	3.6	3.69	3.78	3.88	3.97	4.07	4.17	4.28	4.3899999999999997	4.49	4.6100000000000003	4.72	4.84	4.96	5.08	5.21	5.34	5.48	5.61	5.75	5.9	6.04	6.19	6.35	6.51	6.67	6.84	7.01	7.18	7.36	7.55	7.73	7.93	8.1300000000000008	8.33	8.5399999999999991	8.75	8.9700000000000006	9.19	9.42	9.66	9.9	10.1	10.4	10.7	10.9	11.2	11.5	11.8	12.1	12.4	12.7	13	13.3	13.6	14	14.3	14.7	15.1	15.4	15.8	16.2	16.600000000000001	17	17.5	17.899999999999999	18.3	18.8	19.3	19.7	20.2	20.7	21.3	21.8	22.3	22.9	23.5	24.1	24.7	25.3	25.9	26.6	27.2	27.9	28.6	29.3	30	30.8	31.6	32.299999999999997	33.200000000000003	34	34.799999999999997	35.700000000000003	36.6	37.5	38.4	39.4	40.4	41.4	42.4	43.5	44.6	45.7	46.8	48	49.2	50.4	51.7	53	54.3	55.7	57	58.5	59.9	61.4	63	64.5	66.099999999999994	67.8	69.5	71.2	73	74.8	76.7	78.599999999999994	80.599999999999994	82.6	84.6	86.8	88.9	91.1	93.4	95.8	98.1	101	103	106	108	111	114	117	120	123	126	129	132	135	139	142	146	149	153	157	161	165	169	173	177	182	186	191	196	201	206	211	216	222	227	233	239	245	251	257	263	270	277	284	291	298	305	313	321	329	337	345	354	363	372	381	391	400	410	421	431	442	453	464	476	488	0	2.6600000000000001E-4	2.1700000000000001E-3	6.79E-3	1.4E-2	2.29E-2	3.1300000000000001E-2	3.8800000000000001E-2	4.5400000000000003E-2	5.0799999999999998E-2	5.5100000000000003E-2	5.8000000000000003E-2	5.96E-2	6.0100000000000001E-2	5.9400000000000001E-2	5.79E-2	5.5599999999999997E-2	5.2699999999999997E-2	4.9299999999999997E-2	4.5600000000000002E-2	4.1599999999999998E-2	3.7600000000000001E-2	3.3599999999999998E-2	2.9600000000000001E-2	2.58E-2	2.2200000000000001E-2	1.8800000000000001E-2	1.5699999999999999E-2	1.2999999999999999E-2	1.0500000000000001E-2	8.4600000000000005E-3	6.7499999999999999E-3	5.4000000000000003E-3	4.4200000000000003E-3	3.81E-3	3.5300000000000002E-3	3.5599999999999998E-3	3.8600000000000001E-3	4.3600000000000002E-3	5.0000000000000001E-3	5.7000000000000002E-3	6.43E-3	7.1000000000000004E-3	7.6699999999999997E-3	8.1200000000000005E-3	8.4200000000000004E-3	8.5699999999999995E-3	8.5599999999999999E-3	8.4100000000000008E-3	8.1300000000000001E-3	7.7499999999999999E-3	7.2899999999999996E-3	6.79E-3	6.2599999999999999E-3	5.7099999999999998E-3	5.1799999999999997E-3	4.6699999999999997E-3	4.1900000000000001E-3	3.7499999999999999E-3	3.3500000000000001E-3	3.0000000000000001E-3	2.7000000000000001E-3	2.4399999999999999E-3	2.2300000000000002E-3	2.0699999999999998E-3	1.9400000000000001E-3	1.8500000000000001E-3	1.8E-3	1.7700000000000001E-3	1.7600000000000001E-3	1.7799999999999999E-3	1.81E-3	1.8500000000000001E-3	1.91E-3	1.97E-3	2.0400000000000001E-3	2.1199999999999999E-3	2.2000000000000001E-3	2.2899999999999999E-3	2.3800000000000002E-3	2.47E-3	2.5600000000000002E-3	2.65E-3	2.7299999999999998E-3	2.81E-3	2.8900000000000002E-3	2.96E-3	3.0200000000000001E-3	3.0799999999999998E-3	3.1199999999999999E-3	3.15E-3	3.1700000000000001E-3	3.1800000000000001E-3	3.1800000000000001E-3	3.1700000000000001E-3	3.14E-3	3.1099999999999999E-3	3.0599999999999998E-3	3.0100000000000001E-3	2.9399999999999999E-3	2.8800000000000002E-3	2.81E-3	2.7399999999999998E-3	2.66E-3	2.5899999999999999E-3	2.5100000000000001E-3	2.4299999999999999E-3	2.3500000000000001E-3	2.2799999999999999E-3	2.2000000000000001E-3	2.1199999999999999E-3	2.0400000000000001E-3	1.9599999999999999E-3	1.8799999999999999E-3	1.8E-3	1.72E-3	1.64E-3	1.56E-3	1.49E-3	1.42E-3	1.3500000000000001E-3	1.2800000000000001E-3	1.2199999999999999E-3	1.16E-3	1.1000000000000001E-3	1.0499999999999999E-3	9.9599999999999992E-4	9.4700000000000003E-4	9.01E-4	8.5800000000000004E-4	8.1800000000000004E-4	7.7999999999999999E-4	7.4399999999999998E-4	7.1100000000000004E-4	6.8099999999999996E-4	6.5200000000000002E-4	6.2500000000000001E-4	5.9999999999999995E-4	5.7600000000000001E-4	5.5400000000000002E-4	5.3300000000000005E-4	5.13E-4	4.9399999999999997E-4	4.7600000000000002E-4	4.5800000000000002E-4	4.4099999999999999E-4	4.2299999999999998E-4	4.06E-4	3.8999999999999999E-4	3.7300000000000001E-4	3.57E-4	3.4099999999999999E-4	3.2499999999999999E-4	3.0899999999999998E-4	2.9399999999999999E-4	2.7999999999999998E-4	2.6600000000000001E-4	2.5300000000000002E-4	2.41E-4	2.3000000000000001E-4	2.2000000000000001E-4	2.1100000000000001E-4	2.04E-4	1.9900000000000001E-4	1.95E-4	1.92E-4	1.9000000000000001E-4	1.9000000000000001E-4	1.9100000000000001E-4	1.92E-4	1.95E-4	1.9799999999999999E-4	2.0100000000000001E-4	2.04E-4	2.0699999999999999E-4	2.1000000000000001E-4	2.12E-4	2.14E-4	2.14E-4	2.13E-4	2.1000000000000001E-4	2.0599999999999999E-4	2.0000000000000001E-4	1.92E-4	1.83E-4	1.7100000000000001E-4	1.5899999999999999E-4	1.45E-4	1.2999999999999999E-4	1.1400000000000001E-4	9.8300000000000004E-5	8.2299999999999995E-5	6.6699999999999995E-5	5.1799999999999999E-5	3.79E-5	2.5400000000000001E-5	1.47E-5	6.5699999999999998E-6	1.9E-6	0	TCB	3.6	3.69	3.78	3.88	3.97	4.07	4.17	4.28	4.3899999999999997	4.49	4.6100000000000003	4.72	4.84	4.96	5.08	5.21	5.34	5.48	5.61	5.75	5.9	6.04	6.19	6.35	6.51	6.67	6.84	7.01	7.18	7.36	7.55	7.73	7.93	8.1300000000000008	8.33	8.5399999999999991	8.75	8.9700000000000006	9.19	9.42	9.66	9.9	10.1	10.4	10.7	10.9	11.2	11.5	11.8	12.1	12.4	12.7	13	13.3	13.6	14	14.3	14.7	15.1	15.4	15.8	16.2	16.600000000000001	17	17.5	17.899999999999999	18.3	18.8	19.3	19.7	20.2	20.7	21.3	21.8	22.3	22.9	23.5	24.1	24.7	25.3	25.9	26.6	27.2	27.9	28.6	29.3	30	30.8	31.6	32.299999999999997	33.200000000000003	34	34.799999999999997	35.700000000000003	36.6	37.5	38.4	39.4	40.4	41.4	42.4	43.5	44.6	45.7	46.8	48	49.2	50.4	51.7	53	54.3	55.7	57	58.5	59.9	61.4	63	64.5	66.099999999999994	67.8	69.5	71.2	73	74.8	76.7	78.599999999999994	80.599999999999994	82.6	84.6	86.8	88.9	91.1	93.4	95.8	98.1	101	103	106	108	111	114	117	120	123	126	129	132	135	139	142	146	149	153	157	161	165	169	173	177	182	186	191	196	201	206	211	216	222	227	233	239	245	251	257	263	270	277	284	291	298	305	313	321	329	337	345	354	363	372	381	391	400	410	421	431	442	453	464	476	488	0	2.7900000000000001E-4	2.2799999999999999E-3	7.1300000000000001E-3	1.4800000000000001E-2	2.4400000000000002E-2	3.3599999999999998E-2	4.2200000000000001E-2	0.05	5.67E-2	6.2399999999999997E-2	6.6600000000000006E-2	6.9400000000000003E-2	7.0900000000000005E-2	7.1199999999999999E-2	7.0199999999999999E-2	6.8199999999999997E-2	6.5299999999999997E-2	6.1699999999999998E-2	5.74E-2	5.2600000000000001E-2	4.7600000000000003E-2	4.24E-2	3.7100000000000001E-2	3.1899999999999998E-2	2.69E-2	2.23E-2	1.7999999999999999E-2	1.4200000000000001E-2	1.09E-2	8.1700000000000002E-3	6.0400000000000002E-3	4.5199999999999997E-3	3.5899999999999999E-3	3.2299999999999998E-3	3.3999999999999998E-3	4.0000000000000001E-3	4.9800000000000001E-3	6.2199999999999998E-3	7.62E-3	9.0399999999999994E-3	1.04E-2	1.1599999999999999E-2	1.26E-2	1.3299999999999999E-2	1.3599999999999999E-2	1.37E-2	1.35E-2	1.2999999999999999E-2	1.23E-2	1.14E-2	1.0500000000000001E-2	9.41E-3	8.3499999999999998E-3	7.3200000000000001E-3	6.3299999999999997E-3	5.4200000000000003E-3	4.5999999999999999E-3	3.8800000000000002E-3	3.2499999999999999E-3	2.7399999999999998E-3	2.32E-3	2E-3	1.7600000000000001E-3	1.5900000000000001E-3	1.48E-3	1.4300000000000001E-3	1.4300000000000001E-3	1.4499999999999999E-3	1.5E-3	1.57E-3	1.65E-3	1.73E-3	1.82E-3	1.91E-3	1.99E-3	2.0799999999999998E-3	2.16E-3	2.2499999999999998E-3	2.33E-3	2.4099999999999998E-3	2.49E-3	2.5600000000000002E-3	2.64E-3	2.7000000000000001E-3	2.7699999999999999E-3	2.82E-3	2.8700000000000002E-3	2.9099999999999998E-3	2.9399999999999999E-3	2.96E-3	2.98E-3	2.98E-3	2.97E-3	2.9499999999999999E-3	2.9199999999999999E-3	2.8800000000000002E-3	2.8300000000000001E-3	2.7799999999999999E-3	2.7200000000000002E-3	2.65E-3	2.5899999999999999E-3	2.5100000000000001E-3	2.4399999999999999E-3	2.3700000000000001E-3	2.2899999999999999E-3	2.2200000000000002E-3	2.14E-3	2.0699999999999998E-3	1.99E-3	1.91E-3	1.8400000000000001E-3	1.7600000000000001E-3	1.6900000000000001E-3	1.6100000000000001E-3	1.5399999999999999E-3	1.47E-3	1.4E-3	1.33E-3	1.2700000000000001E-3	1.1999999999999999E-3	1.15E-3	1.09E-3	1.0300000000000001E-3	9.8299999999999993E-4	9.3400000000000004E-4	8.8800000000000001E-4	8.4500000000000005E-4	8.0400000000000003E-4	7.6499999999999995E-4	7.2800000000000002E-4	6.9399999999999996E-4	6.6100000000000002E-4	6.3000000000000003E-4	6.02E-4	5.7399999999999997E-4	5.4799999999999998E-4	5.2400000000000005E-4	5.0100000000000003E-4	4.7899999999999999E-4	4.5800000000000002E-4	4.3800000000000002E-4	4.2000000000000002E-4	4.0200000000000001E-4	3.8400000000000001E-4	3.68E-4	3.5199999999999999E-4	3.3599999999999998E-4	3.21E-4	3.0600000000000001E-4	2.92E-4	2.7900000000000001E-4	2.6499999999999999E-4	2.5300000000000002E-4	2.41E-4	2.2900000000000001E-4	2.1800000000000001E-4	2.0699999999999999E-4	1.9799999999999999E-4	1.8900000000000001E-4	1.8000000000000001E-4	1.73E-4	1.6699999999999999E-4	1.6100000000000001E-4	1.5699999999999999E-4	1.5300000000000001E-4	1.4999999999999999E-4	1.4799999999999999E-4	1.46E-4	1.46E-4	1.45E-4	1.45E-4	1.45E-4	1.45E-4	1.46E-4	1.46E-4	1.45E-4	1.44E-4	1.4300000000000001E-4	1.4100000000000001E-4	1.3799999999999999E-4	1.3300000000000001E-4	1.2799999999999999E-4	1.22E-4	1.15E-4	1.08E-4	9.9099999999999996E-5	8.9900000000000003E-5	8.0199999999999998E-5	7.0300000000000001E-5	6.02E-5	5.02E-5	4.0500000000000002E-5	3.1399999999999998E-5	2.2900000000000001E-5	1.5299999999999999E-5	8.8200000000000003E-6	3.9500000000000003E-6	1.1400000000000001E-6	0	TCB-TU750	3.6	3.6899109999999999	3.7820670000000001	3.8765239999999999	3.973341	4.0725759999999998	4.1742889999999999	4.278543	4.3853999999999997	4.4949260000000004	4.6071869999999997	4.7222530000000003	4.840192	4.9610760000000003	5.0849799999999998	5.2119780000000002	5.3421479999999999	5.4755690000000001	5.6123219999999998	5.752491	5.8961600000000001	6.0434169999999998	6.1943530000000004	6.3490580000000003	6.5076260000000001	6.6701550000000003	6.8367430000000002	7.0074920000000001	7.1825049999999999	7.3618889999999997	7.5457539999999996	7.73421	7.9273730000000002	8.1253609999999998	8.3282930000000004	8.5362930000000006	8.7494879999999995	8.9680079999999993	9.1919850000000007	9.421557	9.6568609999999993	9.8980429999999995	10.145250000000001	10.398630000000001	10.658329999999999	10.924530000000001	11.197369999999999	11.477029999999999	11.763669999999999	12.05747	12.358599999999999	12.667260000000001	12.98363	13.3079	13.64026	13.980930000000001	14.330109999999999	14.688000000000001	15.05484	15.43083	15.81622	16.21123	16.616109999999999	17.031099999999999	17.45646	17.892430000000001	18.339300000000001	18.797329999999999	19.26679	19.747990000000001	20.24119	20.74672	21.264869999999998	21.795970000000001	22.340319999999998	22.89828	23.47017	24.056339999999999	24.657150000000001	25.272960000000001	25.904160000000001	26.551120000000001	27.21424	27.893920000000001	28.59057	29.30463	30.03651	30.78668	31.555579999999999	32.343690000000002	33.151479999999999	33.979439999999997	34.82808	35.697920000000003	36.589480000000002	37.503309999999999	38.439959999999999	39.4	40.38402	41.392620000000001	42.426409999999997	43.48601	44.57208	45.685279999999999	46.826270000000001	47.99577	49.194470000000003	50.423110000000001	51.682429999999997	52.973210000000002	54.296219999999998	55.652279999999998	57.042200000000001	58.466839999999998	59.927059999999997	61.423749999999998	62.957819999999998	64.530199999999994	66.141850000000005	67.793750000000003	69.486909999999995	71.222359999999995	73.001149999999996	74.824359999999999	76.693110000000004	78.608530000000002	80.571789999999993	82.584090000000003	84.646640000000005	86.7607	88.92756	91.148539999999997	93.424989999999994	95.758290000000002	98.149870000000007	100.60120000000001	103.11369999999999	105.68899999999999	108.32859999999999	111.0341	113.80719999999999	116.64960000000001	119.5629	122.54900000000001	125.6097	128.74680000000001	131.9623	135.25800000000001	138.6361	142.0986	145.64750000000001	149.2851	153.01349999999999	156.83510000000001	160.75200000000001	164.76679999999999	168.8819	173.09979999999999	177.423	181.85409999999999	186.39599999999999	191.05119999999999	195.8228	200.71350000000001	205.72630000000001	210.86439999999999	216.13069999999999	221.52860000000001	227.06129999999999	232.73220000000001	238.54480000000001	244.5025	250.60890000000001	256.86790000000002	263.28320000000002	269.85879999999997	276.59859999999998	283.50659999999999	290.58730000000003	297.84469999999999	305.28339999999997	312.90789999999998	320.72289999999998	328.733	336.94310000000002	345.35829999999999	353.9837	362.8245	371.8861	381.17399999999998	390.69389999999999	400.45150000000001	410.4529	420.70400000000001	431.21109999999999	441.98070000000001	453.01920000000001	464.33350000000002	475.93029999999999	487.81670000000003	0	7.9458260000000002E-5	6.4222010000000002E-4	2.032173E-3	4.3382500000000001E-3	7.3506880000000002E-3	1.0675250000000001E-2	1.419492E-2	1.7791419999999999E-2	2.1347850000000002E-2	2.4751510000000001E-2	2.7855620000000001E-2	3.0570070000000001E-2	3.2822610000000002E-2	3.4543079999999997E-2	3.569058E-2	3.6232239999999999E-2	3.6149390000000003E-2	3.5460520000000002E-2	3.416114E-2	3.229079E-2	2.9892720000000001E-2	2.7001560000000001E-2	2.3765970000000001E-2	2.0206249999999999E-2	1.6487720000000001E-2	1.2782389999999999E-2	9.3170240000000001E-3	6.1581079999999998E-3	3.6715340000000002E-3	1.8869340000000001E-3	7.4198720000000001E-4	2.2042399999999999E-4	5.4326020000000003E-5	1.488519E-5	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	1.0081450000000001E-7	1.0044019999999999E-6	6.711376E-6	1.8132570000000001E-5	4.1689310000000002E-5	8.2179820000000004E-5	1.4054359999999999E-4	2.1163709999999999E-4	2.917943E-4	3.7616229999999997E-4	4.6057470000000002E-4	5.4113130000000003E-4	6.1677569999999998E-4	6.8455559999999998E-4	7.440309E-4	7.9473239999999995E-4	8.3629310000000003E-4	8.6811180000000003E-4	8.8978219999999995E-4	9.0171000000000001E-4	9.0494730000000002E-4	9.003409E-4	8.8900640000000005E-4	8.7209750000000002E-4	8.5142750000000004E-4	8.2871959999999999E-4	8.0626639999999996E-4	7.8504870000000002E-4	7.6581000000000002E-4	7.4900499999999996E-4	7.3417860000000003E-4	7.2120180000000004E-4	7.0962819999999998E-4	6.9897320000000005E-4	6.8875239999999997E-4	6.7840659999999998E-4	6.672351E-4	6.5473479999999997E-4	6.4070030000000001E-4	6.2476800000000005E-4	6.0725039999999996E-4	5.8844289999999998E-4	5.6868619999999996E-4	5.4819639999999995E-4	5.2731770000000004E-4	5.060978E-4	4.8459479999999998E-4	4.628136E-4	4.411587E-4	4.1955660000000001E-4	3.9851280000000001E-4	3.784975E-4	3.6008250000000002E-4	3.4328510000000001E-4	3.288748E-4	3.1676300000000002E-4	3.0679090000000002E-4	2.9884239999999998E-4	2.926022E-4	2.8776920000000002E-4	2.840025E-4	2.8093440000000002E-4	2.7823749999999998E-4	2.7559490000000003E-4	2.7272560000000002E-4	2.6937489999999999E-4	2.6545300000000002E-4	2.6074760000000002E-4	2.5525759999999999E-4	2.490107E-4	2.4209390000000001E-4	2.3460690000000001E-4	2.2676639999999999E-4	2.1863399999999999E-4	2.1025030000000001E-4	2.0165539999999999E-4	1.9283350000000001E-4	1.837699E-4	1.7444140000000001E-4	1.6483000000000001E-4	1.549144E-4	1.4469409999999999E-4	1.3417370000000001E-4	1.233683E-4	1.1235910000000001E-4	1.011674E-4	8.9901210000000007E-5	7.8669400000000003E-5	6.756528E-5	5.683877E-5	4.6559679999999999E-5	3.6987760000000002E-5	2.8339549999999999E-5	2.0861610000000001E-5	1.4482670000000001E-5	9.4568140000000006E-6	5.7022530000000002E-6	3.0664540000000002E-6	1.454099E-6	5.7218819999999997E-7	1.589625E-7	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	TCB-TU650	3.6	3.6899109999999999	3.7820670000000001	3.8765239999999999	3.973341	4.0725759999999998	4.1742889999999999	4.278543	4.3853999999999997	4.4949260000000004	4.6071869999999997	4.7222530000000003	4.840192	4.9610760000000003	5.0849799999999998	5.2119780000000002	5.3421479999999999	5.4755690000000001	5.6123219999999998	5.752491	5.8961600000000001	6.0434169999999998	6.1943530000000004	6.3490580000000003	6.5076260000000001	6.6701550000000003	6.8367430000000002	7.0074920000000001	7.1825049999999999	7.3618889999999997	7.5457539999999996	7.73421	7.9273730000000002	8.1253609999999998	8.3282930000000004	8.5362930000000006	8.7494879999999995	8.9680079999999993	9.1919850000000007	9.421557	9.6568609999999993	9.8980429999999995	10.145250000000001	10.398630000000001	10.658329999999999	10.924530000000001	11.197369999999999	11.477029999999999	11.763669999999999	12.05747	12.358599999999999	12.667260000000001	12.98363	13.3079	13.64026	13.980930000000001	14.330109999999999	14.688000000000001	15.05484	15.43083	15.81622	16.21123	16.616109999999999	17.031099999999999	17.45646	17.892430000000001	18.339300000000001	18.797329999999999	19.26679	19.747990000000001	20.24119	20.74672	21.264869999999998	21.795970000000001	22.340319999999998	22.89828	23.47017	24.056339999999999	24.657150000000001	25.272960000000001	25.904160000000001	26.551120000000001	27.21424	27.893920000000001	28.59057	29.30463	30.03651	30.78668	31.555579999999999	32.343690000000002	33.151479999999999	33.979439999999997	34.82808	35.697920000000003	36.589480000000002	37.503309999999999	38.439959999999999	39.4	40.38402	41.392620000000001	42.426409999999997	43.48601	44.57208	45.685279999999999	46.826270000000001	47.99577	49.194470000000003	50.423110000000001	51.682429999999997	52.973210000000002	54.296219999999998	55.652279999999998	57.042200000000001	58.466839999999998	59.927059999999997	61.423749999999998	62.957819999999998	64.530199999999994	66.141850000000005	67.793750000000003	69.486909999999995	71.222359999999995	73.001149999999996	74.824359999999999	76.693110000000004	78.608530000000002	80.571789999999993	82.584090000000003	84.646640000000005	86.7607	88.92756	91.148539999999997	93.424989999999994	95.758290000000002	98.149870000000007	100.60120000000001	103.11369999999999	105.68899999999999	108.32859999999999	111.0341	113.80719999999999	116.64960000000001	119.5629	122.54900000000001	125.6097	128.74680000000001	131.9623	135.25800000000001	138.6361	142.0986	145.64750000000001	149.2851	153.01349999999999	156.83510000000001	160.75200000000001	164.76679999999999	168.8819	173.09979999999999	177.423	181.85409999999999	186.39599999999999	191.05119999999999	195.8228	200.71350000000001	205.72630000000001	210.86439999999999	216.13069999999999	221.52860000000001	227.06129999999999	232.73220000000001	238.54480000000001	244.5025	250.60890000000001	256.86790000000002	263.28320000000002	269.85879999999997	276.59859999999998	283.50659999999999	290.58730000000003	297.84469999999999	305.28339999999997	312.90789999999998	320.72289999999998	328.733	336.94310000000002	345.35829999999999	353.9837	362.8245	371.8861	381.17399999999998	390.69389999999999	400.45150000000001	410.4529	420.70400000000001	431.21109999999999	441.98070000000001	453.01920000000001	464.33350000000002	475.93029999999999	487.81670000000003	0	2.3536029999999999E-4	1.9226320000000001E-3	6.010268E-3	1.236571E-2	2.0252300000000001E-2	2.7529769999999999E-2	3.3994160000000002E-2	3.9475059999999999E-2	4.3748570000000001E-2	4.6943430000000001E-2	4.8775880000000001E-2	4.9383040000000003E-2	4.891968E-2	4.7510040000000003E-2	4.5338150000000001E-2	4.2575229999999999E-2	3.9392440000000001E-2	3.5944480000000001E-2	3.2385700000000003E-2	2.8833549999999999E-2	2.5390530000000001E-2	2.2145350000000001E-2	1.9125699999999999E-2	1.6397709999999999E-2	1.396741E-2	1.183434E-2	9.9971569999999996E-3	8.4218560000000001E-3	7.0944759999999997E-3	5.9829690000000003E-3	5.0579520000000001E-3	4.292049E-3	3.66089E-3	3.1423480000000001E-3	2.7183020000000001E-3	2.3755059999999999E-3	2.1001320000000002E-3	1.8828969999999999E-3	1.715301E-3	1.5898010000000001E-3	1.500244E-3	1.4405469999999999E-3	1.40565E-3	1.39095E-3	1.39219E-3	1.4061099999999999E-3	1.429182E-3	1.4587549999999999E-3	1.4924840000000001E-3	1.5282200000000001E-3	1.564272E-3	1.5991309999999999E-3	1.6315710000000001E-3	1.660728E-3	1.6857109999999999E-3	1.706059E-3	1.7214019999999999E-3	1.731546E-3	1.736764E-3	1.7370269999999999E-3	1.7328059999999999E-3	1.7245870000000001E-3	1.7128499999999999E-3	1.698581E-3	1.6822510000000001E-3	1.664813E-3	1.647206E-3	1.630275E-3	1.6151760000000001E-3	1.6027649999999999E-3	1.594009E-3	1.5897229999999999E-3	1.5906620000000001E-3	1.597361E-3	1.6102499999999999E-3	1.6295350000000001E-3	1.654888E-3	1.686314E-3	1.723151E-3	1.764718E-3	1.8102229999999999E-3	1.8583899999999999E-3	1.908346E-3	1.958886E-3	2.0088950000000001E-3	2.057335E-3	2.1031829999999998E-3	2.1455189999999998E-3	2.183501E-3	2.2164379999999998E-3	2.2436959999999999E-3	2.2648910000000002E-3	2.279709E-3	2.287964E-3	2.2896819999999999E-3	2.2848090000000001E-3	2.2735640000000001E-3	2.2561870000000002E-3	2.2329960000000001E-3	2.2044899999999999E-3	2.1710430000000001E-3	2.133158E-3	2.0913170000000001E-3	2.0459810000000001E-3	1.997684E-3	1.9468510000000001E-3	1.8939670000000001E-3	1.8394679999999999E-3	1.783771E-3	1.7271700000000001E-3	1.6700129999999999E-3	1.612552E-3	1.554995E-3	1.497553E-3	1.440368E-3	1.3835710000000001E-3	1.3272799999999999E-3	1.2716299999999999E-3	1.216717E-3	1.1626780000000001E-3	1.1096389999999999E-3	1.0577200000000001E-3	1.0070770000000001E-3	9.5780840000000002E-4	9.1005860000000004E-4	8.6395470000000002E-4	8.1961920000000001E-4	7.7710880000000004E-4	7.3653339999999996E-4	6.9792460000000004E-4	6.6129640000000005E-4	6.2666100000000004E-4	5.9399650000000002E-4	5.6327549999999997E-4	5.3445490000000005E-4	5.0746389999999997E-4	4.8224820000000002E-4	4.5872090000000001E-4	4.3679560000000001E-4	4.1638359999999998E-4	3.9736490000000002E-4	3.796529E-4	3.6312809999999998E-4	3.4767499999999998E-4	3.331788E-4	3.1952599999999999E-4	3.0659969999999998E-4	2.9430480000000001E-4	2.8255670000000002E-4	2.7127679999999998E-4	2.6040230000000001E-4	2.49876E-4	2.3965020000000001E-4	2.2968850000000001E-4	2.199542E-4	2.104237E-4	2.0107609999999999E-4	1.9189519999999999E-4	1.828763E-4	1.740081E-4	1.652914E-4	1.5672820000000001E-4	1.483206E-4	1.4008299999999999E-4	1.320185E-4	1.241417E-4	1.164655E-4	1.090015E-4	1.0176E-4	9.4750250000000003E-5	8.7979839999999997E-5	8.1455290000000005E-5	7.5181969999999997E-5	6.9164200000000004E-5	6.3405350000000004E-5	5.7907849999999998E-5	5.2673309999999997E-5	4.7702540000000002E-5	4.2995630000000001E-5	3.8551979999999998E-5	3.437042E-5	3.044915E-5	2.6785910000000001E-5	2.3377880000000001E-5	2.0221820000000001E-5	1.7314350000000001E-5	1.465103E-5	1.222828E-5	1.00407E-5	8.0834570000000005E-6	6.3512390000000003E-6	4.8408460000000003E-6	3.548003E-6	2.4593790000000002E-6	1.573529E-6	8.7483670000000001E-7	3.8445679999999998E-7	1.111375E-7	0	Pore Width, Å 


Differential Pore Volume, (cm3/g)/Å




B

Measured CO2	1.17895E-4	2.81585E-4	4.7416500000000002E-4	6.9108500000000003E-4	9.2895100000000002E-4	1.1883799999999999E-3	1.5503400000000001E-3	1.9436200000000001E-3	2.3645200000000002E-3	2.8117400000000001E-3	3.2819799999999999E-3	3.7732E-3	4.28248E-3	4.8086700000000001E-3	5.3513500000000004E-3	5.9079299999999996E-3	6.4771400000000002E-3	7.0580699999999996E-3	7.6489100000000001E-3	8.2489099999999999E-3	8.8589099999999994E-3	9.4772299999999997E-3	1.0101799999999999E-2	1.0735E-2	1.1374499999999999E-2	1.20193E-2	1.2669400000000001E-2	1.3324300000000001E-2	1.39834E-2	1.46482E-2	1.53066E-2	1.5978800000000001E-2	1.66549E-2	1.7333000000000001E-2	1.8012299999999998E-2	1.8687200000000001E-2	1.9371099999999999E-2	2.0056500000000001E-2	2.07466E-2	2.1434700000000001E-2	2.2127299999999999E-2	2.2818700000000001E-2	2.35141E-2	2.4208400000000001E-2	2.48939E-2	2.55926E-2	2.6292099999999999E-2	2.69964E-2	2.7688600000000001E-2	2.83833E-2	2.90861E-2	2.9789800000000002E-2	3.04789E-2	2.95689	5.5720700000000001	7.9515599999999997	10.1395	12.160500000000001	14.0433	16.293500000000002	18.3813	20.318100000000001	22.112200000000001	23.782800000000002	25.345400000000001	26.803899999999999	28.1722	29.4542	30.6632	31.803100000000001	32.878300000000003	33.899000000000001	34.871699999999997	35.790900000000001	36.6646	37.5047	38.299399999999999	39.0608	39.793700000000001	40.496400000000001	41.1706	41.8202	42.444299999999998	43.091099999999997	43.674500000000002	44.235199999999999	44.781399999999998	45.312600000000003	45.860100000000003	46.363900000000001	46.852600000000002	47.328099999999999	47.795000000000002	48.248100000000001	48.6952	49.118200000000002	49.5379	49.989100000000001	50.385899999999999	50.775599999999997	51.1464	51.552199999999999	51.927199999999999	52.291200000000003	52.643799999999999	53.037700000000001	Fit	1.17895E-4	2.81585E-4	4.7416500000000002E-4	6.9108500000000003E-4	9.2895100000000002E-4	1.1883799999999999E-3	1.5503400000000001E-3	1.9436200000000001E-3	2.3645200000000002E-3	2.8117400000000001E-3	3.2819799999999999E-3	3.7732E-3	4.28248E-3	4.8086700000000001E-3	5.3513500000000004E-3	5.9079299999999996E-3	6.4771400000000002E-3	7.0580699999999996E-3	7.6489100000000001E-3	8.2489099999999999E-3	8.8589099999999994E-3	9.4772299999999997E-3	1.0101799999999999E-2	1.0735E-2	1.1374499999999999E-2	1.20193E-2	1.2669400000000001E-2	1.3324300000000001E-2	1.39834E-2	1.46482E-2	1.53066E-2	1.5978800000000001E-2	1.66549E-2	1.7333000000000001E-2	1.8012299999999998E-2	1.8687200000000001E-2	1.9371099999999999E-2	2.0056500000000001E-2	2.07466E-2	2.1434700000000001E-2	2.2127299999999999E-2	2.2818700000000001E-2	2.35141E-2	2.4208400000000001E-2	2.48939E-2	2.55926E-2	2.6292099999999999E-2	2.69964E-2	2.7688600000000001E-2	2.83833E-2	2.90861E-2	2.9789800000000002E-2	3.04789E-2	1.1914560000000001	3.07131	5.4975040000000002	8.1396250000000006	10.68125	13.07287	15.89555	18.469989999999999	20.810390000000002	22.936050000000002	24.879429999999999	26.657389999999999	28.252459999999999	29.708880000000001	31.045400000000001	32.261769999999999	33.36159	34.375169999999997	35.31812	36.185839999999999	36.968069999999997	37.718940000000003	38.3902	39.031610000000001	39.62191	40.179470000000002	40.693719999999999	41.190890000000003	41.636620000000001	42.086210000000001	42.473579999999998	42.861890000000002	43.238190000000003	43.572690000000001	43.907780000000002	44.224780000000003	44.51332	44.802500000000002	45.08952	45.337229999999998	45.586550000000003	45.835439999999998	46.067439999999998	46.281280000000002	46.49241	46.707610000000003	46.907290000000003	47.092619999999997	47.274760000000001	47.457560000000001	47.641260000000003	47.79965	47.954749999999997	Measured N2	8.8016099999999996E-3	4.1625000000000002E-2	7.4156799999999995E-2	7.7181E-2	0.102919	0.12617400000000001	0.15159300000000001	0.17602999999999999	0.20075999999999999	0.28639300000000001	0.37451200000000001	0.46276699999999998	0.55051300000000003	0.63842900000000002	0.72942700000000005	0.809554	0.89814799999999995	0.94792699999999996	59.940600000000003	66.811000000000007	68.474199999999996	68.768500000000003	69.672799999999995	70.372500000000002	70.9726	71.502899999999997	71.994500000000002	73.357600000000005	74.771900000000002	76.242900000000006	77.801599999999993	79.542100000000005	81.5792	83.633700000000005	86.5839	89.356200000000001	Fit	8.8016099999999996E-3	4.1625000000000002E-2	7.4156799999999995E-2	7.7181E-2	0.102919	0.12617400000000001	0.15159300000000001	0.17602999999999999	0.20075999999999999	0.28639300000000001	0.37451200000000001	0.46276699999999998	0.55051300000000003	0.63842900000000002	0.72942700000000005	0.809554	0.89814799999999995	0.94792699999999996	69.442009999999996	71.570679999999996	72.387320000000003	72.442989999999995	72.888819999999996	73.206299999999999	73.502139999999997	73.754940000000005	73.989059999999995	74.722830000000002	75.363550000000004	75.93065	76.670209999999997	78.237359999999995	80.543329999999997	82.68244	85.981809999999996	88.720950000000002	Relative pressure 


Amounte adsorbed, cm3/g (STP)




CB

Measured CO2	1.00555E-4	2.3250899999999999E-4	3.8244800000000002E-4	5.4666999999999997E-4	7.2308599999999995E-4	9.0999099999999997E-4	1.10629E-3	1.3109300000000001E-3	1.5236200000000001E-3	1.7432000000000001E-3	1.9687099999999998E-3	2.20017E-3	2.4369000000000001E-3	2.6783000000000002E-3	2.9245899999999999E-3	3.1746600000000002E-3	3.4295200000000001E-3	3.6866999999999998E-3	3.94744E-3	4.2120400000000002E-3	4.4771699999999999E-3	4.7476300000000001E-3	5.0210200000000002E-3	5.2961099999999997E-3	5.5740599999999996E-3	5.8540299999999997E-3	6.1364100000000001E-3	6.4205E-3	6.7058600000000001E-3	6.99419E-3	7.2833200000000002E-3	7.5748200000000003E-3	7.8618000000000004E-3	8.1563199999999999E-3	8.4515000000000007E-3	8.7484599999999996E-3	9.0466399999999999E-3	9.3456900000000002E-3	9.6462200000000005E-3	9.9474000000000003E-3	1.02509E-2	1.05542E-2	1.08597E-2	1.11658E-2	1.1471800000000001E-2	1.1779299999999999E-2	1.20879E-2	1.23964E-2	1.2706200000000001E-2	1.30177E-2	1.33285E-2	1.3640599999999999E-2	1.4088E-2	1.4527E-2	1.49786E-2	1.5431500000000001E-2	1.5885699999999999E-2	1.63412E-2	1.6796700000000001E-2	1.72537E-2	1.7712599999999998E-2	1.8171099999999999E-2	1.86307E-2	1.90945E-2	1.9559699999999999E-2	2.0015600000000001E-2	2.04767E-2	2.09406E-2	2.1405899999999999E-2	2.18718E-2	2.2337900000000001E-2	2.2805499999999999E-2	2.3272899999999999E-2	2.3739199999999998E-2	2.42057E-2	2.4673500000000001E-2	2.51416E-2	2.5609900000000001E-2	2.6078E-2	2.6547500000000002E-2	2.70193E-2	2.7489199999999998E-2	2.7961699999999999E-2	2.8433099999999999E-2	2.8911900000000001E-2	2.9390199999999998E-2	2.9829899999999999E-2	3.02983E-2	2.6559599999999999	4.9594399999999998	7.0502500000000001	8.9723699999999997	10.748100000000001	12.403700000000001	13.9519	15.4039	16.770499999999998	18.0594	19.286100000000001	20.4453	21.549299999999999	22.5992	23.601299999999998	24.5579	25.4709	26.354299999999999	27.203399999999998	28.0139	28.810400000000001	29.563400000000001	30.287099999999999	30.9923	31.670500000000001	32.326700000000002	32.961599999999997	33.579599999999999	34.177100000000003	34.753100000000003	35.323500000000003	35.865299999999998	36.433700000000002	36.9529	37.456800000000001	37.946199999999997	38.423900000000003	38.894199999999998	39.348799999999997	39.798200000000001	40.2271	40.651200000000003	41.063000000000002	41.467799999999997	41.869599999999998	42.261099999999999	42.639800000000001	43.017000000000003	43.382899999999999	43.735599999999998	44.084099999999999	44.4268	44.912700000000001	45.447099999999999	45.899799999999999	46.343499999999999	46.776499999999999	47.201900000000002	47.6233	48.028100000000002	48.415500000000002	48.811900000000001	49.187800000000003	49.532200000000003	49.860199999999999	50.256500000000003	50.616900000000001	50.9557	51.290399999999998	51.612900000000003	51.938000000000002	52.251800000000003	52.560400000000001	52.869799999999998	53.169800000000002	53.462499999999999	53.755600000000001	54.036299999999997	54.319800000000001	54.601700000000001	54.870800000000003	55.143700000000003	55.405900000000003	55.6663	55.8797	56.091900000000003	56.497100000000003	56.774700000000003	Fit	1.00555E-4	2.3250899999999999E-4	3.8244800000000002E-4	5.4666999999999997E-4	7.2308599999999995E-4	9.0999099999999997E-4	1.10629E-3	1.3109300000000001E-3	1.5236200000000001E-3	1.7432000000000001E-3	1.9687099999999998E-3	2.20017E-3	2.4369000000000001E-3	2.6783000000000002E-3	2.9245899999999999E-3	3.1746600000000002E-3	3.4295200000000001E-3	3.6866999999999998E-3	3.94744E-3	4.2120400000000002E-3	4.4771699999999999E-3	4.7476300000000001E-3	5.0210200000000002E-3	5.2961099999999997E-3	5.5740599999999996E-3	5.8540299999999997E-3	6.1364100000000001E-3	6.4205E-3	6.7058600000000001E-3	6.99419E-3	7.2833200000000002E-3	7.5748200000000003E-3	7.8618000000000004E-3	8.1563199999999999E-3	8.4515000000000007E-3	8.7484599999999996E-3	9.0466399999999999E-3	9.3456900000000002E-3	9.6462200000000005E-3	9.9474000000000003E-3	1.02509E-2	1.05542E-2	1.08597E-2	1.11658E-2	1.1471800000000001E-2	1.1779299999999999E-2	1.20879E-2	1.23964E-2	1.2706200000000001E-2	1.30177E-2	1.33285E-2	1.3640599999999999E-2	1.4088E-2	1.4527E-2	1.49786E-2	1.5431500000000001E-2	1.5885699999999999E-2	1.63412E-2	1.6796700000000001E-2	1.72537E-2	1.7712599999999998E-2	1.8171099999999999E-2	1.86307E-2	1.90945E-2	1.9559699999999999E-2	2.0015600000000001E-2	2.04767E-2	2.09406E-2	2.1405899999999999E-2	2.18718E-2	2.2337900000000001E-2	2.2805499999999999E-2	2.3272899999999999E-2	2.3739199999999998E-2	2.42057E-2	2.4673500000000001E-2	2.51416E-2	2.5609900000000001E-2	2.6078E-2	2.6547500000000002E-2	2.70193E-2	2.7489199999999998E-2	2.7961699999999999E-2	2.8433099999999999E-2	2.8911900000000001E-2	2.9390199999999998E-2	2.9829899999999999E-2	3.02983E-2	1.1232409999999999	2.771906	4.8429539999999998	7.1669890000000001	9.4975260000000006	11.704739999999999	13.758649999999999	15.64827	17.417819999999999	19.041799999999999	20.553840000000001	21.967130000000001	23.290520000000001	24.52984	25.67285	26.750150000000001	27.780449999999998	28.7301	29.622250000000001	30.488890000000001	31.262730000000001	32.041559999999997	32.7361	33.434959999999997	34.055199999999999	34.676090000000002	35.247300000000003	35.795679999999997	36.334200000000003	36.816070000000003	37.299289999999999	37.759430000000002	38.173009999999998	38.597450000000002	39.002719999999997	39.370489999999997	39.739759999999997	40.110120000000002	40.430619999999998	40.750250000000001	41.072339999999997	41.38241	41.6599	41.937939999999998	42.215890000000002	42.489249999999998	42.72878	42.968240000000002	43.2087	43.450490000000002	43.670490000000001	43.877119999999998	44.17333	44.463970000000003	44.737659999999998	44.993279999999999	45.249639999999999	45.506729999999997	45.737909999999999	45.95776	46.178530000000002	46.39911	46.608499999999999	46.798999999999999	46.990090000000002	47.177349999999997	47.366750000000003	47.541420000000002	47.704210000000003	47.86721	48.030290000000001	48.193890000000003	48.351730000000003	48.491100000000003	48.630519999999997	48.770330000000001	48.910229999999999	49.050190000000001	49.184060000000002	49.303759999999997	49.424050000000001	49.543849999999999	49.664319999999996	49.784500000000001	49.906570000000002	50.015999999999998	50.111750000000001	50.213760000000001	Measured N2	8.7168300000000001E-3	3.1637999999999999E-2	7.3961499999999999E-2	7.7306899999999998E-2	0.101618	0.12582499999999999	0.150975	0.175675	0.20069999999999999	0.28662700000000002	0.375031	0.46295799999999998	0.550647	0.63873100000000005	0.72958400000000001	0.80973099999999998	0.89956999999999998	0.94921	58.896599999999999	65.061000000000007	67.407399999999996	67.693299999999994	68.5154	69.172200000000004	69.766199999999998	70.303399999999996	70.771600000000007	72.087900000000005	73.535600000000002	75.131	76.936899999999994	78.992800000000003	81.416899999999998	83.878799999999998	87.036600000000007	89.386899999999997	Fit	8.7168300000000001E-3	3.1637999999999999E-2	7.3961499999999999E-2	7.7306899999999998E-2	0.101618	0.12582499999999999	0.150975	0.175675	0.20069999999999999	0.28662700000000002	0.375031	0.46295799999999998	0.550647	0.63873100000000005	0.72958400000000001	0.80973099999999998	0.89956999999999998	0.94921	71.205010000000001	72.862960000000001	73.940179999999998	73.995410000000007	74.370890000000003	74.661810000000003	74.916849999999997	75.13673	75.337630000000004	75.940119999999993	76.451629999999994	76.887309999999999	77.300849999999997	77.822280000000006	79.089269999999999	81.260739999999998	85.470609999999994	87.879639999999995	Realative pressure 


Amount adsorbed, cm3/g (STP)
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