Gasification of Heavy Metal–Contaminated Biochar: Experimental Investigation and Thermodynamic Analysis

Nastaran Abbaspour*, Naeimeh Vali2, Towhid Gholizadeh3, Daniela Tomasetig4, Andrzej Szlęk5, Agnieszka Korus5, Franz winter1

1 Institute of Chemical, Environmental and Bioscience Engineering, TU Wien, Vienna, Austria

2Swedish Centre for Resource Recovery, University of Borås, Borås, Sweden

3Department of Power Engineering and Turbomachinery, Silesian University of Technology, Gliwice, Poland

4Institute of Chemical Technologies and Analytics, TU Wien, Vienna, Austria

5Department of Thermal Technology, Silesian University of Technology, Gliwice, Poland

List of contents:

S1. Gas evolution profiles for biochar gasification

S2. Dry-gas composition of the gaseous products from biochar gasification: effect of temperature on the average gas composition

S3. Dry-gas composition of the gaseous products from biochar gasification: effect of reaction time on the average gas composition

S4. Raman spectrum of  pyrolytic and activated birch biochars

Tables:

ST1. Content of inorganics in birch biomass harvested from the contaminated and uncontaminated areas

ST2. Summary of the activation tests

ST3. Elemental analysis of pyrolyzed and activated biochar (on a dry basis)

ST4. Moisture, ash and ultimate (elemental) analysis of contaminated birch biomass

ST5. List of elements and solution compound compositions included in the thermodynamic databases used for equilibrium modelling

ST6. Content of selected inorganics in pyrolyzed and activated biochars

ST7. BET surface area, total pore volume, and average pore diameter of activated biochars

S1. Gas evolution profiles for biochar gasification

S2. Dry-gas composition of the gaseous products from biochar gasification: effect of temperature on the average gas composition

S3. Dry-gas composition of the gaseous products from biochar gasification: effect of reaction time on the average gas composition

S4. Raman spectrum of  pyrolytic and activated birch biochars

ST1. Content of inorganics in birch harvested from the contaminated and uncontaminated areas [1]

| Elements | Contaminated Birch (mg/kg) | ± | Uncontaminated Birch (mg/kg) | ± |
| --- | --- | --- | --- | --- |
| Ag | 0.8 | 0 | 0.5 | 0.3 |
| Al | 92 | 10 | 65 | 11 |
| As | 2.3 | 0.1 | 1.2 | 0.3 |
| Ba | 15 | 0 | 29 | 0 |
| Ca | 4014 | 122 | 9109 | 811 |
| Cd | 88.9 | 2.8 | 1.2 | 0.1 |
| Co | 0.4 | 0 | 0.1 | 0.1 |
| Cr | 12 | 3 | 8 | 1 |
| Cu | 36 | 1 | 7 | 1 |
| Fe | 241 | 7 | 133 | 6 |
| K | 1567 | 28 | 2104 | 144 |
| Mg | 498 | 4 | 424 | 12 |
| Mn | 43 | 1 | 18 | 0 |
| Mo | 1.8 | 0.6 | 1.2 | 0.3 |
| Na | 239 | 6 | 233 | 17 |
| Ni | 6 | 2 | 3 | 0 |
| P | 454 | 2 | 501 | 7 |
| Pb | 1863 | 47 | 23 | 1 |
| Sb | 2.3 | 0.1 | 2.3 | 0.2 |
| Sn | 2.7 | 0.2 | 0 | 0.6 |
| Ti | 3.7 | 0.1 | 2.9 | 0.1 |
| Zn | 1580 | 39 | 308 | 41 |
| Si | 1130 | 260 | 951 | 250 |
| Hg | 0.094 | 0.002 | 0.01 | 0.001 |

ST2. Summary of the activation tests

| No | Biochar Type | Atmosphere | Temperature (℃) | Reaction time(min) | Abbreviation |
| --- | --- | --- | --- | --- | --- |
| 1 | CB | CO2 | 700 | 240 | TCB-CO2-700-240 |
| 2 | CB | 50/50 vol.% H2O/CO2 | 700 | 120 | TCB-H2O-700-120 |
| 3 | CB | CO2 | 800 | 120 | TCB-CO2-800-120 |
| 4 | CB | 50/50 vol.% H2O/CO2 | 800 | 60 | TCB-H2O-800-60 |
| 5 | CB | CO2 | 900 | 20 | TCB-CO2-900-20 |
| 6 | CB | 50/50 vol.% H2O/CO2 | 900 | 10 | TCB-H2O-900-10 |
| 7 | B | CO2 | 800 | 120 | TB-CO2-800-120 |
| 8 | B | 50/50 vol.% H2O/CO2 | 800 | 60 | TB-H2O-800-60 |

ST3. Elemental analysis of pyrolyzed and activated biochar (on a dry basis) [2]

| Sample name | C (Wt.%) | ± | H (Wt.%) | ± | N (Wt.%) | ± | S (Wt.%) | ± | O (Wt.%) | ± | Sum |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| B | 70.418 | 0.10 | 2.48 | 0.01 | 1.29 | 0.00 | 0.29 | 0.01 | 13.06 | 0.17 | 87.55 |
| CB | 70.790 | 0.03 | 2.11 | 0.02 | 1.01 | 0.01 | 0.65 | 0.01 | 12.24 | 0.10 | 86.81 |
| TB-H2O-800-60 | 66.92 | 0.16 | 0.89 | 0.01 | 0.81 | 0.00 | 0.00 | 0.00 | 17.92 | 0.86 | 86.56 |
| TB-CO2-800-120 | 71.00 | 0.02 | 0.77 | 0.01 | 1.89 | 0.01 | 0.03 | 0.01 | 16.81 | 0.38 | 90.51 |
| TCB-H2O-700-120 | 78.61 | 0.34 | 1.02 | 0.06 | 0.98 | 0.00 | 0.09 | 0.02 | 10.95 | 0.14 | 91.65 |
| TCB-CO2-700-240 | 77.42 | 0.33 | 0.92 | 0.02 | 1.67 | 0.02 | 0.14 | 0.02 | 12.18 | 0.13 | 92.34 |
| TCB-H2O-800-60 | 77.55 | 0.26 | 0.94 | 0.01 | 0.84 | 0.01 | 0.11 | 0.05 | 11.80 | 0.53 | 91.24 |
| TCB-CO2-800-120 | 77.57 | 0.17 | 0.74 | 0.01 | 1.76 | 0.01 | 0.11 | 0.04 | 12.32 | 1.19 | 92.50 |
| TCB-H2O-900-10 | 81.14 | 0.56 | 0.79 | 0.04 | 1.06 | 0.02 | 0.11 | 0.04 | 10.47 | 0.15 | 93.57 |
| TCB-CO2-900-20 | 81.50 | 0.47 | 0.83 | 0.14 | 1.36 | 0.02 | 0.14 | 0.05 | 10.21 | 0.47 | 94.03 |

ST4. Moisture, ash and ultimate (elemental) analysis of contaminated birch biomass

| Parameter | Value | Unit / basis |
| --- | --- | --- |
| Moisture | 3.13 | wt% (as received) |
| Ash | 3.3 | wt% (dry basis) |
| C | 49.8 | wt% (dry basis) |
| H | 6.61 | wt% (dry basis) |
| O | 41.14 | wt% (dry basis) |
| N | 0.72 | wt% (dry basis) |
| S | 0.53 | wt% (dry basis) |
| Cl | 0.11 | wt% (dry basis) |

ST5. List of elements and solution compound compositions included in the thermodynamic databases used for equilibrium modelling

| Parameter | Input data for thermodynamics equilibrium calculations |
| --- | --- |
| Elements | C, H, O, N, S, Cl, Al, Ca, Fe, K, Mg, Na, P, Si, As, Cd, Mo, Cr, Cu, Ni, Mn, Pb, Zn |
| Databases stoichiometric compounds | Fact PS, FT oxid, FTsalt |
| Databases gas compounds | Fact PS, HSCA |
| Solution phases | Nepheline (Na,K)AlSiO4), Feldspar (Na,K)AlSi3O8 - CaAl2Si2O8 Slag-A SiO2 + (Na,K)AlO2 + (Na2, K2, Cu2, Pb, Zn)O, Spinel (Al,Co,Cr,Fe,Mg,Ni,Zn)3O4, M2O3 (Corundum) (Fe,Al,Mn,Cr)2O, cPyrA, OliveA, MelA, LEU |

ST6. Content of selected inorganics in pyrolyzed and activated biochars [2]

| Sample name | Al (mg/kg) | ± | Ca (mg/kg) | ± | K(mg/kg) | ± | Pb (mg/kg) | ± | Zn (mg/kg) | ± |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CB | 330 | 2 | 20490 | 30 | 8130 | 10 | 6750 | 30 | 3920 | 13 |
| TCB-H2O-700-120 | 450 | 20 | 27700 | 1190 | 11700 | 360 | 11000 | 170 | 4830 | 80 |
| TCB-CO2-700-240 | 330 | 20 | 22300 | 930 | 10500 | 10 | 9500 | 100 | 5890 | 130 |
| TCB-H2O-800-60 | 590 | 10 | 39500 | 700 | 16700 | 100 | 11100 | 200 | 270 | 5 |
| TCB-CO2-800-120 | 710 | 20 | 37500 | 780 | 17400 | 360 | 8540 | 110 | 830 | 40 |
| TCB-H2O-900-10 | 540 | 10 | 24900 | 500 | 15100 | 370 | 1660 | 30 | 110 | 10 |
| TCB-CO2-900-20 | 340 | 10 | 20600 | 660 | 9470 | 220 | 3860 | 50 | 100 | 10 |

ST7. BET surface area, total pore volume, and average pore diameter of activated biochars

| Sample | S BET (m2/g) | Vt (cm3/g) | da (nm) |
| --- | --- | --- | --- |
| TCB-CO2-700-240 | 608.04 | 0.2900 | 1.3205 |
| TCB-H2O-700-120 | 609.83 | 0.4187 | 1.4606 |
| TCB-CO2-800-120 | 673.33 | 0.3214 | 1.3808 |
| TCB-H2O-800-60 | 617.44 | 0.3976 | 1.4976 |
| TCB-CO2-900-20 | 566.65 | 0.2813 | 1.3084 |
| TCB-H2O-900-10 | 580.01 | 0.2857 | 1.4986 |
| TB-CO2-800-120 | 597.03 | 0.2841 | 1.4133 |
| TB-H2O-800-60 | 533.44 | 0.3783 | 1.6741 |

References

[1]	Abbaspour N, Szlęk A, Winter F, Korus A. Kinetics of model tar decomposition over activated biochar from a heavy metal-contaminated area. Renew Energy 2025;253:123661. https://doi.org/10.1016/j.renene.2025.123661.

[2]	Abbaspour N, Jordan C, Tondl G, Wąsik P, Gholizadeh T, Tomasetig D, et al. Activated biochars from heavy metal-contaminated biomass for CO2 capture: Adsorption performance and dominant mechanisms. Journal of CO2 Utilization 2025;101:103217. https://doi.org/10.1016/j.jcou.2025.103217.

* Corresponding author: Nastaran Abbaspour, email: nastaran.abbaspour@tuwien.ac.at